# Featured Technical Topic Summary

# FGI Monthly Members Meeting

# Friday, August 7, 2026

TOPIC:	Field Testing and Repairs

Each month Tim Stark introduces a new technical topic for discussion and possible action. This month’s topic is: “Field Testing and Repairs”. This topic generated significant discussion with the main “take-aways” listed below.

Field Testing and Repairs

    - Seam peel and shear testing – how do you repair the holes from destructive sampling? Regulations require destructive sampling

    - Cut destructive samples in the middle of the seam; cut destructive samples from near anchor trench

    - Requirement of destructive sample every 500 ft was suggested by JP Giroud so not required

    - Extrusion weld is weaker than a thermal weld so take destructive samples near anchor trenches

    - IAGI is working on guidelines for testing patches and T-seams

    - Phone call on Sunday: Your liner is leaking? Ask if it is single or double-lined system. If double-lined system, easy because there is leak detection zone. If single lined system, it is difficult to determine if it is leaking, may be due to loss of fluid

    - Use smart welders that record welding data, such as, speed, temperature, pressure, etc.

    - Sample at end of the seam, not in the middle of the seam

    - How do you handle the repair for the destructive sample?

    - Do we need to conduct seam peel and shear tests? Yes condition change

    - Testing an extrusion weld? Take a destructive sample?

    - Concern is heat effects on geomembrane behavior with seaming

    - Destructive sample of extrusion? Is it required and problem is patching the extrusion weld

    - Perform conformance welds at beginning and end of seam? Conditions change with time so need more testing – changes in humidity

    - Review FGI factory and field seam testing requirements

    - How do we avoid patch over patch? What is most important parameter? Seam strength or leakage?

    - Consider size of the defect? Smaller patches only use vacuum box and not destructive sample

    - Repair must extend six inches past defect

    - If defect is less than six inches, only vacuum box especially if vacuum covers entire patch so no destructive sample

    - If defect is six inches or greater or long linear defect, hot air and extrusion weld the patch not two extrusion welds

    - Need repair specifications