SECTION 07 27 26 - FLUID-APPLIED MEMBRANE AIR BARRIERS

- GENERAL

  - SUMMARY

    - Section Includes:

      - Liquid-applied air and water-resistive barrier system.

    - Related Sections:

      - Division 01: Administrative, procedural, and temporary work requirements.

      - Section [03 30 00 - Cast-in-Place Concrete] __ __ - ______]: Concrete substrate to receive air barrier.

      - Section [04 22 00 - Concrete Unit Masonry] [__ __ __ - ______]: Masonry substrate to receive air barrier.

      - Section [06 16 00 - Sheathing] [__ __ __ - ______]: Sheathing substrate to receive air barrier.

  - SUBMITTALS

    - Action Submittals:

      - Product Data:  Submit manufacturer's technical data sheets, installation instructions, SDS, and warranty.

      - Samples: [12 x 12] [__ x __] inch ([300 x 300] [__ x __] mm) air barrier samples on representative substrate.

    - Informational Submittals:

      - Current ICC-ES Evaluation Report verifying fluid applied material conformance with AC 212.

      - Current Clean Air Gold product certification verifying conformance to ANSI/ BIFMA e3 standard credits 7.6.1, 7.6.2 and/or credit 7.6.3, which includes California Department of Public Health (CDPH) Standard Method v1.2 01350 (2017), as well as conformance to low-emitting materials for WELL and LEED.

      - Contractor qualifications.

  - QUALITY ASSURANCE

    - Installer Qualifications:

      - Minimum [2] [__] years experience in work of this Section.

      - [Licensed by ABAA to ABAA Quality Assurance Program.]

    - Preconstruction Conference:

      - Convene [__] weeks prior to commencing Work of this Section.

      - Attendees: [Owner,] [Architect,] [Contractor,] [Construction Manager,] installer, and air barrier manufacturer’s representative.

      - Review air barrier requirements and installation, special details, mockups, air leakage and bond testing, air barrier protection, and work scheduling.

    - Mockup:

      - Apply air barrier to verify details under submittals and to demonstrate tie-ins with adjoining construction, other termination conditions, and method of installation.

      - Size: [8] [__] feet wide x [8] [__] wide.

      - Incorporate backup wall construction, exterior cladding, window and door frame and sill, insulation, flashings, [building corner condition,] [junction with roof system] [foundation wall] [and] [typical penetrations and gaps].

      - Approved mockup [may] [may not] remain as part of the Work.

  - PROJECT CONDITIONS

    - Environmental Requirements:

      - Do not apply air barrier at temperatures below 0 degrees F (minus 18 degrees C) or if frost or moisture is present on surfaces to be coated.

  - WARRANTY

    - Provide manufactures [10] [15] [20] year material warranty.

- PRODUCTS

  - MANUFACTURERS

    - Contract Documents are based on products by Momentive Performance Materials, Inc., 260 Hudson River Rd., Waterford, NY 12188, (877) 943-7325, www.siliconesforbuilding.com.

  - MATERIALS

    - Fluid-Applied Air Barrier: Elemax™ 2600.

    - Liquid Flashing (Detail Sealant/Adhesive): Elemax 5000 Liquid Flashing, SilPruf SCS2000, SilPruf SCS2700, SilPruf SCS9000NB, or SWS.

    - Reinforcing Fabric: RF100; width as dictated by project conditions.

    - Sheet Flashing: Elemax SS Flashing; width as dictated by project conditions.

    - Silicone Transition Membrane: UltraSpan UST2200; width as dictated by project conditions.

    - Pre-Cured Silicone Molded Corners: UltraSpan USM inside and outside corners.

  - PERFORMANCE REQUIREMENTS

    - UV Exposure: No limit.

    - Application Temperature: 0 to 158 degrees F (minus 18 to 70 degrees C).

    - Performance Properties:

| Property | Value(1) | Test Method |
| --- | --- | --- |
| Required Dry Film Thickness | 17 mils (430 µ) dry | Apply 19 mils (480 µ) wet |
| Air Permeance – tested at 1.57 psf (75 Pa) | 0.00004 cfm/ft² (0.0002 L/s·m²) | ASTM E2178 |
|  | 0.00008 cfm/ft² (0.0004 L/s·m²) | CAN/ULC-741 |
| Assembly Air Leakage - tested at 1.57 psf (75 Pa) | 0.0002 cfm/ft² (0.0009 L/s·m²) | ASTM E2357 |
|  | 0.0004 cfm/ft² (0.0019 L/s·m²) Class A1 | CAN/ULC-742 |
| Water Resistance | Pass | AATCC 127 |
| Water Penetration | No water penetration observed after 15 min. @ 62.5 psf (2993 Pa) | ASTM E331 |
| Water Penetration | No water penetration after structural, racking, restrained environmental conditioning: Tested for 15 minutes at 2.86 psf (137 Pa) | ASTM E331 |
| Resistance to Wind-Driven Rain | Pass: No visual leaks or moisture weight gain observed after 24 hrs @ 26 psf (1245 Pa) | ASTM D6904 |
| Water Vapor Permeance | 10.5 perms @ 17 mils (430 µ) DFT | ASTM E96 Procedure BW (Inverted Water Method) |
| Water Vapor Permeance UV & Weathering Resistance | 10.2 perms @ 17 mils (430 µ) DFT | ASTM E96 Procedure B (Water Method) |
|  | 7.9 perms @ 17 mils (430 µ) DFT | ASTM E96 Procedure A (Desiccant Method) |
|  | No degradation after 5000 hours | ASTM G154 |
| Self Sealability around Nails | Pass @ 17 mils (430 µ) DFT | ASTM D1970 |
| Crack Bridging Ability (1/16 inch or 1.5 mm) | Pass | ASTM C1305 |
| Mildew Resistance | 0 - No Growth | ASTM D5590 |
| Service Temperature Range | Minus 40 F to plus 300 degrees F (minus 40 to plus 149 degrees C) |  |
| Pull off Strength (concrete) | 126 psi (0.87 MPa) | ASTM D4541 |
| Pull off Strength (fiberglass mat faced gypsum sheathing) | 44 psi (0.30 MPa)(2) | ASTM D4541 |
| Tensile Strength | 204 psi (1.40 MPa) | ASTM D412(3) |
| Elongation | 542 percent | ASTM D412(3) |
| Multi-Story Wall Assembly Burn Test | Passed in assembly tested and acceptable for use in various wall assemblies per engineering analysis | NFPA 285 |

| Surface Burning | Flame Spread: 10 Smoke Developed: 185 NFPA Class A, UBC Class 1 | ASTM E84 |
| --- | --- | --- |

| Sequential Testing- Weathering |  |  |
| --- | --- | --- |
| UV Light Exposure |  | ICC-ES AC212 |
| Accelerated Aging |  | ICC-ES AC212 |
| Hydrostatic Pressure Test | No water penetration after UV exposure and accelerated aging: Tested for 5 hours with 21.7 in (55 cm) of hydrostatic head | AATCC 127 |
| Freeze-Thaw | No cracking, checking, crazing, erosion, delamination or other deleterious effects. | ICC-ES AC212 ASTM E2485 Method B |
| Water Resistance | No deleterious effects after 14 day exposure | ASTM D2247 |
| Tensile Bond | Minimum 15 psi (105 kPa) | ASTM C297 |

(1) Average value. Actual value may vary.

(2) Full strength of silicone not realized due to failure of fiberglass mat / sheathing substrate prior to coating failure.

(3) Samples were prepared per ASTM D2370 and tested in accordance to ASTM D412.

- EXECUTION

  - PREPARATION

    - Condition of Surfaces:

      - Clean, dry and free of contaminants that could interfere with proper bonding of materials.

      - Masonry joints: Struck flush. Fill cracks greater than crack bridging ability of material, routed and filled where necessary, with trowel application of liquid flashing prior to application of liquid membrane.

      - Sheathing joints: Treated per manufacturer’s installation details.

    - Remove loose mortar and other contaminations by wire brush or similar abrasion to provide stable clean surface for application.’

    - Remove grease, oil, bitumen, form release agents, paints, curing compounds, other contaminants, and film forming coatings from concrete.

    - Mask adjoining surfaces not to be covered by air barrier.

    - Spot treat over and under fasteners with liquid flashing or air barrier material.

  - INSTALLATION

    - Perform installation in accordance with manufacturer’s instructions.

    - Transition and Detailing Treatment:

      - Install appropriate materials to treat sheathing joints, expansion joints, rough openings, transitions, terminations, penetrations, and other similar surface irregularities.

      - Perform detailing before or after air barrier membrane application.

    - Treat sheathing joints less than 1/4 inch (13 mm) in width using any of following methods:

      - Liquid flashing.

      - 4 inch (100 mm) reinforcing fabric embedded in air barrier material and centered on joint.

    - Inside and Outside Corners: Extend liquid flashing or reinforcement minimum 3 inches (75 mm) onto each angle change using any of following methods:

      - Liquid flashing.

      - Minimum 6 inch (150 mm) reinforcing fabric embedded in air barrier material and centered on joint.

      - Minimum 6 inch (150 mm) sheet flashing centered on corner.

      - Silicone transition membrane set in liquid flashing and centered on corner.

    - Rough Openings. Extend liquid flashing or reinforcement minimum 3 inches (75 mm) onto vertical wall and into rough opening using any of following methods:

      - Liquid flashing.

      - Minimum 6 inch (150 mm) reinforcing fabric embedded in air barrier material and centered on joint.

      - Minimum 6 inch (150 mm) sheet flashing centered on corner.

      - Minimum 6 inch (150 mm) silicone transition membrane set in liquid flashing and centered on corner.

      - Pre-cured silicone molded outside corners in combination with any of above methods.

    - Pipe and Duct Penetrations: Treat using any of following methods:

      - Liquid flashing.

      - Reinforcing fabric embedded in air barrier material and centered on joint. Ensure that reinforcing fabric extends minimum 2 inches (50 mm) onto wall.

    - Static Joints less than 1/2 inch (13 mm) in width and Expansion Joints:

      - Treat using minimum 3 inch (150 mm) silicone transition membrane set in liquid flashing or air barrier material and centered on joint.

      - Ensure that transition membrane extends minimum 1 inch (25 mm) onto wall.

    - Transitions: Treat using any of following methods:

      - Liquid flashing.

      - Reinforcing fabric embedded in air barrier material and centered on joint.

      - Sheet flashing centered on corner.

      - Silicone transition membrane set in liquid flashing.

    - Through Wall Flashing. Install sheet flashing.

    - Air Barrier:

      - Apply by spray, power roller, roller, or brush at to minimum dry film thickness recommended by manufacturer.

      - Touch up damaged areas using same procedures as initial application, at any time after application; coating may be wet or cured.

  - PROTECTION

    - Protect air barrier from damage during application and for remainder of construction.

    - If damage occurs, repair per manufacturer’s instructions.

  - CLEANING

    - Clean air barrier materials from surfaces that will be exposed in completed work using cleaning agents and procedures recommended by manufacturer.

    - Remove masking materials after installation.

END OF SECTION