The following specification text has been prepared to assist design professionals in the preparation of a specification section incorporating EndurisTM 3525 used as a remedial roof coating system applied over existing single ply TPO, PVC, or EPDM roofing membranes. Design professional is responsible for editing information to meet their Project requirements and coordinate with other specifications sections and Drawings.

SECTION 07 56 00

FLUID APPLIED ROOFING

Editor notes are included in hidden text to assist with product attributes and performance.

EndurisTM 3525 forms a durable, breathable, and waterproof roofing membrane that is highly resistant to degradation from heat, cold, UV light, and natural weathering.

EndurisTM 3525 is not permitted over gravel-surfaced membranes and is restricted to substrates that are in sound condition that are able to be properly prepared, having suffered from the normal effects of aging, exposure, and use.

For assistance on the use of the products in this section, contact Momentive Performance Materials at 877-943-7325, or visit their website at www.siliconesforbuilding.com.

GENERAL

SUMMARY

Section Includes: Remedial roof coating system applied over existing single-ply roofing membranes.

Related Sections:

Section 07 01 50 – Roof Repairs.

Section 07 62 00 – Sheet Metal Flashing and Trim.

Section 07 71 00 – Roof Specialties.

Section 07 72 00 – Roof Accessories.

Section 07 92 00 – Joint Sealants.

SUBMITTALS

Action Submittals:

Product Data: Manufacturer’s current technical data sheet, descriptive data and application instructions.

Shop Drawings: Roof plan showing scope of Work and roof details.

Samples: Physical samples and color samples of products to be installed.

A Moisture Scan Report is required for Projects requiring a Labor and Material Warranty.

Moisture scan report.

Informational Submittals:

Retain Installer Certification for Projects requiring a Product Plus or Labor and Material Warranty.

Certifications: Signed by roof coating manufacturer certifying that installer is approved, authorized, or licensed by manufacturer to install coating system.

Sample Warranty:

Installer’s warranty sample.

Manufacturer’s warranty sample.

Manufacturer’s Field Installation Guide.

QUALITY ASSURANCE

Manufacturer Qualifications:

Not less than 25 years documented experience in manufacturing silicone roof coatings.

ISO 9001 certified.

Retain following Applicator Qualifications for Projects requiring a Product Plus or Labor and Material warranty.

Applicator Qualifications:

Approved by roof coating manufacturer.

Eligible to offer the specified manufacturer warranty.

Experienced with installation of the same or similar waterproofing materials.

Roof Coating:

UL Listed.

FM Class 1, 4470 approved.

NSF P151 Certified.

Adhesion Test: Conduct an adhesion test to all differing surfaces that are to receive coating. Perform testing in accordance with manufacturer’s written instructions. Document results and submit to Architect and manufacturer.

DELIVERY, STORAGE AND HANDLING

Deliver materials and products in their original and unopened packaging with legible labels showing the manufacturer’s name, lot numbers, and product identification visible.

Handling and Storage:

Store roof coating containers between 15 °F and 109 °F (-9 °C to 43 °C).

Store other materials in accordance with the manufacturer’s instructions.

Keep products out of direct sunlight.

Dispose of materials according to applicable regulations and laws.

PROJECT CONDITIONS

Ensure roof appurtenances are in place prior to surface preparation and roof coating application.

Weather Conditions: Proceed with the Work only when existing and forecasted weather conditions will permit materials to be installed in accordance with the manufacturer’s written instructions and requirements.

Substrate Conditions: Do not install materials over substrates that are damp, wet, or otherwise contaminated in such a way to prevent proper adhesion.

Apply roof coatings at temperatures above 0 °F (-18 °C). Do not apply coating materials when temperatures are within 5 °F (3 °C) of dew point.

Contact manufacturer for recommendations if applying coating to substrates over 120 °F (49 °C).

WARRANTIES

Select one of the following manufacturer warranties.

Manufacturer’s Product Warranty: Submit a written warranty from manufacturer agreeing to replace any defective product as defined by the Warranty, at no charge.

Warranty term: [10] [15] [20] years.

Product Plus Warranty requires applicator to be authorized by the manufacturer.

Manufacturer’s Product Plus Warranty: Submit a written warranty from manufacturer agreeing to replace any defective product as defined by the Warranty and pay the cost of labor to install the replaced product.

Warranty term: [10] [20] [30] years.

Labor and Material Warranty requires applicator to be authorized by the manufacturer and a Moisture Scan.

Manufacturer’s Labor and Material Warranty: Provide roof coating manufacturer’s labor and material warranty.

Warranty term: [10] [15] [20] years.

Installer’s Warranty: Submit roofing installer’s warranty, signed by Installer, covering the work of this section, including all components installed, for the following term:

Warranty term: [2] [5] [__] years.

PRODUCTS

MANUFACTURERS

Basis of Design: EndurisTM 3525 by Momentive Performance Materials
(www.siliconeforbuilding.com).

Substitutions: [Substitutions not permitted.] [Refer to Division 01 for Substitution Procedures.]

MATERIALS

Silicone Roof Coating:

Description: High solids, solvent-free, alkoxy-based, moisture-cured, silicone roof coating.

Physical Properties: Tested to ASTM D6694.

Tensile strength: 253 PSI, tested to ASTM D2370.

Elongation: 550 percent, tested to ASTM D2370.

Volume solids: 90 percent, tested to ASTM D2697.

ACCESSORIES

Seam Treatment and Flashing Materials:

EndurisTM Liquid Flashing by Momentive Performance Materials.

UltraSpanTM UST / USM pre-cured silicone transition sheets and molded corners by Momentive Performance Materials.

Reinforcement Fabric: RF100TM series, 100 percent polyester spun-laced textile reinforcing fabric.

SWS Silicone SealantTM by Momentive Performance Materials.

Walkway Coating: EndurisTM 3525 protection silicone coating, [yellow,] [contrasting color,] with granules installed in coating at the minimum rate of 30 pounds per 100 square feet or until rejection.

Slip Sheet: TPO single ply membrane for use as a slip sheet under loose-laid materials and equipment such as sleepers, pipe supports, etc.

EXECUTION

EXAMINATION

Momentive has a Pre-Job Evaluation Checklist on their website to assist the construction team in evaluation of the existing roof for acceptability of EndurisTM product.

Conduct a roof inspection to determine the necessary repairs and the type(s) of materials to use. Manufacturer will not be responsible for any defects or deficiencies that will inhibit proper performance of the coating.

Preinstallation Testing: Conduct adhesion tests in accordance with manufacturer’s adhesion testing procedures to determine if primer or other surface preparation is required. Document adhesion test results.

Verify that existing substrate is sloped a minimum of 0.25 inches of vertical rise per 12 inches (1/4:12) of horizontal run to promote positive drainage.

Evaluate existing shrinking and tenting. Contact single-ply membrane manufacturer for required repair and preparation.

Verification of Existing Conditions:

Ensure the roof is not in the process of failing.

Walk the roof to identify defective items and issues that will affect the performance of the coating.

Examples of defective items are, bur are not limited to: open seams, open flashing laps and voids, edge securements, rusted or deteriorated pitch pans, shrunken pitch pan filler, deficient sealant on storm collars, ponding conditions, deteriorated sealant on surface-mounted counter flashings, deteriorated wall joint sealant, and pipe penetration flashing defects.

Core the existing roof on all separate roof sections to document the existing roof assembly, and to help identify and address any concerns or issues that may be present, such as:

Moisture laden roofing, especially within the bottom assembly, if multiple roofs are present.

Moisture damaged gypsum or lightweight insulating concrete roof decks.

Moisture damaged cement fiber roof decking.

Inspect all roof drainage details for defects that will result in leaks or inhibit proper drainage. Notify Owner of any issues needing corrective action.

Identify existing roof leaks and notify Owner if any leaks are present that cannot be addressed as part of the Work.

Do not proceed with Work until deficiencies are corrected. Beginning of Work constitutes acceptance of substrate.

Moisture surveys are strongly recommended on all membrane roofs and are required where a Labor and Material warranty is to be issued

Conduct a Moisture Survey to identify moisture laden materials in need of replacement prior to application of the coating. Provide a written report detailing the results of the scan to the coating manufacturer. Provide moisture scans compliant with the current versions of the following ASTM standards:

ASTM C1153 – Standard Practice for Location of Wet Insulation in Roofing Systems Using Infrared Imaging.

ASTM D7954 – Moisture Surveying of Roofing and Waterproofing Systems Using Nondestructive Electrical Impedance Scanners.

PREPARATION

Repair all existing roof leaks according to industry standards, prior to performing any pressure washing to prevent additional moisture intrusion. Reference repair procedures in the NRCA Repair Manual for Low-Sloped Membrane Roof Systems.

Mask or otherwise protect surfaces not to be coated.

Review existing and imminent weather conditions including potential for extreme temperatures, relative humidity, frost, dew, and precipitation. Ensure that coating and accessory materials will have sufficient curing time.

Surface Preparation and Repairs:

Remove loose granules, dirt, debris, and sediment from the surface of the roof.

Take corrective measures before beginning coating preparations. Repair failed, damaged, and open areas that could allow water infiltration during cleaning.

Remove all trash and heavy deposits of sediment, dirt, and other vegetative growth.

Remove all moisture-damaged insulation and replace insulation and roof membrane with similar materials.

Follow code requirements for Work performed, including attachment of new insulation and membrane, to comply with wind uplift requirements.

Properly secure membrane repairs to the structural deck.

Inspect the roof for loose or open field seams and side laps, including vertical flashing laps and repair as follows:

Remove dirt and debris from inside the seam.

Ensure roof system components are completely dry.

More than 1 Option can be selected. Retain Option 1 regardless of surface being recoated.

Repair defective seams or laps with one of the following options:

Option 1: Seal the seam by 3-course method using liquid flashing and fabric reinforcement.

Select the following Option if coating over existing TPO or PVC.

Option 2: Seal the seam by hot-air-welding a new piece of membrane over the open seam in accordance with membrane manufacturer requirements.

Select the following Option if coating over existing EPDM or TPO.

Option 3: Install single-ply manufacturer’s approved cover strip over properly prepared surface(s) in accordance with manufacturer’s requirements

Mechanically remove loose and flaking rust on metal flashings. Severely damaged sheet metal flashings are to be replaced. Follow NRCA and SMACNA guidelines.

Seal all seams with a 3- to 4-inch-wide application of minimum 40 wet mils of liquid flashing. This includes field seams, penetration flashing seams, wall and curb flashing seams, and similar.

Pipe Penetrations:

Vent and Pipe Penetrations with Undamaged Existing Flashings: Apply a minimum of 40 wet mils of coating extending 4 inches up the pipe or vent.

Inspect prefabricated flashing boots. Repair damaged prefabricated flashing boots using the 3-course liquid flashing and fabric reinforcement. Reseal the tops of all flashing boots using coating manufacturer’s approved sealant.

Properly prepare and encapsulate the tops of all surface-mounted counter flashings with a minimum of 60 mils of liquid flashing. Perform adhesion tests as needed, and in accordance with the manufacturer’s instructions. Remove chalking from existing sealants.

Pitch Pans (aka Penetration Pockets): Pitch pans are not warrantable. The following are recommendations for sealing pitch pans.

Ensure the liquid flashing will adhere to the pitch pan filler by performing an adhesion test.

Cut a “V” at the base of the pitch pan penetration(s).

Apply a manufacturer-approved sealant to the base of the penetrations.

Encapsulate the entire pitch pan with a 3-course application of silicone coating and fabric reinforcement

Rusted or corroded pitch pans should be removed and replaced with new pitch pans.

Roof Drains

Drains with damaged flashings or components: Remove strainers and clamping rings and set aside for reinstallation. Trim the roof membrane and wire brush or otherwise remove contaminants from the drain bowl. Seal the roof-to-drain bowl connection by 3-course method using liquid flashing and fabric reinforcement.

Drains with undamaged flashings and/or components: After cleaning and drying around the drain, apply coating up to the clamping ring. Do not apply any sealant or liquid flashing where the clamping ring meets the roof.

Scupper drains are to be flashed with the 3-course method using liquid flashing and fabric reinforcement.

Seal storm collars using liquid flashing or a compatible sealant approved by the coating manufacturer.

Seal exposed fasteners with liquid flashing or a compatible sealant approved by the coating manufacturer.

Pressure wash the roof surface at approximately 2500 PSI utilizing manufacturer’s recommended roof preparation wash or approved biodegradable detergent; remove oils and other materials that could interfere with adhesion. Rinse with clean water until no soap bubbles or foaming remains. Allow to completely dry.

Double wash all areas where water collects as sediments other debris will collect in these areas and can inhibit proper adhesion.

Allow the roof to completely dry. Any areas where water collects will take longer to dry. The use of mechanical means to help dry the roof is recommended. Examples are hot air roof dryer machines.

Seal all horizontal sheet metal flashing joints such as copings and expansion joint covers by using a bond breaker and then covering with a 2-inch-wide strip of minimum 60 wet mils of liquid flashing or manufacturer-provided, compatible sealant. An example of a bond breaker is running a lumber crayon over the joint and then encapsulating it with the sealant. Note: Standing seam joints are excluded from this requirement.

Required Condition of Surfaces: Clean, sound, dry, and free of materials, laitance, chalking, and loose coatings that could inhibit proper adhesion of coatings or sealants. Seal penetrations and flashings watertight prior to coating application.

APPLICATION

Apply roof coating in accordance with manufacturer’s instructions and approved Drawings.

Application rates will vary depending on the complexity of the project. The following rates do not consider waste. Applicator is required to calculate the waste factor needed. “Waste” includes material left in the buckets or barrels, on roller frame covers, inside hoses (when spray applied), etc. All application rates apply to both the roof and any walls or curbs to be coated.

Include the stretch out of the metal panels so that all ribs, flutes, and pans are properly coated.

Select one of the following application mil thicknesses based on 10, 15, or 20 year warranty requirements.

[Apply roof coating at rate of 1.5 gallons per 100 square feet to minimum 21 mils cured coating thickness.]

[Apply roof coating at rate of 2.0 gallons per 100 square feet to minimum 28 mils cured coating thickness.]

[Apply roof coating at rate of 2.5 gallons per 100 square feet to minimum 36 mils cured coating thickness.]

Apply coating by squeegee, brush, roller, airless sprayer, or a combination of these.

Apply liquid flashing by brush, trowel, gloved hand, or with a bulk caulking gun.

Final Roof Coating: Monolithic and seamless, encapsulating entire roof surface.

Retain below if granular coat finish is desired.

Granular Coat: Apply granular coat once the underlying coat has cured. Apply one (1) coat of silicone at the minimum rate of approximately one (1) gallon per 100 square feet (3.8 liters per 9.25 square meters) to achieve a minimum wet film thickness of 16 mils (.016 inches). Simultaneously embed #11 ceramic granules at the rate of approximately 30 pounds per 100 square feet (13.6 kilograms per 9.25 square meters) or until rejection. Granules must be applied before the coating skins over.

Walkway Protection is optional but strongly suggested when mechanical units or other equipment is located on the roof. Retain below if roof is subject to maintenance of rooftop equipment.

Walkway Protection: At roof access locations and around rooftop equipment requiring servicing. Apply walkway coating a minimum of 60 wet mils thick, simultaneously embedding roofing granules at the rate of approximately 35 pounds per 100 square feet (16 kilograms per 9.25 square meters). Walkway shall be a minimum of 30 inches (760mm) wide. Mask sides to achieve straight lines.

Lift and coat under all sleeper supports, including both wood and manufactured supports, for service lines and rooftop equipment such as mechanical units and satellite dishes. After coating has cured ,place a slip sheet under supports to protect the coating. Extend slip sheet past the edges of the sleeper a minimum of 1 inch on all sides.

CLEANING

Clean finished roof surface after completion; ensure that drainage components are not clogged.

PROTECTION

Protect roof coating from foot traffic and damage while. A cure time of 3 days is recommended to achieve full cure.

FIELD QUALITY CONTROL

Verify proper application rates by using a wet film gauge. Check wet film thickness a minimum of once every 100 square feet (9.25 square meters).

Verify cured mil thickness of coating at end of work and prior to warranty inspection.

Repair deficient areas with liquid flashing or roof coating, as applicable to size of deficient area.

Manufacturer’s project acceptance is subject to pre-job, progress, and final inspections by coating manufacturer or its designated third-party inspectors.

END OF SECTION