GENERAL SPECIFICATIONS FOR

INSULROCK® BRAND INSULATING PANELS

1.0	GENERAL

1.1	Insulating panels as shown on the drawings shall be    INSULROCK brand insulating panels as manufactured by Advanced Insulation Concepts, Inc. (AIC).

2.0	PANEL DESCRIPTION

2.1	Panel facings shall be permanently bonded to the insulating 				core with a heat polymerizing adhesive.

2.1.1	Exterior facings shall be .020” to .026” G-90 hot dipped galvanized or AZ-50 Galvalume steel, conforming to ASTM A653 Grade 33, precoated with a nominal 1 mil thick silicone modified polyester finish.  Facings shall be designated as smooth or stucco embossed.

2.1.2	Exterior facings, where designated, shall be embossed, .023” G-90 hot dipped galvanized or AZ-50 Galvalume steel, conforming to ASTM A653 Commercial Quality, precoated with a nominal 1 mil thick Kynar finish (Beige, Sandstone, Light Gray or Surrey Beige.

2.1.3	Interior facings shall be .020” to .026” G-90 hot dipped galvanized or AZ-50 Galvalume steel, conforming to ASTM A653 Grade 33, precoated with a nominal 1 mil thick Polar White silicone modified polyester finish acceptable to the USDA.  Facings shall be designated as smooth or stucco embossed.

2.1.4	Stainless steel interior facings, where designated, shall be .020”to .024” Type 304 stainless steel stucco embossed.

2.1.5	Plastic Coated Steel interior facings, where designated, shall be .020” galvanized steel, G-90 Hot dipped, or Galvalume (AZ-50) steel conforming to ASTM 653 Commercial Quality, precoated with .004” White polyvinyl chloride Plastisol acceptable to the USDA.

2.1.6	Composite facings, where designated, shall be .090” fiberglass reinforced polyester laminated to .020 “   primed hot dipped galvanized (G-90) steel or Galvalume (AZ-50) steel.  The FRP shall have a flame spread rating of 200 or less and a smoke developed rating of 450 or less when tested by ASTM E84.

2.1.7	Fiberglass reinforced polyester facings, where 						designated, shall be nominal .090” with a flame spread 					rating of 25 or less and a smoke developed rating 450 or 				less when tested by ASTM E84 and shall be acceptable 					to the USDA.

2.1.8	Liner facings, where designated, shall be .020” 						Galvannealled steel A40.

2.2	Panel edges shall be precisely formed to assure core to core 				contact and alignment of panel facings and to facilitate vapor 				barrier and sanitary sealing as required.

2.2.1	Tongue and Groove Edge Treatment (TAGET) shall be 					continuously roll formed into facings such that the 					formed tongue of one panel fits into the groove formed 					by the facing and core of the adjacent panel.  In 						addition, the core shall be grooved to accept a .5” x 					2.75” fiber reinforced cement board spline.

2.2.2	Panels with FRP or Composite Facings shall be formed and grooved to accept polyvinyl chloride H-Moldings.  In addition, the core shall be grooved to accept a .5” x 2.75” fiber reinforced cement board spline.

2.3	Metal panel facings shall have a roll formed configuration 				which enhances appearance and panel strength.

2.3.1	Exterior wall facings with TAGET may have a 						continuously roll formed light mesa configuration.

2.3.2	Exterior wall facings with TAGET may have a 						continuously roll formed configuration consisting of 					0.06” deep grooves spaced approximately 6” apart so 					that the joint between panels simulates a groove.

2.3.3	Interior facings with TAGET may have a continuously 					roll formed configuration consisting of 0.06” deep 					grooves spaced approximately 6” apart so that the joint 					between panels simulates a groove.

2.3.4   Interior facings with TAGET may have a continuously     roll formed light mesa configuration.

2.4	Insulating core thickness shall be determined based on the fire rating, temperature differential, and other building requirements.

2.4.1	Shall be Conrock L brand structural mineral wool insulation having the following typical physical properties:

Density (pcf)						8.5

Compressive Strength, 10% Defl.,psi		15

Water Absorption (ASTM C-209), % by Vol 	 3

K-Factor @ 40° F Mean (ASTM C-518)		.277

Thermal Resistance @ 40º F Mean			3.61/in

2.5	Dimensions

2.5.1	Panel width shall be 47.375 inches +/- 1/16 inch.

2.5.2	Panel thickness shall be as ordered +/- 1/16 inch.

2.5.3	Panel length shall be full height unless otherwise 					designated.  Length tolerance shall be +/- 1/8 inch.

2.5.4	Panels shall be fabricated in the field to fit the structure 					including the sloping walls to fit roof shape and fitting 					wall corners.

3.0	PANEL ACCESSORIES

3.1	Trim.

3.1.1	Angles and other trim painted to match the panels shall be made with .020” or thicker corrosion resistant steel sheets.

3.2	Splines

3.2.1	Fiber Reinforced Cement Board Splines shall be ½” x 2 ¾” x  8’.

4.0	WARRANTY

4.1	All INSULROCK panels furnished by Advanced Insulation Concepts, 			Inc. shall conform to the specifications set forth above and in the Bill 			of Materials used to order them and will be free from defects in 			material and workmanship when delivered to the job site.  If any of 			the panels fails to conform to the above warranty, AIC will, upon 			written notice thereof received within two years following the initial 			date of installation, repair or replace, at AIC’s option, the 				nonconforming panels.  This Warranty shall not apply to failure 			caused by acts of God, fire, abuse or abnormal use, or other 				casualties, nor to panels which have not been used in a building 			application of adequate design, engineering and construction and in 			accordance with AIC’s current design and installation 					recommendation.  AIC MAKES NO OTHER WARRANTIES, 			EXPRESS OR IMPLIED (INCLUDING WITHOUT 					LIMITATION, MERCHANTABILITY, FITNESS FOR A 				PARTICULAR PURPOSE, OR AGAINST INFRINGEMENT OF 			ANY PATENT).  REPAIR OR REPLACEMENT, AS SET 				FORTH HEREIN, IS THE SOLE AND EXCLUSIVE REMEDY 			OF PURCHASER AND WILL SATISFY ALL LIABILITIES OF 			AIC TO PURCHASER WHETHER BASED ON CONTRACT, 			NEGLIGENCE OR OTHERWISE ARISING OUT OF THE 			PURCHASE OR USE OF THE PANELS.  IN NO EVENT WILL 			AIC BE LIABLE FOR INCIDENTAL OR CONSEQUENTIAL 			DAMAGES.

February, 2018