Copyright 2024 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to The Pittsburgh Paints Company (formerly PPG Paints) ("Licensee"). The Pittsburgh Paints Company is the exclusive distributor of PPG Protective and Marine Coatings products.

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact The Pittsburgh Paints Company, 400 Bertha Lamme Dr., Cranberry Township, PA 16066; Phone: (888) PPG-IDEA | (888) 774-4332, Option 4; Website: www.pittsburghpaints.com; Email: ppgspec@ppg.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 099113 - EXTERIOR PAINTING

Access Manufacturer's Specpoint Product Cards:

<Double click here to view the manufacturer's product cards available at Deltek Specpoint>

GENERAL

SUMMARY

Section Includes: Surface preparation of exterior substrates and application of the following:

Primers.

Water-based finish coatings.

Solvent-based finish coatings.

Floor sealers and paints.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed exterior products and insert references to this Section to establish primer requirements.

[Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming structural steel substrates.

Section 055000 "Metal Fabrications" for shop priming metal fabrications.

Section 055113 "Metal Pan Stairs" for shop priming metal pan stairs.

Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

[Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

Section 099123 "Interior Painting."

Section 099300 "Staining and Transparent Finishing" for surface preparation and application of wood stains and transparent finishes on exterior wood substrates.

Section 099600 "High-Performance Coatings" for tile-like coatings.

ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

Product Data: For each type of product.

Include preparation requirements and application instructions.

Indicate VOC content.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples. Delete "Samples" and "Samples for Initial Selection" paragraphs if colors and other characteristics are preselected and specified or scheduled and only verification Samples are required.

Samples: For each type of topcoat product.

Samples for Initial Selection: For each type of topcoat product.

Samples for Verification: For each type of paint system and each color and gloss of topcoat. Submit [actual paint drawdowns as specified below] [paint manufacturer's standard printed cards] for verification Samples.

Retain subparagraphs below only if retaining first option in "Samples for Verification" Paragraph above for actual paint drawdowns for verification Samples. Color and gloss of Samples change as they age; seven-day-old Samples appear different from freshly dried Samples.

Submit Samples on rigid backing, 8 inches (200 mm) square.

Apply coats on Samples in steps to show each coat required for system.

Label each coat of each Sample.

Label each Sample for location and application area.

Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in applicable exterior painting schedule articles to cross-reference paint systems specified in this Section. Include color designations.

Retain "Sustainable Design Submittals" Paragraph below if required to attain sustainability rating or to track sustainability submittals.

Sustainable Design Submittals:

"Product Data" Subparagraph below applies to LEED v4 and LEED v4.1 for Schools and LEED v4 and LEED v4.1 for Healthcare. Coordinate with requirements for paints and coatings.

Product Data: For paints and coatings, indicating VOC content.

Retain first three subparagraphs below to be eligible for LEED v4 or LEED v4.1 credit. See the Evaluations.

"Environmental Product Declaration (EPD)" Subparagraph below applies to LEED v4 and LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Environmental Product Declarations." Verify, with manufacturer, that EPDs are available for each product.

Environmental Product Declaration (EPD): For each product.

"Health Product Declaration (HPD)" Subparagraph below applies to LEED v4 and LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting." Verify, with manufacturer, that HPDs are available and comply with requirements of the HPD Open Standard or USGBC-approved program.

Health Product Declaration (HPD): For each product.

"Sourcing of Raw Materials" Subparagraph below applies to LEED v4 and LEED v4.1 (all) MR Credit "Building Project Disclosure and Optimization - Sourcing of Raw Materials," Option 1 - "Raw Material Source and Extraction Reporting." Verify, with manufacturer, that corporate sustainability reports are available, have been prepared within the last year or are applicable to the year of production, and are by USGBC-approved organization.

Sourcing of Raw Materials: Corporate sustainability report for each manufacturer.

Retain "Manufacturer Inventory" Subparagraph below for LEED v4 and LEED v4.1 MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting."

Manufacturer Inventory: For each product, provide manufacturer's manifest of ingredients.

MAINTENANCE MATERIAL SUBMITTALS

See Section 017700 "Closeout Procedures" for submission of maintenance material items.

Extra Stock Material: Furnish extra materials[, from the same production run,] to Owner that match paint products applied and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint Products" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

Paint Products: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert value> of each material and color applied.

MOCKUPS

Apply mockups of each paint system indicated and each color and finish selected to verify selections made under Sample submittals, demonstrate aesthetic effects, and set quality standards for materials and execution.

Architect will select one surface to represent surfaces and conditions for application of each paint system.

Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

Other Items: Architect will designate items or areas required.

Final approval of color selections will be based on mockups.

If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Owner specifically approves such deviations by Change Order.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site in paragraph below.

Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

Maintain containers in clean condition, free of foreign materials and residue.

Remove rags and waste from storage areas daily.

FIELD CONDITIONS

Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

Do not apply paints in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

PRODUCTS

Retain "Source Limitations" Article below to limit sources for the entire Section. Source limitations may also be specified in individual articles if desired.

SOURCE LIMITATIONS

Obtain each paint product from single source from single manufacturer.

EXTERIOR PAINTS, GENERAL

Exterior Paints: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include but are not limited to products] listed in product types below and applicable exterior painting schedule articles for the paint category indicated.

Generally, retain "Material Compatibility" Paragraph below. Systems could fail if paints used for separate coats are incompatible.

Material Compatibility:

Materials for use within each paint system must be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer based on testing and field experience.

For each coat in a paint system, provide products recommended in writing by topcoat manufacturer for use in paint system and on substrate indicated.

"VOC Content" Paragraph below applies to LEED v4 or LEED v4.1 for Schools and LEED v4 or LEED v4.1 for Healthcare credit for exterior-applied products.

VOC Content: For field applications, verify paints and coatings comply with VOC content limits of authorities having jurisdiction and the following VOC content limits:

Categories in subparagraphs below are taken from LEED rating systems and the standards referenced by them; if clarification is required, see those documents or the reference guides.

Flat Paints and Coatings: 50 g/L.

Nonflat Paints and Coatings: 50 g/L.

Dry-Fog Coatings: 150 g/L.

Primers, Sealers, and Undercoaters: 100 g/L.

Rust-Preventive Coatings: 100 g/L.

Zinc-Rich Industrial Maintenance Primers: 100 g/L.

Pretreatment Wash Primers: 420 g/L.

Shellacs, Clear: 730 g/L.

Shellacs, Pigmented: 550 g/L.

Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule on Drawings] <Insert requirements>.

[10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

PRIMERS

Alkali-Resistant, Water-Based Primer: Water-based primer formulated for use on alkaline substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT] [Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT] or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Exterior, Latex Wood Primer: Waterborne-emulsion primer formulated for resistance to extractive bleeding, mold, and microbials; for hiding stains; and for use on exterior wood substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Exterior, Alkyd/Oil Wood Primer: Solvent-based primer formulated for resistance to extractive bleeding, sag, mold, and microbials; for hiding stains; and for use on exterior wood substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Latex Block Filler: Water-based, pigmented, high-solids, emulsion coating formulated to bridge and fill porous surfaces of CMU substrates in preparation for specified subsequent coatings.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 to 11.0 mils DFT] [Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils DFT] or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based Bonding Primer: Water-based-emulsion primer formulated to promote adhesion of subsequent specified coatings.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Solvent-Based Bonding Primer: Solvent-based primer formulated to seal substrates and promote adhesion of specified subsequent coatings.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based, Rust-Inhibitive Primer: Corrosion-resistant, water-based-emulsion primer; formulated for resistance to flash rusting when applied to cleaned, ferrous metal substrates subject to mildly corrosive environments.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Red Primer, 90-1908; applied at 2.0 mils DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Zinc-Rich, Inorganic Primer: Corrosion-resistant, inorganic-based, zinc-rich primer formulated for use on prepared ferrous metal substrates subject to severe industrial or marine environments.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; [Dimetcote 9 two component, moisture-curing zinc (ethyl) silicate, applied at 2.0 to 4.0 mils DFT] [Dimetcote 9H Inorganic Zinc Silicate Primer; applied at 2.0 to 5.0 mils DFT] [Metalhide One Pac one-component, inorganic zinc silicate primer, 97-676, applied at 3.0 to 4.0 mils DFT] or comparable product by one of the following:

Hempel (USA), Inc.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Epoxy Zinc-Rich Primer: Multi-component, epoxy-type anti-corrosive primer; formulated for use on cleaned ferrous metal surfaces that will be exposed to moderate industrial or marine environments.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; Amercoat 68 HS Zinc Rich Epoxy; applied at 2.0 to 5.0 mils DFT or comparable product.

Surface-Tolerant Metal Primer: Corrosion-resistant, solvent-based metal primer formulated for use on structural steel and metal fabrications that have been minimally prepared.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Quick-Drying, Alkyd Metal Primer: Corrosion-resistant, solvent-based, modified-alkyd primer; lead and chromate free; formulated for quick-drying capabilities and for use on cleaned, ferrous metal substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Alkyd Metal Primer: Corrosion-resistant, solvent-based, alkyd primer formulated for use on prepared ferrous metal substrates subject to industrial and light marine environments.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT] [Speedhide LV Rust Inhibitive Steel Primer, 6-212N Series; applied at 1.5 mils minimum DFT] or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based, Galvanized-Metal Primer: Corrosion-resistant, pigmented, acrylic primer; formulated for use on cleaned/etched galvanized metal substrates to prepare it for subsequent water-based coatings.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Epoxy, Anticorrosive Primer: Solvent-based, two-component, epoxy, anti-corrosive primer; formulated for use on ferrous and galvanized metal substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; [Amerlock 2 AL Aluminum Epoxy Mastic; applied at 4.0 to 8.0 mils DFT] [Amercoat 235 Multi-Purpose Phenalkamine Epoxy; applied at 4.0 to 8.0 mils DFT] [Amerlock 600 Multi-Purpose Epoxy Coating; applied at 5.0 to 10.0 mils DFT] or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Epoxy High Build Self Priming Primer: A two-component epoxy, high-solids, low-gloss coating for use on interior or exterior ferrous metal surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; Amerlock 600 Multi-Purpose Epoxy; applied at 5.0 to 10.0 mils DFT or comparable product.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Vinyl Wash Primer: Two-component, vinyl butyral/phosphoric acid-wash primer formulated for use over cleaned ferrous metal substrates and zinc-rich primers as a tie coat for subsequent corrosion-resistant primers or finish coatings.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Quick-Drying Aluminum Primer: Corrosion-resistant, solvent-based, alkyd or modified-alkyd primer formulated for quick-drying capabilities and for use on prepared aluminum substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT or comparable product by one of the following:

<Insert manufacturer's name>.

Water-Based Epoxy Metal Primer: Corrosion-resistant, water-based, two-component epoxy primer formulated for use on prepared, exterior ferrous- and galvanized-metal surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Aquapon WB EP, 98E-46/98E-99, Two-Component Waterborne Epoxy Primer; applied at 2.0 mils minimum DFT or comparable product.

Textured Latex Primer, Flat: Water-based, pigmented coating that contains sand or other hard aggregate and is formulated for use on exterior masonry, concrete masonry unit, and concrete surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT or comparable product.

Wood-Knot Sealer: White shellac or other sealer recommended in writing by manufacturer for this purpose.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

WATER-BASED FINISH COATINGS

Exterior Latex Paint: Water-based, pigmented coating; formulated for alkali, mold, microbial, and water resistance and for use on exterior substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Flat, Gloss Level 1:

- [Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT]

- [Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT]

- [Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT]

- [Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT]

- Gloss, Gloss Level 2:

- [Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT]

- Low Sheen, Gloss Levels 3 and 4:

- [Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT]

- [Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 1.6 mils minimum DFT]

- [Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT]

- [Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT]

- Semi-Gloss, Gloss Level 5:

- [Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT]

- [Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT]

- [Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT]

- [Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT]

- Gloss, Gloss Level 6:

- [Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT]

- [Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen: Manufacturer's standard [flat] [low sheen] [semigloss] [gloss].

Exterior, High-Build Latex Paint: Water-based, high-build, pigmented, emulsion coating; is formulated for abrasion, mold, microbial, and wind-driven rain resistance and for use on exterior substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, High Build Interior/Exterior Flat, 4-22XI Series; applied at 3.2 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard.

Textured Latex Coating: Water-based, pigmented, self-priming coating that contains sand or other hard aggregate for selected texture and is formulated for use on concrete and masonry substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [nonflat].

Texture: [Manufacturer's standard] [Fine] [Medium] [Coarse].

Exterior, Water-Based, Light Industrial Coating: Corrosion-resistant, water-based, pigmented, emulsion coating formulated for resistance to water, alkalis, moderate abrasion, and mild chemical exposure and for use on exterior substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Low Sheen, Gloss Level 3:

- [Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel 90-1710 Series; applied at 2.0 mils minimum DFT]

- Semi-Gloss, Gloss Level 5:

- [Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT]

- Gloss, Gloss Level 6:

- [Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [low-sheen] [semigloss] [gloss].

Exterior, Water-Based Alkyd Paint: Water-based, pigmented, low-VOC alkyd paint formulated for flash rust and water resistance and for use on exterior substrates.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [low sheen] [semigloss] [gloss].

Exterior, High-Performance Architectural Latex: Water-based, pigmented, low VOC, emulsion coating formulated for use on exterior substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

Low Sheen, Gloss Levels G3 and G4:

#### [Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT]

#### [Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT]

#### Semi-Gloss, Gloss Level G5:

#### [Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT]

#### [Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with Gloss Level 3 or Level 4; third corresponds with Gloss Level 5.

Gloss Level: [Manufacturer's standard low sheen finish] [Gloss of 10 to 35 units at 60 degrees and minimum sheen of 10 units at 85 degrees when tested in accordance with ASTM D523] [Gloss of 35 to 70 units at 60 degrees when tested in accordance with ASTM D523].

SOLVENT-BASED FINISH COATINGS

Exterior Alkyd Paint: Solvent-based, pigmented, alkyd coating formulated for mold, microbial, and water resistance and for use on exterior substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Semi-Gloss, Gloss Level 5:

- [HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT]

- Gloss, Gloss Level 6:

- [HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT]

- [Sil-Shield LV High Gloss Silicone Alkyd Enamel 95-5000N; applied at 1.5 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [semigloss] [gloss].

Quick-Drying Alkyd Paint: Solvent-based, alkyd or modified-alkyd coating formulated for quick-drying capabilities and for use on exterior substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Semi-Gloss, Gloss Level 5:

- [HPC Rust Inhibitive Interior/Exterior Alkyd Enamel Semi-Gloss, 4306 Series; applied at 2.0 mils minimum DFT]

- [HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT]

- Gloss, Gloss Level 7:

- [Fast Dry 35 Interior/Exterior Alkyd Gloss, 95-912 Series; applied at 1.0 mil minimum DFT]

- [HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss Level: Manufacturer's standard [semigloss] [gloss].

Aluminum Paint: Aliphatic, solvent-based coating consisting of varnish or alkyd binder combined with aluminum pigment that is formulated for use as a stain-blocking coating and sealer, is able to be recoated with conventional alkyd and latex paints, and for use on wood, metal, bituminous-coated, and prepared masonry substrates.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Benjamin Moore & Co.

Rodda Paint Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

High-Build Epoxy Paint, Low Gloss: High-solids, two-component epoxy; formulated for use on exterior concrete, masonry, and primed-metal surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; Amerlock 600 Multi-Purpose Epoxy; applied at 5.0 to 10.0 mils DFT or comparable product.

Second option in "Gloss and Sheen Level" Subparagraph below corresponds with Gloss Level 1, 2, or 3.

Gloss and Sheen Level: [Manufacturer's standard low-gloss finish] [Maximum gloss of 25 units at 60 degrees and sheen of 10 to 35 units at 85 degrees when tested in accordance with ASTM D523] <Insert requirements>.

Exterior, Water-Based, Light Industrial Coating: Corrosion-resistant, water-based, pigmented, emulsion coating formulated for resistance to blocking (sticking of two painted surfaces), water, alkalis, moderate abrasion, and mild chemical exposure and for use on exterior, primed, wood and metal surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Low Sheen, Gloss Level 3:

- [Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel 90-1710 Series; applied at 2.0 mils minimum DFT]

- Semi-Gloss, Gloss Level 5:

- [Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT]

- Gloss, Gloss Level 6:

- [Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT]

- or comparable product.

Second option in "Gloss and Sheen" Subparagraph below corresponds with Gloss Level 3; third option with Gloss Level 5.

Gloss and Sheen Level: [Manufacturer's standard low-sheen finish] [Gloss of 10 to 25 units at 60 degrees and sheen of 10 to 35 units at 85 degrees when tested in accordance with ASTM D523] [Gloss of 35 to 70 units at 60 degrees when tested in accordance with ASTM D523] <Insert requirements>.

FLOOR SEALERS AND PAINTS

Concrete Stain: Penetrating semitransparent stain specifically manufactured for interior and exterior concrete horizontal and vertical surfaces.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

H&C Decorative Concrete Products; a brand of Sherwin-Williams Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Latex Floor Enamel: Water-based, pigmented coating formulated to hide stains, for alkali and incidental water resistance, and for use on concrete and primed-wood substrates subject to low to medium foot traffic.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510XI Series; applied at 1.0 mil minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [low gloss] [gloss].

Retain "Slip-Resistant Aggregate" Subparagraph below if required.

Slip-Resistant Aggregate: Manufacturer's standard.

Latex Deck Coating: Water-based, high-solids, acrylic-emulsion coating; formulated for use on exterior substrates subject to low to medium foot traffic.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Flood Pro Series Resurfacer 100% Acrylic Stain, FLD 922 Series; applied at 75 sq. ft./gal. (1.84 sq. m/L) minimum coverage or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss Level: Manufacturer's standard.

Surface Texture: [Smooth] [Slip resistant].

Alkyd Floor Enamel: Solvent-based, pigmented coating; self-priming where applied to bare wood; formulated to hide stains, for durability, for microbial and abrasion resistance, and for exterior substrates subject to low to medium foot traffic.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Floor & Porch Waterborne Alkyd Gloss, 3-610 Series; applied at 1.3 mils minimum DFT or comparable product by one of the following:

Benjamin Moore & Co.

<Insert manufacturer's name>.

Second option in "Gloss Level" Subparagraph below corresponds with MPI Gloss Level G6.

Gloss Level: Manufacturer's standard [low gloss] [gloss].

Retain "Slip-Resistant Aggregate" Subparagraph below if required.

Slip-Resistant Aggregate: Manufacturer's standard additive.

Water-Based, Concrete-Floor Sealer: Clear, water-based, acrylic-copolymer-emulsion sealer formulated for oil, gasoline, alkali, and water resistance and for use on concrete traffic substrates.

Retain "Basis-of-Design Product" Subparagraph and list of manufacturers below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete Plex-Seal WB Interior/Exterior 100% Acrylic Clear Sealer, 4-6200XI Series; applied at 0.8 mil minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Solvent-Based, Concrete-Floor Sealer: Clear, acrylic, solvent-based sealer formulated for oil, gasoline, alkali, and water resistance and for use on concrete traffic substrates.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Benjamin Moore & Co.

H&C Decorative Concrete Products; a brand of Sherwin-Williams Co.

Hempel (USA), Inc.

Insl-X Products; Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Epoxy Deck Coating (Slip Resistant): Solvent-based, two-component epoxy, non-slip coating formulated for resistance to abrasion, solvents, fuel, and oils; for use on interior and exterior decks.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; [Amerlock 600 Multi-Purpose Epoxy Coating + NSA; applied at 5.0 to 10.0 mils DFT] [HPC High Gloss Epoxy, 95-501 Series + NSA; applied at 4 to 8 mils DFT] or comparable product.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in subparagraphs below are based on MPI recommendations.

Concrete: 12 percent.

Cementitious Composition Board: 12 percent.

Masonry (Clay and CMU): 12 percent.

Wood: 15 percent.

Portland Cement Plaster (Stucco): 12 percent. Verify that plaster is fully cured.

Verify suitability of substrates, including surface conditions and compatibility, with finishes and primers. Proceed with coating application only after unsatisfactory conditions have been corrected.

Application of coating indicates acceptance of substrates and conditions.

PREPARATION

For renovation or maintenance projects where repainting is required, consult manufacturers for recommendations and revise first paragraph below and paint systems specified in applicable exterior painting schedule articles.

Comply with manufacturer's written instructions applicable to substrates and paint systems indicated.

Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection.

Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems specified in this Section.

Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

Steel Substrates: Remove loose rust, loose mill scale, loose shop primer, and other loose foreign matter. Clean using methods recommended in writing by paint manufacturer[.][ but not less than the following:]

Usually, retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

SSPC-SP 2.

SSPC-SP 3.

SSPC-SP 7/NACE No. 4 "Brush-Off Blast Cleaning" permits tight residues of rust, mill scale, and coatings to remain. "Commercial Blast Cleaning" methods specified in SSPC-SP 6/NACE No. 3 may be impractical for use at Project site or allowed by authorities having jurisdiction.

SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed substrates.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized-Metal Substrates: Remove grease and oil residue from galvanized metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

Aluminum Substrates: Remove loose surface oxidation.

Wood Substrates:

If necessary, insert requirements for power or pressure washing.

Scrape and clean knots. Before applying primer, apply coat of knot sealer recommended in writing by topcoat manufacturer for exterior use in paint system indicated.

Sand surfaces that will be exposed to view and remove sanding dust.

Prime edges, ends, faces, undersides, and backsides of wood.

After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

Canvas and Cotton Insulation Covering Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

Plastic Trim Fabrication Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

APPLICATION OF EXTERIOR PAINT PRODUCTS

Apply paints in accordance with manufacturer's written instructions.

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

Use applicators and techniques suited for paint and substrate indicated.

Paint surfaces behind movable items same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed items with prime coat only.

Paint [both sides] [exterior side] and edges of exterior doors and entire exposed surface of exterior door frames.

Retain first subparagraph below if required for steel windows.

Paint entire exposed surface of window frames and sashes.

Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

Primers specified in applicable exterior painting schedule articles may be omitted on items that are factory primed or factory finished if compatible with intermediate and topcoat coatings and acceptable to intermediate and topcoat paint manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Tint undercoats to match color of topcoat but provide sufficient difference in shade of undercoats to distinguish each separate coat.

If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

Painting, Fire-Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

First subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

Paint the following work where exposed to view:

Subparagraphs below contains items that are often field painted, plus others that are often not. Revise list to suit Project.

Equipment, including panelboards[ and switch gear].

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Tanks that do not have factory-applied final finishes.

<Insert requirements>.

FIELD QUALITY CONTROL

Dry Film Thickness (DFT) Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for DFT.

Touch up and restore painted surfaces damaged by testing.

If test results show that DFT of applied paint does not comply with paint manufacturer's written instructions, apply additional coats as needed to provide DFT that complies with paint manufacturer's written instructions.

Cost of retesting is Contractor's responsibility.

CLEANING AND PROTECTION

At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

Do not clean equipment with free-draining water and prevent solvents, thinners, cleaners, and other contaminants from entering into waterways, sanitary and storm drain systems, and ground.

Dispose of contaminants in accordance with requirements of authorities having jurisdiction.

Allow empty paint cans to dry before disposal.

Retain subparagraph below if paint recycling or collection facilities are available in vicinity of Project.

Collect waste paint by type and deliver to recycling or collection facility.

After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

EXTERIOR PAINTING SCHEDULE, CONCRETE SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Vertical (Nontraffic) Surfaces:

Latex System: <Insert drawing designation>

Prime Coat: [Alkali-resistant, water-based primer] [Matching topcoat].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Latex Aggregate System: <Insert drawing designation>

Prime Coat: Textured latex coating, flat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex Aggregate System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, [flat] [nonflat].

High-Build Latex System: <Insert drawing designation>. DFT of not less than 10 mils (0.25 mm).

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Exterior, high-build latex paint.

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Alkali-resistant, water-based primer] [As recommended in writing by topcoat manufacturer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

High Performance Architectural Latex over Latex Aggregate System: <Insert drawing designation>

Prime Coat: Textured coating, latex, flat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Horizontal (Traffic) Surfaces:

Latex Floor Enamel System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Latex floor enamel, [low gloss] [gloss].

Latex Deck Coating System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex deck coating.

Alkyd Floor Enamel System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Alkyd floor enamel, [low gloss] [gloss].

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Solvent-Based Concrete Floor Sealer System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Solvent-based, concrete-floor sealer.

Water-Based Concrete Floor Sealer System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Water-based, concrete-floor sealer.

Latex Zone/Traffic-Marking Paint System: <Insert drawing designation>

Traffic-marking paint, latex.

Alkyd Zone/Traffic-Marking Paint System: <Insert drawing designation>

Traffic-marking paint, solvent-based.

EXTERIOR PAINTING SCHEDULE, CEMENTITIOUS SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Cementitious Composition Board Substrates: [Siding] [Trim] [Panels] <Insert requirements>.

Latex System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex Aggregate System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Exterior, textured coating, latex [flat] [nonflat].

High-Build Latex System: <Insert drawing designation>. Dry film thickness of not less than 10 mils (0.25 mm).

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Exterior, high-build latex paint.

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Alkali-resistant, water-based primer] [As recommended in writing by topcoat manufacturer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Portland Cement Plaster (Stucco) Substrates:

Latex System: <Insert drawing designation>

Prime Coat: [Matching topcoat] [Alkali-resistant, water-based primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

High-Build Latex System: <Insert drawing designation>. Dry film thickness of not less than 10 mils (0.25 mm).

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Exterior, high-build latex paint.

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd enamel, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Alkali-resistant, water-based primer] [As recommended in writing by topcoat manufacturer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

EXTERIOR PAINTING SCHEDULE, MASONRY SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Clay Masonry Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex Aggregate System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, [flat] [nonflat].

High-Build Latex System: <Insert drawing designation>. Dry film thickness of not less than 10 mils (0.25 mm).

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Exterior, high-build latex paint.

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

CMU Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkali-Resistant Primer System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex Aggregate System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, [flat] [nonflat].

High-Build Latex System: <Insert drawing designation>. Dry film thickness of not less than 10 mils (0.25 mm).

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Exterior, high-build latex paint.

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Alkali-resistant, water-based primer] [Latex block filler].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

EXTERIOR PAINTING SCHEDULE, METAL SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Steel and Iron Substrates:

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: [Zinc-rich, inorganic primer] [Alkyd metal primer] [Acrylic metal primer] [Epoxy metal primer] [Shop primer specified in Section in which substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating over Epoxy System: <Insert drawing designation>

Prime Coat: Epoxy metal primer.

Intermediate Coat: High-build epoxy paint, low gloss.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: [Alkyd metal primer] [Surface-tolerant metal primer] [Shop primer specified in Section in which substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Alkyd metal primer] [Quick-dry, alkyd metal primer] [Surface-tolerant metal primer] [Shop primer specified in Section in which substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

Quick-Dry Enamel System: <Insert drawing designation>

Prime Coat: Quick-dry, alkyd metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Quick-dry alkyd enamel, [semigloss] [gloss].

Aluminum Paint System: <Insert drawing designation>

Prime Coat: [Alkyd metal primer] [Shop primer specified in Section in which substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Galvanized metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized Metal Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Water-based, galvanized-metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: [Water-based, galvanized-metal primer] [Epoxy metal primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Water-based, galvanized-metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Water-based, galvanized-metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

Aluminum Paint System: <Insert drawing designation>

Prime Coat: Water-based, galvanized-metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Water-based, galvanized-metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Bituminous Coating System: <Insert drawing designation>

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Bituminous coating.

Aluminum (Not Anodized or Otherwise Coated) Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Pretreatment Coat: Vinyl wash primer.

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Quick-dry aluminum primer] [Vinyl wash primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Aluminum Paint System: <Insert drawing designation>

Pretreatment Prime Coat: Vinyl wash primer.

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Bituminous Coating System: <Insert drawing designation>

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Bituminous coating.

Copper Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Pretreatment Coat: [Vinyl wash] [Quick-dry aluminum] primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Quick-dry aluminum primer] [Vinyl wash primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Aluminum Paint System: <Insert drawing designation>

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Bituminous Coating System: <Insert drawing designation>

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Bituminous coating.

Stainless Steel Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Quick-dry aluminum primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Solvent-based bonding primer] [Alkyd metal primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Aluminum Paint System: <Insert drawing designation>

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

EXTERIOR PAINTING SCHEDULE, WOOD SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Glue-Laminated Wood Substrates:

Latex over Latex Primer System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Exposed Wood-Framed Substrates:

Latex over Latex Primer System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Dressed-Wood Substrates: [Wood trim] [Architectural woodwork] [Doors] [Windows] [Wood board siding] [Railings] [and] [Fences] <Insert requirements>.

Latex over Latex Primer System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Wood-Based Panel Substrates:

Latex over Latex Primer System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Wood-Board, Traffic-Surface Substrates: [Lumber decking] [and] [stairs]

Latex Porch and Floor Enamel over Latex Primer System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Latex floor enamel, [low gloss] [gloss].

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Latex Porch and Floor Enamel over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Latex floor enamel, [low gloss] [gloss].

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Latex Deck Coating System (for Plywood Decks): <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommending in writing by topcoat manufacturer.

Topcoat: Latex deck coating.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Alkyd Floor Enamel System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Alkyd floor enamel, [low gloss] [gloss].

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Alkyd Floor Enamel over Wood Preservative System: <Insert drawing designation>

Preservative Coat: Exterior wood preservative.

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Alkyd floor enamel, [low gloss] [gloss].

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Wood Shingle and Shake Siding Substrates:

Latex over Latex Primer System: <Insert drawing designation>

Prime Coat: Exterior, latex wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex over Alkyd Primer System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior, alkyd wood primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Exterior, latex wood primer] [Exterior, alkyd wood primer].

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

EXTERIOR PAINTING SCHEDULE, MISCELLANEOUS SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Fiberglass Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Plastic Trim Fabrication Substrates:

Latex System: <Insert drawing designation>

Prime Coat: [Solvent] [Water]-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: [Solvent] [Water]-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: [Solvent] [Water]-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: [Solvent] [Water]-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Exterior Canvas and Cotton Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based, Light Industrial Coating System: <Insert drawing designation>

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Alkyd System: <Insert drawing designation>

Prime Coat: Exterior latex paint, flat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Exterior latex paint, flat.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

Aluminum Paint System: <Insert drawing designation>

Prime Coat: Exterior latex paint, flat.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

Exterior Bituminous-Coated Substrates:

Latex System: <Insert drawing designation>

Prime Coat: Water-based, rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior latex paint, [flat] [low sheen] [semigloss] [gloss].

Latex Aggregate System: <Insert drawing designation>

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, [flat] [nonflat].

Alkyd System: <Insert drawing designation>

Prime Coat: Water-based, rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior alkyd paint, [flat] [semigloss] [gloss].

Water-Based Alkyd System: <Insert drawing designation>

Prime Coat: Water-based, rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior water-based alkyd paint, [low sheen] [semigloss] [gloss].

Aluminum Paint System: <Insert drawing designation>

Prime Coat: Water-based, rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

High Performance Architectural Latex System: <Insert drawing designation>

Prime Coat: Water-based, rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Exterior, high performance architectural latex, [low sheen] [semigloss].

END OF SECTION 099113