Copyright 2024 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to The Pittsburgh Paints Company (formerly PPG Paints) ("Licensee"). The Pittsburgh Paints Company is the exclusive distributor of PPG Protective and Marine Coatings products.

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact The Pittsburgh Paints Company, 400 Bertha Lamme Dr., Cranberry Township, PA 16066; Phone: (888) PPG-IDEA | (888) 774-4332, Option 4; Website: www.pittsburghpaints.com; Email: ppgspec@ppg.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 099123 - INTERIOR PAINTING

Access Manufacturer's Specpoint Product Cards:

<Double click here to view the manufacturer's product cards available at Deltek Specpoint>

GENERAL

SUMMARY

Section Includes: Surface preparation of interior substrates and application of the following:

Primers.

Water-based finish coatings.

Solvent-based finish coatings.

Floor sealers and paints.

Dry fall coatings.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed products and insert references to this Section to establish primer requirements.

[Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming structural steel substrates.

Section 055000 "Metal Fabrications" for shop priming metal fabrications.

Section 055113 "Metal Pan Stairs" for shop priming metal pan stairs.

Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

[Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

Section 099113 "Exterior Painting."

Section 099300 "Staining and Transparent Finishing" for surface preparation and application of wood stains and transparent finishes on interior wood substrates.

Section 099600 "High-Performance Coatings" for tile-like coatings.

DEFINITIONS

Retain this article if paints are specified by manufacturers' trade names rather than by paint numbers. Definitions of gloss levels are listed below.

Retain terms that remain after this Section has been edited for a project. Include only essential definitions or acronyms not well understood by the affected industry or trade.

Gloss Level 1: Not more than five units at 60 degrees and 10 units at 85 degrees, in accordance with ASTM D523.

Gloss Level 2: Not more than 10 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.

Gloss Level 3: 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.

Gloss Level 4: 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, in accordance with ASTM D523.

Gloss Level 5: 35 to 70 units at 60 degrees, in accordance with ASTM D523.

Gloss Level 6: 70 to 85 units at 60 degrees, in accordance with ASTM D523.

Gloss Level 7: More than 85 units at 60 degrees, in accordance with ASTM D523.

ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

Product Data: For each type of product.

Include preparation requirements and application instructions.

Indicate VOC content.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples. Delete "Samples" and "Samples for Initial Selection" paragraphs if colors and other characteristics are preselected and specified or scheduled and only verification Samples are required.

Samples: For each type of topcoat product.

Samples for Initial Selection: For each type of topcoat product.

Delete "Samples for Initial Selection" Paragraph above if colors and other characteristics are preselected and specified or scheduled. Retain "Samples for Verification" Paragraph below with or without above.

Samples for Verification: For each type of paint system and each color and gloss of topcoat. Submit [actual paint drawdowns as specified below] [paint manufacturer's standard printed cards] for verification Samples.

Retain subparagraphs below only if retaining first option in "Samples for Verification" Paragraph above for actual paint drawdowns for verification Samples. Color and gloss of Samples change as they age; seven-day old Samples appear different from freshly dried Samples.

Submit Samples on rigid backing, 8 inches (200 mm) square.

Apply coats on Samples in steps to show each coat required for system.

Label each coat of each Sample.

Label each Sample for location and application area.

Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in applicable interior painting schedule articles to cross-reference paint systems specified in this Section. Include color designations.

Retain "Sustainable Design Submittals" Paragraph below if required to attain sustainability rating or to track sustainability submittals.

Sustainable Design Submittals:

"Product Data" Subparagraph below applies to LEED v4, LEED v4.1, IgCC/ASHRAE 189.1, Green Globes, and CALGreen. Coordinate with requirements for paints and coatings.

Product Data: For paints and coatings, indicating VOC content.

"Environmental Product Declaration (EPD)" Subparagraph below applies to LEED v4 (all) MR Credit "Building Product Disclosure and Optimization - Environmental Product Declarations." Verify, with manufacturer, that EPDs are available for each product. Use at least 20 different permanently installed products from at least five different manufacturers.

Environmental Product Declaration (EPD): For each product.

"Health Product Declaration (HPD)" Subparagraph below applies to LEED v4 (all) MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting." Verify, with manufacturer, that HPDs are available and comply with requirements of the HPD Open Standard or USGBC-approved program.

Health Product Declaration (HPD): For each product.

"Sourcing of Raw Materials" Subparagraph below applies to LEED v4 (all) MR Credit "Building Project Disclosure and Optimization - Sourcing of Raw Materials," Option 1 - "Raw Material Source and Extraction Reporting." Verify, with manufacturer, that corporate sustainability reports are available, have been prepared within the last year or are applicable to the year of production, and are by USGBC-approved organization.

Sourcing of Raw Materials: Corporate sustainability report for each manufacturer.

"Environmental Product Declaration (EPD)" Subparagraph below applies to LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Environmental Product Declarations." Verify, with manufacturer, that EPDs are available for each product. Use at least 20 different permanently installed products from at least five different manufacturers.

Environmental Product Declaration (EPD): For each product.

"Health Product Declaration (HPD)" Subparagraph below applies to LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting." Verify, with manufacturer, that HPDs are available and comply with requirements of the HPD Open Standard or USGBC-approved program.

Health Product Declaration (HPD): For each product.

"Sourcing of Raw Materials" Subparagraph below applies to LEED v4.1 (all) MR Credit "Building Project Disclosure and Optimization - Sourcing of Raw Materials," Option 1 - "Raw Material Source and Extraction Reporting." Verify, with manufacturer, that corporate sustainability reports are available, have been prepared within the last year or are applicable to the year of production, and are by USGBC-approved organization.

Sourcing of Raw Materials: Corporate sustainability report for each manufacturer.

Retain first "Environmental Product Declaration (EPD)" Subparagraph below if products specified in this Section are required to have an EPD to comply with IgCC/ASHRAE 189.1's requirement of 55 percent recycled materials. Use at least 20 different permanently installed products from at least five different manufacturers.

Environmental Product Declaration (EPD): For each product.

First "Environmental Product Declaration (EPD)" Subparagraph below applies to IgCC/ASHRAE 189.1 if products specified in this Section are used to comply with requirements of paragraph 9.4.1.4, "Multiple-Attribute Product Declaration or Certification," which require EPDs for a minimum of 10 products.

Environmental Product Declaration (EPD): For each product.

Three subparagraphs below apply to Green Globes v1.4 if products specified in this Section are used to comply with requirements of paragraph 3.5.1.2, "Path B: Prescriptive Path for Building Core and Shell," which require that a certain percentage of materials used in the core and shell have EPDs, third-party certifications, and/or third-party life-cycle assessments. Use at least 20 different permanently installed products from at least five different manufacturers.

Environmental Product Declaration (EPD): For each product.

Third-Party Certifications: For each product.

Third-Party-Certified Life-Cycle Assessment: For each product.

MAINTENANCE MATERIAL SUBMITTALS

See Section 017700 "Closeout Procedures" for submission of maintenance material items.

Furnish extra materials that match paint products applied and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint Products" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

Paint Products: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert value> of each material and color applied.

MOCKUPS

Apply mockups of each paint system indicated and each color and finish selected to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

Architect will select one surface to represent surfaces and conditions for application of each paint system.

Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

Other Items: Architect will designate items or areas required.

Final approval of color selections will be based on mockups.

If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Owner specifically approves such deviations by Change Order.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site in paragraph below.

Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

Maintain containers in clean condition, free of foreign materials and residue.

Remove rags and waste from storage areas daily.

FIELD CONDITIONS

Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

Do not apply paints when relative humidity exceeds 85 percent; at temperatures of less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

PRODUCTS

Manufacturers and products listed in this Section are neither recommended nor endorsed by the AIA or Deltek. Before selecting manufacturers and products, verify availability, suitability for intended applications, and compliance with minimum performance requirements. Product options commonly available from manufacturers are included in square brackets throughout the Section Text. Not every manufacturer listed can provide every option offered; verify availability with manufacturers. For definitions of terms and requirements for Contractor's product selection, see Section 016000 "Product Requirements."

Retain "Source Limitations" Article below to limit sources for the entire Section. Source limitations may also be specified in individual articles if desired.

SOURCE LIMITATIONS

Obtain each paint product from single source from single manufacturer.

INTERIOR PAINTS, GENERAL

Interior Paints: Subject to compliance with requirements, [provide product] [provide one of the products] [available products that may be incorporated into the Work include but are not limited to products] listed in product types below and applicable interior painting schedule articles for the paint category indicated.

Generally, retain "Material Compatibility" Paragraph below. Systems could fail if paints used for separate coats are incompatible.

Material Compatibility:

Materials for use within each paint system must be compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer based on testing and field experience.

For each coat in a paint system, provide products recommended in writing by topcoat manufacturer for use in paint system and on substrate indicated.

"VOC Content" and "Low-Emitting Materials" paragraphs below apply to LEED v4 and LEED v4.1 EQ Credit "Low-Emitting Materials." Delete option in "VOC Content" Paragraph for LEED v4.1 for Schools and LEED v4.1 for Healthcare credit for exterior-applied products.

For interior applications, LEED v4 or LEED v4.1 compliance, 100 percent of interior applied paint and coatings products by volume must comply with wet-applied VOC content limits. Paint and coatings wet-applied on site must comply with applicable VOC limits of the California Air Resources Board (CARB) 2007, Suggested Control Measure (SCM) for Architectural Coatings, or the South Coast Air Quality Management District (SCAQMD) Rule 1113, effective June 3, 2011. Both the CARB 2007 SCM and SCAQMD Rule 1113 are cited in the LEED v4 EQ Credit 2, "Low-Emitting Materials Reference Guide." Choose one wet-applied VOC content limit compliance path below, either CARB or SCAQMD.

For CARB 2007 SCM, see https://ww2.arb.ca.gov/our-work/programs/coatings/architectural-coatings/suggested-control-measure.

For SCAQMD Rule 1113 (more restrictive), see latest updated version amended February 5, 2016, at www.aqmd.gov/docs/default-source/rule-book/reg-xi/r1113.pdf.

VOC Content: For field applications[ that are inside the weatherproofing system], verify paints and coatings comply with VOC content limits of authorities having jurisdiction and the following VOC content limits:

Categories in subparagraphs below are taken from LEED rating systems and the standards referenced by them; if clarification is required, see those documents or the reference guides.

In general, avoid paint systems using alkyd primers and topcoats for compliance with LEED v4. These products are not likely to comply with VOC content cutoff limits or the emissions certification requirements of LEED v4.

SCAQMD and CARB apply to "Flat Paints and Coatings" Subparagraph below.

Flat Paints and Coatings: 50 g/L.

Retain first option in "Nonflat Paints and Coatings" Subparagraph below for SCAQMD; second, for CARB.

Nonflat Paints and Coatings: [50 g/L] [100 g/L].

Retain first option in "Nonflat - High-Gloss Coatings" Subparagraph below for SCAQMD; second, for CARB.

Nonflat - High-Gloss Coatings: [50 g/L] [150 g/L].

Primers, Sealers, and Undercoaters: 100 g/L.

Retain first option in "Rust-Preventive Coatings" below for South Coast; second, for CARB.

Rust-Preventive Coatings: [100 g/L] [250 g/L].

Retain first option in "Zinc-Rich Industrial Maintenance Primers" Subparagraph below for SCAQMD; second, for CARB.

Zinc-Rich Industrial Maintenance Primers: [100 g/L] [340 g/L].

Pretreatment Wash Primers: 420 g/L.

Retain first option in "Floor Coatings" Subparagraph below for SCAQMD; second, for CARB.

Floor Coatings: [50 g/L] [100 g/L].

Retain first option in "Industrial Maintenance Coatings" Subparagraph below for SCAQMD; second, for CARB.

Industrial Maintenance Coatings: [100 g/L] [250 g/L].

Shellacs, Clear: 730 g/L.

Shellacs, Pigmented: 550 g/L.

Consult a Pittsburgh Paints Architectural Representative or Pittsburgh Paints Technical Service about the compliance of individual products. Emissions testing certificates in accordance with LEED v4 may be found through publicly available sites such as those posted to UL SPOT (Greenguard Gold) or SCS Indoor Advantage Gold, as well as the Pittsburgh Paints website; see www.ppgpaints.com/products/ecological-solutions/certifications-leed/usgbc-leed-v4.

Low-Emitting Materials: For field applications that are inside the weatherproofing system, verify 90 percent of paints and coatings comply with requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers."

"Material Emissions and Pollutant Control" Paragraph below applies to IgCC/ASHRAE 189.1.

Material Emissions and Pollutant Control: Verify not less than 85 percent of field-applied paints and coatings that are inside the weatherproofing system comply with either of the following:

Low-Emitting Materials: Verify VOC emissions comply with requirements of the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." Verify formaldehyde emissions do not exceed 9 mcg/cu. m or 7 ppb, whichever is less.

Verify VOC content does not exceed limits of authorities having jurisdiction and the following:

Flat Coatings: 50 g/L.

Nonflat Coatings: 100 g/L.

Nonflat - High-Gloss Coatings: 150 g/L.

Concrete/Masonry Sealers: 100 g/L.

Floor Coatings: 100 g/L.

Industrial Maintenance Coatings: 250 g/L.

Low-Solids Coatings: 120 g/L.

Mastic Texture Coatings: 100 g/L.

Metallic Pigmented Coatings: 500 g/L.

Pretreatment Wash Primers: 420 g/L.

Primers, Sealers, and Undercoaters: 100 g/L.

Reactive Penetrating Sealers: 350 g/L.

Recycled Coatings: 250 g/L.

Rust-Preventive Coatings: 250 g/L.

"VOC Emissions" Paragraph below applies to Green Globes.

VOC Emissions: For field applications inside the building, wall paints to contain no more than half of the chronic REL of VOCs when tested in accordance with the California Department of Public Health's "Standard Method for the Testing and Evaluation of Volatile Organic Chemical Emissions from Indoor Sources Using Environmental Chambers." The building concentration of formaldehyde will not exceed half of the indoor recommended exposure limit or 33 mcg/cu. m and that of acetaldehyde will not exceed 9 mcg/cu. m.

Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule] <Insert requirements>.

[10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

PRIMERS

Latex Block Filler: Water-based, pigmented, high-solids, emulsion coating formulated to bridge and fill porous surfaces of CMU substrates in preparation for specified subsequent coatings.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

The Pittsburgh Paints Company's "Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI" and "Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI" block fillers are LEED v4.1 wet-applied VOC-content-limit compliant at 100 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use The Pittsburgh Paints Company's "Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI."

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT] [Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT] or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Alkali-Resistant, Water-Based Primer: Water-based primer formulated for use on alkaline substrates.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Seal Grip Gripper Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT] [Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT] or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Interior Latex Primer Sealer: Pigmented, water-based latex sealer; formulated to reduce porosity of substrate for finish coats; for use on new interior plaster, concrete, and gypsum board substrates. Not intended for use on wood or previously painted surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Pittsburgh Paints's "Speedhide Interior Latex Quick-Drying Sealer, 6-2," "Speedhide Zero Interior Latex Sealer, 6-4900XI," and "Pure Performance Interior Latex Primer, 9-900" primers comply with wet-applied VOC content limits and emission requirements of LEED v4.1.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Speedhide Interior Latex Quick-Drying Sealer, 6-2; applied at 1.0 mils minimum DFT] [Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT] [Pure Performance Interior Latex Primer, 9-900; applied at 1.4 mils minimum DFT] or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Interior, Institutional Low-Odor/VOC Primer Sealer: Water-based primer sealer with low-odor characteristics and a VOC of less than 10 grams per liter for use on new interior plaster, concrete, and gypsum wallboard surfaces that are subsequently to be painted with latex finish coats.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Speedhide Zero Interior Latex Sealer, 6-4900XI; applied at 1.4 mils minimum DFT] [Pure Performance 100% Acrylic Latex Primer, 9-900; applied at 1.4 mils minimum DFT] or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Interior, Latex Primer for Wood: Waterborne-emulsion primer formulated for resistance to extractive bleeding, mold, and microbials; for hiding stains; and for use on interior wood substrates.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Pittsburgh Paints's "Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series" primer complies with wet-applied VOC content limits of LEED v4.1. Use "Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series" for emissions compliance with LEED v4.1.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Interior Alkyd Primer Sealer: Solvent-based, alkyd-type, primer/sealer for new interior wood, plaster, and porous surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based Alkyd Primer Sealer: Waterborne-emulsion primer/sealer formulated for new interior gypsum board and plaster substrates.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Rodda Paint Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based, Rust-Inhibitive Primer: Corrosion-resistant, water-based-emulsion primer; formulated for resistance to flash rusting when applied to cleaned, ferrous metal substrates subject to mildly corrosive environments.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908, applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Quick-Drying, Alkyd Metal Primer: Corrosion-resistant, solvent-based, modified-alkyd primer; lead and chromate free; formulated for quick-drying capabilities and for use on cleaned, ferrous metal substrates.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Alkyd Metal Primer: Corrosion-resistant, solvent-based, alkyd primer formulated for use on prepared ferrous metal substrates subject to industrial and light marine environments.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; [Multiprime Multi-Purpose Primer, 4160; applied at 2.0 mils minimum DFT] [Speedhide LV Alkyd Metal Primer, 6-212N Series; applied at 1.5 mils minimum DFT] or comparable product by one of the following:

Benjamin Moore & Co.

Hempel (USA), Inc.

McCormick Paints.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Epoxy, Anticorrosive Primer: Solvent-based, two-component, epoxy, anti-corrosive primer; formulated for use on ferrous and galvanized metal substrates.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide PPG Protective and Marine Coatings; [Amercoat 235 Multi-Purpose Phenalkamine Epoxy; applied at 4.0 mils minimum DFT] [Amerlock 600 Multi-Purpose Epoxy Coating; applied at 5.0 to 10.0 mils DFT] [Amerlock 2 AL Aluminum Epoxy Mastic; applied at 4.0 mils minimum DFT] or comparable product by one of the following:

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Surface-Tolerant Metal Primer: Corrosion-resistant, solvent-based metal primer formulated for use on structural steel and metal fabrications that have been minimally prepared.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based, Galvanized-Metal Primer: Corrosion-resistant, pigmented, acrylic primer; formulated for use on cleaned/etched galvanized metal substrates to prepare it for subsequent water-based coatings.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1912; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Quick-Drying Aluminum Primer: Corrosion-resistant, solvent-based, alkyd or modified-alkyd primer formulated for quick-drying capabilities and for use on prepared aluminum substrates.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

<Insert manufacturer's name>.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Vinyl Wash Primer: Two-component, vinyl butyral/phosphoric acid-wash primer formulated for use over cleaned ferrous metal substrates and zinc-rich primers as a tie coat for subsequent corrosion-resistant primers or finish coatings.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Water-Based Bonding Primer: Water-based-emulsion primer formulated to promote adhesion of subsequent specified coatings.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Gripper Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Solvent-Based Bonding Primer: Solvent-based primer formulated to seal substrates and promote adhesion of specified subsequent coatings.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Wood-Knot Sealer: White shellac or other sealer recommended in writing by manufacturer for this purpose.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Shop-Applied Primer: Quick-dry shop primer for application to interior structural steel. Intended to withstand exposure to essentially noncorrosive interior environments.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Quick Dry Shop Coat Primer, 4190; applied at 2.0 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Textured Latex Coating, Gloss Level 1: Pigmented, water-based coating, containing a coarse or medium-sized sand or other hard aggregate, for use on exterior masonry, concrete, and concrete block.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

Pittsburgh Paints's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

WATER-BASED FINISH COATINGS

Interior Latex Paint: Pigmented, water-based coating for use on interior primed/sealed plaster and gypsum board, and on primed wood and metals.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 1

- [Speedhide Pro-EV Zero Interior Latex Flat, 12-110XI Series; applied at 1.3 mils minimum DFT]

- [Speedhide low VOC Interior Latex Ultra-Flat, 6-0011 Series; applied at 1.3 mils minimum DFT]

- [Speedhide low VOC Interior Latex Flat, 6-70 Series; applied at 1.3 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Ultra-Flat, 6-0011ZV Series; applied at 1.3 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Flat, 6-70ZV Series; applied at 1.3 mils minimum DFT]

- [Hi-Hide Interior Latex Ultra-Flat, 679-10 Series; applied at 1.6 mils minimum DFT]

- [Hi-Hide Interior Latex Flat, 689-10 Series; applied at 1.1 mils minimum DFT]

- [Hi-Hide Interior Latex Ceramic Matte, 369-10 Series; applied at 1.4 mils minimum DFT]

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT]

- Gloss Level 2

- [Speedhide Pro-EV Zero Interior Latex Eggshell, 12-310XI Series; applied at 1.3 mils minimum DFT]

- [Speedhide low VOC Interior Latex Eggshell, 6-411 Series; applied at 1.5 mils minimum DFT]

- [Speedhide low VOC Interior Latex Low Sheen Eggshell, 6-4101 Series; applied at 1.5 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Eggshell, 6-411ZV Series; applied at 1.5 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Low Sheen Eggshell, 6-4101ZV Series; applied at 1.5 mils minimum DFT]

- [Hi-Hide Interior Latex Eggshell, 389-10 Series; applied at 1.4 mils minimum DFT]

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT]

- Gloss Level 3

- [Speedhide low VOC Interior Latex Satin, 6-3511 Series; applied at 1.3 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Satin, 6-3511ZV Series; applied at 1.4 mils minimum DFT]

- Gloss Level 4

- [Speedhide low VOC Interior Latex Lo Lustre, 6-3011 Series; applied at 1.2 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Lo Lustre, 6-3011ZV Series; applied at 1.2 mils minimum DFT]

- [Hi-Hide Interior Latex Satin, 379-10 Series; applied at 1.1 mils minimum DFT]

- Gloss Level 5

- [Speedhide Pro-EV Zero Interior Latex Semi-Gloss, 12-510XI Series; applied at 1.2 mils minimum DFT]

- [Speedhide low VOC Interior Latex Semi-Gloss, 6-500 Series; applied at 1.4 mils minimum DFT]

- [Speedhide zero VOC Interior Latex Semi-Gloss, 6-500ZV Series; applied at 1.5 mils minimum DFT]

- [Hi-Hide Interior Latex Semi-Gloss, 109-10 Series; applied at 1.4 mils minimum DFT]

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT]

- [Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT]

- Gloss Level 6

- [Speedhide Interior/Exterior Acrylic Paint High Gloss, 6-8534 Series; applied at 1.4 mils minimum DFT]

- [Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT]

- [Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Interior, Latex, Institutional Low-Odor/VOC Paint: White or colored latex coating with low-odor characteristics and a VOC of less than 10 grams per liter, for use in areas, such as hospitals and other occupied buildings, where the odor and VOC levels of conventional latex products would preclude their use.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 1

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.5 mils minimum DFT]

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT]

- Gloss Level 2

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT]

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT]

- [Speedhide Max Interior Acrylic Paint Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT]

- Gloss Level 3

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT]

- [Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT]

- [Speedhide Max Interior Acrylic Paint Satin, 6-9410; applied at 1.4 mils minimum DFT]

- Gloss Level 4

- Speedhide Max Interior Acrylic Paint Lo Lustre, 6-9610; applied at 1.4 mils minimum DFT

- Gloss Level 5

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT]

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Semi-Gloss, 84-3510 Series; applied at 1.6 mils minimum DFT]

- [Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Interior, Water-Based Light Industrial Coating: Pigmented, water-based emulsion coating for interior primed wood and metal surfaces (e.g., walls, doors, frames, trim, and sash), providing resistance to moderate abrasion and mild chemical exposure and corrosive conditions.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 3

- [Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT]

- [Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT]

- Gloss Level 5

- [Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT]

- [Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT]

- [Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT]

- Gloss Level 6

- [Advantage 900 Interior/Exterior Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT]

- [Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [eggshell] [semigloss] [gloss].

Interior, High-Performance Architectural Latex: Water-based, pigmented, low-VOC, emulsion coating formulated to provide a significantly higher level of performance than conventional latex paints in the areas of scrub resistance, burnish resistance, and ease of stain removal.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 1

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Flat, 9-110XI Series; applied at 1.4 mils minimum DFT]

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Flat, 84-3110 Series; applied at 1.8 mils minimum DFT]

- Gloss Level 2

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Eggshell, 9-310XI Series; applied at 1.4 mils minimum DFT]

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Eggshell, 84-3310 Series; applied at 1.6 mils minimum DFT]

- [Speedhide Max Interior Acrylic Paint Eggshell, 6-9310 Series; applied at 1.3 mils minimum DFT]

- Gloss Level 3

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Satin, 84-3410 Series; applied at 1.6 mils minimum DFT]

- [Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Eggshell, 16-1310 Series; applied at 1.5 mils minimum DFT]

- [Speedhide Max Interior Acrylic Paint Satin, 6-9410; applied at 1.4 mils minimum DFT]

- Gloss Level 4

- Speedhide Max Interior Acrylic Paint Lo Lustre, 6-9610; applied at 1.4 mils minimum DFT

- Gloss Level 5

- [Pure Performance Paint & Primer in One, 100% Acrylic Latex Semi-Gloss, 9-510XI Series; applied at 1.5 mils minimum DFT]

- [Prominence Interior 100 Percent Acrylic Latex Paint & Primer in One Satin, 84-3510 Series; applied at 1.6 mils minimum DFT]

- [Advantage 900 Interior/Exterior Acrylic Semi-Gloss, 919-10 Series; applied at 1.5 mils minimum DFT]

- [Pitt-Glaze WB1 Interior High Performance Pre-Catalyzed Waterborne Epoxy Semi-Gloss, 16-1510 Series; applied at 1.6 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [low sheen] [eggshell] [satin] [semigloss].

High-Performance Textured Latex Coating: Water-based, pigmented, self-priming coating that contains sand or other hard aggregate for selected texture and is formulated for use on concrete and masonry substrates.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Pittsburgh Paints's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [nonflat].

Texture: [Manufacturer's standard] [Fine] [Medium] [Coarse].

Interior, Water-Based Alkyd Paint: Water-based, pigmented, low-VOC alkyd paint formulated for flash rust and water resistance and for use on interior, primed, wood, plaster, masonry, and metal surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Pittsburgh Paints's "Speedhide Interior/Exterior WB Alkyd" product line, at 100 g/L or less and complies with VOC content limits in accordance with LEED v4.1.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 3

- Speedhide Interior/Exterior WB Alkyd Satin, 6-1410XI Series; applied at 1.4 mils minimum DFT

- Gloss Level 5

- Speedhide Interior/Exterior WB Alkyd Semi-Gloss, 6-1510XI Series; applied at 1.4 mils minimum DFT

- Gloss Level 6 and 7

- Speedhide Interior/Exterior WB Alkyd Gloss, 6-1610XI Series; applied at 1.4 mils minimum DFT

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [low sheen] [semigloss] [gloss].

Interior Latex, Antiviral/Antibacterial Coating: Water-based, pigmented, low-VOC paint with EPA-registered proprietary antimicrobial copper ion technology formulated to kill 99 percent of viruses and bacteria within 2 hours, for use on interior, primed, concrete, masonry, metal, wood, gypsum board, and plaster surfaces.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Behr Paint Company (Behr Process LLC).

<Insert manufacturer's name>.

Gloss Level: Manufacturer's standard [eggshell] [semigloss].

SOLVENT-BASED FINISH COATINGS

Interior Alkyd Paint: Pigmented, solvent-based alkyd coating for use on primed/sealed interior plaster, gypsum, wood, and metal substrates primarily in moderate traffic commercial environments.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 3

- Glyptex Interior Alkyd Enamel Satin, 39-10 Series; applied at 2.2 mils minimum DFT

- Gloss Level 5

- [Glyptex Interior Alkyd Enamel Semi-Gloss, 439-10 Series; applied at 2.0 mils minimum DFT]

- [HPC Industrial Alkyd 4306 Semi-Gloss, 4306-0110 Series; applied at 2.0 mils minimum DFT]

- Gloss Level 6 and 7

- [Glyptex Interior/Exterior Alkyd Enamel Gloss, 4139-10 Series; applied at 1.8 mils minimum DFT]

- [7 Line LV Interior/Exterior Industrial Alkyd Gloss, 7-282N Series; applied at 2.0 mils minimum DFT]

- [HPC Industrial Alkyd 4308H Gloss, 4308-0100H Series; applied at 2.0 mils minimum DFT]

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [eggshell] [semigloss] [gloss].

Aluminum Paint: Aliphatic, solvent-based coating consisting of varnish or alkyd binder combined with aluminum pigment that is formulated for use as a stain-blocking coating and sealer, is able to be recoated with conventional alkyd and latex paints, and for use on wood, metal, bituminous-coated, and prepared masonry substrates.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Benjamin Moore & Co.

Rodda Paint Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Quick-Drying Alkyd Enamel: Solvent-based, alkyd or modified-alkyd enamel formulated for quick-drying capabilities and for use on exterior, primed, metal and dimensionally stable wood surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product.

          - Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 5

- [HPC Alkyd Semi-Gloss, 4306 Series; applied at 2.0 mils minimum DFT]

- [HPC Urethane Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT]

- Gloss Level 6 and 7

- [Fast Dry 35 Interior/Exterior Alkyd Gloss, 95-912 Series; applied at 1.0 mil minimum DFT]

- [HPC Urethane Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT]

- or comparable product by one of the following:

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [eggshell] [semigloss] [gloss].

FLOOR SEALERS AND PAINTS

Concrete Stain: Penetrating semitransparent stain specifically manufactured for interior and exterior concrete horizontal and vertical surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete Color Seal WB Interior/Exterior 100% Acrylic Concrete Stain, 4-4210XI Series; applied at 1.3 mils minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Latex Floor Enamel: Water-based, pigmented coating formulated to hide stains, for alkali and incidental water resistance, and for use on concrete and primed-wood substrates subject to low to medium foot traffic.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510XI Series; applied at 1.0 mil minimum DFT or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Provide maximum Gloss Level 3.

Gloss and Sheen Level: Manufacturer's standard [low gloss] [gloss].

Retain "Slip-Resistant Aggregate" Subparagraph below if required.

Slip-Resistant Aggregate: Manufacturer's standard additive.

Alkyd Floor Enamel: Solvent-based, pigmented coating; self-priming where applied to bare wood; formulated to hide stains, for durability, for microbial and abrasion resistance, and for use on wood-board substrates subject to low to medium foot traffic.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Floor & Porch Waterborne Alkyd Gloss, 3-610 Series; applied at 1.3 mils minimum DFT.

Provide a Gloss Level 6.

Gloss Level: Manufacturer's standard [low gloss] [gloss].

Retain "Slip-Resistant Aggregate" Subparagraph below if required.

Slip-Resistant Aggregate: Manufacturer's standard additive.

Water-Based Concrete Floor Sealer: Clear, water-based, acrylic-copolymer-emulsion sealer formulated for oil, gasoline, alkali, and water resistance and for use on concrete traffic surfaces.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Perma-Crete Plex-Seal WB Interior/Exterior 100% Acrylic Clear Sealer, 4-6200XI Series; applied at 0.8 mil minimum DFT or comparable product by one of the following:

Solvent-Based Concrete Floor Sealer: Clear, acrylic, solvent-based sealer formulated for oil, gasoline, alkali, and water resistance and for use on concrete traffic surfaces.

Retain "Manufacturers" Subparagraph and list of manufacturers below to require products from manufacturers listed or a comparable product from other manufacturers.

Manufacturers: Subject to compliance with requirements, provide products by one of the following:

Benjamin Moore & Co.

H&C Decorative Concrete Products; a brand of Sherwin-Williams Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

DRY FALL COATINGS

Dry Fall, Latex: Pigmented, water-based, emulsion-type, fast-drying coating for use on interior plaster, concrete, gypsum board, primed wood, and metal ceilings.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Pittsburgh Paints's "Speedhide Super Tech WB Latex Dry Fog" line is LEED v4.1 wet-applied VOC-content-limit compliant at 50 g/L or less VOC content. For emissions certification in accordance with LEED v4.1, use "Speedhide Super Tech WB Flat 6-725XI Series" or "Speedhide Super Tech WB Semi-Gloss 6-727XI."

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 1

- Speedhide Super Tech WB Interior Latex Dry Fog, Flat 6-725XI Series; applied at 2.2 mils minimum DFT

- Gloss Level 3

- Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Eggshell 6-724XI Series; applied at 2.0 mils minimum DFT

- Gloss Level 5

- Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Semi-Gloss 6-727XI Series; applied at 2.2 mils minimum DFT

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [eggshell] [semigloss].

Dry Fall, Water-Based for Galvanized Steel: Pigmented, water-based coating for direct application to cleaned, interior galvanized-metal ceiling surfaces and adjacent primed metals.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 1

- Speedhide Super Tech WB Interior Latex Dry Fog, Flat 6-725XI Series; applied at 2.2 mils minimum DFT

- Gloss Level 3

- Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Eggshell 6-724XI Series; applied at 2.0 mils minimum DFT

- Gloss Level 5

- Speedhide Super Tech WB Interior 100% Acrylic Latex Dry Fog, Semi-Gloss 6-727XI Series; applied at 2.2 mils minimum DFT

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [eggshell] [semigloss].

Dry Fall, Alkyd: Pigmented, solvent-based, fast-setting, alkyd coating for use on interior ceiling substrates such as primed plaster, gypsum board, wood, and metals.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints;

- Gloss Level 1

- Speedhide Interior Alkyd Dry Fog, Flat 6-160XI Series; applied at 2.3 mils minimum DFT

- Gloss Level 3

- Speedhide Interior Alkyd Dry Fog, Eggshell 6-151XI Series; applied at 1.6 mils minimum DFT

- Gloss Level 5

- Speedhide Interior Alkyd Dry Fog, Low Lustre Semi-Gloss 6-161XI Series; applied at 3.1 mils minimum DFT

- or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Gloss and Sheen Level: Manufacturer's standard [flat] [eggshell] [semigloss].

TRAFFIC MARKING PAINTS

Traffic Marking Paint, Latex: A water-based, latex-type, pigmented coating used for interior or exterior, zone and parking line marking. May be used in residential, commercial, and industrial locations.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Ennis-Flint [Federal Specification Fast Dry Waterborne Paint, 98520x Series] [Fast Dry Waterborne Paint, 98530x Series] or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

Traffic Marking Paint, Solvent: A solvent-based paint available in standard yellow and white for roads or parking areas as a zone marking paint. May be used in residential, commercial, and industrial locations.

Retain "Basis-of-Design Product" Subparagraph below to require a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints; Ennis-Flint Low VOC Traffic Paint, 98515x Series or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in subparagraphs below are based on manufacturer's written instructions.

Concrete: 12 percent.

Cementitious Composition Board: 12 percent.

Masonry (Clay and CMU): 12 percent.

Wood: 15 percent.

Gypsum Board: 12 percent. Verify that finishing compound is dry and sanded smooth.

Plaster: 12 percent. Verify that plaster is fully cured.

Verify suitability of substrates, including surface conditions and compatibility, with finishes and primers. Proceed with coating application only after unsatisfactory conditions have been corrected.

Application of coating indicates acceptance of surfaces and conditions.

PREPARATION

For renovation or maintenance projects where repainting is required, consult manufacturers for recommendations and revise first paragraph below and paint systems specified in the Interior Painting Schedule.

Comply with manufacturer's written instructions applicable to substrates and paint systems indicated.

Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection if any.

Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints to be painted exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

Steel Substrates: Remove loose rust, loose mill scale, loose shop primer, and other loose foreign matter. Clean using methods recommended in writing by paint manufacturer[.] [ but not less than the following:]

Usually, retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

SSPC-SP 2.

SSPC-SP 3.

SSPC-SP 7/NACE No. 4 permits tight residues of rust, mill scale, and coatings to remain. Be aware that blast-cleaning methods may not be practical for use at Project site and may not be allowed by authorities having jurisdiction.

SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized Metal Substrates: Remove grease and oil residue from galvanized metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

Aluminum Substrates: Remove loose surface oxidation.

Wood Substrates:

Scrape and clean knots. Before applying primer, apply coat of knot sealer recommended in writing by topcoat manufacturer for interior use in paint system indicated.

Sand surfaces that will be exposed to view and remove sanding dust.

Prime edges, ends, faces, undersides, and backsides of wood.

After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

Canvas and Cotton Insulation Covering Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

Plastic Trim Fabrication Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

APPLICATION OF INTERIOR PAINT PRODUCTS

Apply paints in accordance with manufacturer's written instructions.

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

Use applicators and techniques suited for paint and substrate indicated.

Paint surfaces behind movable equipment and furniture same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed equipment or furniture with prime coat only.

Paint front and backsides of access panels, removable or hinged covers, and similar hinged items to match exposed surfaces.

Retain first subparagraph below if required for steel windows.

Paint entire exposed surface of window frames and sashes.

Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

Primers specified in the applicable interior painting schedule articles may be omitted on items that are factory primed or factory finished if compatible with intermediate and topcoat coatings and acceptable to intermediate and topcoat paint manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Tint undercoats to match color of topcoat but provide sufficient difference in shade of undercoats to distinguish each separate coat.

If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

Painting Fire-Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

First subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

Paint the following work where exposed to view in equipment rooms:

Subparagraphs below contain items that are often field painted, plus others that are often not. Revise list to suit Project.

Equipment, including panelboards[ and switch gear].

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Tanks that do not have factory-applied final finishes.

Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

<Insert mechanical items to be painted>.

Paint the following work where exposed to view in occupied spaces:

Subparagraphs below contain items that are usually field painted. Revise list to suit Project.

Equipment, including panelboards.

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Duct, equipment, and pipe insulation having cotton or canvas insulation covering or other paintable jacket material.

Other items as directed by Architect.

<Insert requirements>.

Paint portions of internal surfaces of metal ducts, without liner, behind air inlets and outlets that are visible from occupied spaces.

FIELD QUALITY CONTROL

Dry-Film Thickness (DFT) Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for DFT.

Touch up and restore painted surfaces damaged by testing.

If test results show that DFT of applied paint does not comply with paint manufacturer's written recommendations, apply additional coats as needed to provide DFT that complies with paint manufacturer's written recommendations.

Cost of retesting is Contractor's responsibility.

CLEANING AND PROTECTION

At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

Do not clean equipment with free-draining water and prevent solvents, thinners, cleaners, and other contaminants from entering into waterways, sanitary and storm drain systems, and ground.

Dispose of contaminants in accordance with requirements of authorities having jurisdiction.

Allow empty paint cans to dry before disposal.

Retain subparagraph below if paint recycling or collection facilities are available in vicinity of Project.

Collect waste paint by type and deliver to recycling or collection facility.

After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

INTERIOR PAINTING SCHEDULE, CONCRETE SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Vertical (Nontraffic) Surfaces:

Latex System <Insert drawing designation>:

Prime Coat: [Alkali-resistant, water-based primer] [Matching topcoat].

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Latex Aggregate System <Insert drawing designation>:

Prime Coat: Textured latex coating, flat.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex Aggregate System <Insert drawing designation>:

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, [flat] [nonflat].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior, institutional low-odor/VOC primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [eggshell] [semigloss] [gloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Concrete Stain System <Insert drawing designation>:

First Coat: Matching topcoat.

Topcoat: Interior concrete stain.

Horizontal (Traffic) Surfaces:

Latex Floor Enamel System <Insert drawing designation>:

Prime Coat: Matching topcoat

Intermediate Coat: Matching topcoat.

Topcoat: Latex floor enamel, [low gloss] [gloss].

Alkyd Floor Enamel System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Alkyd floor enamel, [low gloss] [gloss].

Concrete Stain System <Insert drawing designation>:

First Coat: Matching topcoat.

Topcoat: Interior concrete stain.

Solvent-Based Concrete Floor Sealer System <Insert drawing designation>:

First Coat: Matching topcoat.

Topcoat: Solvent-based concrete floor sealer.

Water-Based Concrete Floor Sealer System <Insert drawing designation>:

First Coat: Matching topcoat.

Topcoat: Water-based concrete floor sealer.

Latex Zone/Traffic-Marking Paint System <Insert drawing designation>:

Traffic-marking paint, latex.

Alkyd Zone/Traffic-Marking Paint System <Insert drawing designation>:

Traffic-marking paint, solvent based.

INTERIOR PAINTING SCHEDULE, CEMENTITIOUS SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Cementitious Composition Board Substrates: [Siding] [Trim] [Panels] <Insert requirements>.

Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior, institutional low-odor/VOC primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [eggshell] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

INTERIOR PAINTING SCHEDULE, MASONRY SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Clay Masonry Substrates:

Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex Aggregate System <Insert drawing designation>:

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: Matching topcoat.

Topcoat: Textured latex coating, [flat] [nonflat].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior, institutional low-odor/VOC primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [eggshell] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Alkali-resistant, water-based primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

CMU Substrates:

Latex System <Insert drawing designation>:

Block Filler: Interior/exterior latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex Aggregate System <Insert drawing designation>:

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: Matching topcoat.

Topcoat: Textured latex coating, [flat] [nonflat].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Block Filler: Interior/exterior latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

[Block Filler: Interior/exterior latex block filler] [Prime Coat: Alkali-resistant, water-based primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Block Filler: Interior/exterior latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [eggshell] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Block Filler: Interior/exterior latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Block Filler: Interior/exterior latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Block Filler: Interior/exterior latex block filler.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

INTERIOR PAINTING SCHEDULE, METAL SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Steel and Iron Substrates:

Latex System, Alkyd Primer <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Alkyd metal primer] [Shop primer specified in Section where substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Shop-Applied Quick-Drying Shop Primer System <Insert drawing designation>:

Prime Coat: Quick-dry primer for shop application.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Water-based rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Alkyd metal primer] [Shop primer specified in Section where substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Primer, rust-inhibitive, water based.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [eggshell] [semigloss] [gloss].

Water-Based Light Industrial Coating System over Epoxy Primer System <Insert drawing designation>:

Prime Coat: Epoxy, anticorrosive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [eggshell] [semigloss] [gloss].

Water-Based Dry-Fall System <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Alkyd metal primer] [Shop primer specified in Section where substrate is specified].

Topcoat: [Dry fall, latex, flat] [Dry fall, water-based for galvanized steel, flat] [Dry fall, latex, low sheen] [Dry fall, latex, semigloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Alkyd quick-dry primer for metal.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Alkyd metal primer] [Shop primer specified in Section where substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd over Surface-Tolerant Primer System <Insert drawing designation>:

Prime Coat: Surface-tolerant metal primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd over Rust-Inhibitive Primer System <Insert drawing designation>:

Prime Coat: Primer, rust inhibitive, water based.

Intermediate Coat: Alkyd, interior, matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd over Shop-Applied Quick-Drying Shop Primer System <Insert drawing designation>:

Prime Coat: Primer, quick dry, for shop application.

Intermediate Coat: Alkyd, interior, matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Quick-dry primer for shop application] [Primer, rust inhibitive, water based] [Surface-tolerant metal primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Quick-Dry Enamel System <Insert drawing designation>:

Prime Coat: Alkyd quick-dry primer for metal.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Alkyd Dry-Fall System <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Alkyd metal primer] [Shop primer specified in Section where substrate is specified].

Topcoat: Dry fall, alkyd [flat] [low sheen] [semigloss].

Alkyd Dry Fall over Quick-Drying Primer System <Insert drawing designation>:

Prime Coat: Quick-dry primer for shop application.

Topcoat: Dry fall, alkyd [flat] [low sheen] [semigloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: [Alkyd quick-dry primer for metal] [Alkyd metal primer] [Shop primer specified in Section where substrate is specified].

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Galvanized metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate primers.

Galvanized Metal Substrates:

Latex System <Insert drawing designation>:

Prime Coat: [Cementitious galvanized primer] [Water-based galvanized primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Cementitious galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Water-Based Dry-Fall System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Topcoat: Dry fall, water-based for galvanized steel, flat.

Alkyd System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Alkyd Dry-Fall System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Topcoat: Dry fall, alkyd [flat] [low sheen] [semigloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: Water-based galvanized primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Aluminum (Not Anodized or Otherwise Coated) Substrates:

Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Primer, [Vinyl wash primer] [Quick-dry primer for aluminum].

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Copper Substrates:

Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Stainless Steel Substrates:

Latex System <Insert drawing designation>:

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Quick-dry primer for aluminum].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Quick-dry primer for aluminum.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Vinyl wash primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

INTERIOR PAINTING SCHEDULE, WOOD SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Glued-Laminated Wood Substrates:

Latex over Latex Primer System <Insert drawing designation>:

Prime Coat: Interior, latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Primer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Exposed Wood Framed Substrates:

Latex over Latex Primer System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Primer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Finish Carpentry Substrates: [Wood trim] [Doors] [Windows] [and] [Wood board paneling].

Latex over Latex Primer System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Primer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Architectural Woodwork Substrates: [Wood paneling] [and] [Casework].

Latex over Latex Primer System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Primer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Wood Traffic Substrates: [Floors] [and] [stairs].

Latex Porch and Floor Enamel System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Latex floor enamel, low gloss.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Alkyd Floor Enamel System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Alkyd floor enamel, gloss.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Wood Shingle and Shake Substrates:

Latex over Latex Primer System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Primer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Interior, alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

INTERIOR PAINTING SCHEDULE, GYPSUM-BASED SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Gypsum Board and Plaster Substrates:

Latex over Latex Sealer System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Primer System (for Plaster Only) <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior, institutional low-odor/VOC primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: [Interior latex primer sealer] [Interior, institutional low-odor/VOC primer sealer] [Interior alkyd primer sealer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd over Latex Sealer System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Interior latex primer for wood.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

INTERIOR PAINTING SCHEDULE, MISCELLANEOUS SUBSTRATES

Paint systems in this article are for new construction. For renovation or maintenance projects where repainting is required, revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs throughout this article for high-quality systems; delete if not required.

Fiberglass Substrates:

Latex System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: [Water-based bonding primer] [Solvent-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: [Interior latex primer sealer] [Interior, institutional low-odor/VOC primer sealer] [Interior alkyd primer sealer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Plastic Trim Fabrication Substrates:

Latex System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Water-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Water-Based Light Industrial Coating System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based, light industrial coating, [low sheen] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: [Interior latex primer sealer] [Interior, institutional low-odor/VOC primer sealer] [Interior alkyd primer sealer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Solvent-based bonding primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: [Solvent-based bonding primer] [Water-based bonding primer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

Spray-Textured Ceiling Substrates:

Latex, Flat System: Spray applied <Insert drawing designation>:

Prime Coat: Matching topcoat.

Topcoat: Interior latex paint, flat.

Latex System: Spray applied <Insert drawing designation>:

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Latex over Alkyd Sealer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Alkyd, Flat System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Topcoat: Interior alkyd paint, flat.

Alkyd over Alkyd Sealer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Acoustic Panels and Tiles:

Latex, Flat System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Topcoat: Interior latex paint, flat.

Latex over Alkyd Sealer System <Insert drawing designation>:

Prime Coat: Interior alkyd primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

High-Performance Architectural Latex System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, high-performance architectural latex, [low sheen] [eggshell] [satin] [semigloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: [Interior latex primer sealer] [Interior, institutional low-odor/VOC primer sealer] [Interior alkyd primer sealer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd, Flat System <Insert drawing designation>:

Prime Coat: Matching topcoat.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, flat.

Canvas and Cotton Insulation-Covering Substrates: Including [pipe and duct coverings] <Insert description>.

Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Institutional Low-Odor/VOC Latex System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, institutional low odor/VOC, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Antiviral/Antibacterial Latex System <Insert drawing designation>:

Prime Coat: [Interior latex primer sealer] [Interior, institutional low-odor/VOC primer sealer] [Interior alkyd primer sealer].

Intermediate Coat: Matching topcoat.

Topcoat: Interior, latex, antiviral/antibacterial coating, [eggshell] [semigloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: Interior latex primer sealer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Bituminous-Coated Substrates:

Latex System <Insert drawing designation>:

Prime Coat: Water-based rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior latex paint, [flat] [low sheen] [eggshell] [satin] [semigloss] [gloss].

Alkyd System <Insert drawing designation>:

Prime Coat: Water-based rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior alkyd paint, [flat] [low sheen] [semigloss] [gloss].

Aluminum Paint System <Insert drawing designation>:

Prime Coat: Water-based rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Aluminum paint.

Water-Based Alkyd System <Insert drawing designation>:

Prime Coat: Water-based, rust-inhibitive primer.

Intermediate Coat: Matching topcoat.

Topcoat: Interior, water-based alkyd paint, [low sheen] [semigloss] [gloss].

END OF SECTION 099123