Copyright 2024 by The American Institute of Architects (AIA)

Exclusively published and distributed by Deltek, Inc. for the AIA

This Product MasterSpec Section is licensed by Deltek, Inc. to The Pittsburgh Paints Company (formerly PPG Paints) ("Licensee"). The Pittsburgh Paints Company is the exclusive distributor of PPG Protective and Marine Coatings products.

This Product MasterSpec Section modifies the original MasterSpec text and does not include the full content of the original MasterSpec Section.

Revisions made to the original MasterSpec text are made solely by the Licensee and are not endorsed by, or representative of the opinions of, Deltek or The American Institute of Architects (AIA). Neither AIA nor Deltek are liable in any way for such revisions or for the use of this Product MasterSpec Section by any end user. A qualified design professional should review and edit the document to suit project requirements.

For more information, contact The Pittsburgh Paints Company, 400 Bertha Lamme Dr., Cranberry Township, PA 16066; Phone: (888) PPG-IDEA | (888) 774-4332, Option 4; Website: www.pittsburghpaints.com; Email: ppgspec@ppg.com.

For information about MasterSpec, contact Deltek at (800) 424-5080 or visit masterspec.com.

SECTION 099114 - EXTERIOR PAINTING (MPI STANDARDS)

Access Manufacturer's Specpoint Product Cards:

<Double click here to view the manufacturer's product cards available at Deltek Specpoint>

GENERAL

SUMMARY

Section Includes: Surface preparation of substrates and application of the following:

Exterior paint systems.

Related Requirements:

Retain subparagraphs below to cross-reference requirements Contractor might expect to find in this Section but are specified in other Sections.

Primers in other Sections must be coordinated for compatibility with finish coats specified in this Section. Review other Sections for shop-primed exterior products and insert references to this Section to establish primer requirements.

[Section 051200 "Structural Steel Framing"] [Section 051213 "Architecturally Exposed Structural Steel Framing"] for shop priming structural steel substrates.

Section 055000 "Metal Fabrications" for shop priming metal fabrications.

Section 055113 "Metal Pan Stairs" for shop priming metal pan stairs.

Section 055116 "Metal Floor Plate Stairs" for shop priming metal floor plate stairs.

Section 055119 "Metal Grating Stairs" for shop priming metal grating stairs.

Section 055213 "Pipe and Tube Railings" for shop [priming] [painting] pipe and tube railings.

[Section 055313 "Bar Gratings"] [Section 055316 "Plank Gratings"] [Section 055319 "Expanded Metal Gratings"] for shop priming metal gratings.

Section 099124 "Interior Painting (MPI Standards)."

Section 099301 "Staining and Transparent Finishing (MPI Standards)" for surface preparation and application of wood stains and transparent finishes on exterior wood substrates.

Section 099601 "High-Performance Coatings (MPI Standards)" for tilelike coatings.

DEFINITIONS

Definitions of MPI Gloss Levels below are from "MPI Architectural Painting Specification Manual" (hereafter, "MPI Manual").

MPI Gloss Level G1: Not more than five units at 60 degrees and 10 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G2: Not more than 10 units at 60 degrees and between 10 to 35 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G3: Between 10 to 25 units at 60 degrees and 10 to 35 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G4: Between 20 to 35 units at 60 degrees and not less than 35 units at 85 degrees, in accordance with ASTM D523.

MPI Gloss Level G5: Between 35 to 70 units at 60 degrees, in accordance with ASTM D523.

MPI Gloss Level G6: Between 70 to 85 units at 60 degrees, in accordance with ASTM D523.

MPI Gloss Level G7: More than 85 units at 60 degrees, in accordance with ASTM D523.

ACTION SUBMITTALS

Action submittals are submittals requiring responsive action and return of reviewed documents to Contractor.

Product Data: For each type of product.

See "Writing Guide" Article in the Evaluations for discussion of first subparagraph below.

Include printout of current "MPI Approved Products List" for each product category specified, with the proposed product highlighted.

Include preparation requirements and application instructions.

Indicate VOC content.

Retain "Samples" Paragraph below for single-stage Samples, with a subordinate list if applicable. Retain "Samples for Initial Selection" and "Samples for Verification" paragraphs for two-stage Samples. Delete "Samples" and "Samples for Initial Selection" paragraphs if colors and other characteristics are preselected and specified or scheduled and only verification Samples are required.

Samples: For each type of topcoat product.

Samples for Initial Selection: For each type of topcoat product.

Samples for Verification: For each type of paint system and each color and gloss of topcoat. Submit [actual paint drawdowns as specified below] [paint manufacturer's standard printed cards] for verification Samples.

Retain subparagraphs below only if retaining first option in "Samples for Verification" Paragraph above for actual paint drawdowns for verification Samples. Color and gloss of Samples change as they age; seven-day old Samples appear different from freshly dried Samples.

Submit Samples on rigid backing, 8 inches (200 mm) square.

Apply coats on Samples in steps to show each coat required for system.

Label each coat of each Sample.

Label each Sample for location and application area.

Product List: Cross-reference to paint system and locations of application areas. Use same designations indicated on Drawings and in applicable exterior painting schedule articles to cross-reference paint systems specified in this Section. Include color designations.

Retain "Sustainable Design Submittals" Paragraph below if required to attain sustainability rating or to track sustainability submittals.

Sustainable Design Submittals:

"Product Data" Subparagraph below applies to LEED v4 and LEED v4.1 for Schools and LEED v4 and LEED v4.1 for Healthcare. Coordinate with requirements for paints and coatings.

Product Data: For paints and coatings, indicating VOC content.

Retain first three subparagraphs below to be eligible for LEED v4 or LEED v4.1 credit. See the Evaluations.

"Environmental Product Declaration (EPD)" Subparagraph below applies to LEED v4 and LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Environmental Product Declarations." Verify, with manufacturer, that EPDs are available for each product.

Environmental Product Declaration (EPD): For each product.

"Health Product Declaration (HPD)" Subparagraph below applies to LEED v4 and LEED v4.1 (all) MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting." Verify, with manufacturer, that HPDs are available and comply with requirements of the HPD Open Standard or USGBC-approved program.

Health Product Declaration (HPD): For each product.

"Sourcing of Raw Materials" Subparagraph below applies to LEED v4 and LEED v4.1 (all) MR Credit "Building Project Disclosure and Optimization - Sourcing of Raw Materials," Option 1 - "Raw Material Source and Extraction Reporting." Verify, with manufacturer, that corporate sustainability reports are available, have been prepared within the last year or are applicable to the year of production, and are by USGBC-approved organization.

Sourcing of Raw Materials: Corporate sustainability report for each manufacturer.

Retain "Manufacturer Inventory" Subparagraph below for LEED v4 and LEED v4.1 MR Credit "Building Product Disclosure and Optimization - Material Ingredients," Option 1 - "Material Ingredient Reporting."

Manufacturer Inventory: For each product, provide manufacturer's manifest of ingredients.

MAINTENANCE MATERIAL SUBMITTALS

See Section 017700 "Closeout Procedures" for submission of maintenance material items.

Extra Stock Material: Furnish extra materials that match paint products applied and that are packaged with protective covering for storage and identified with labels describing contents.

If necessary, replace percentage in "Paint Products" Subparagraph below with a specific number of gallons (liters) or cases and include an expanded description of the quantity of each material and color.

Paint Products: [5] <Insert number> percent, but not less than [1 gal. (3.8 L)] <Insert value> of each material and color applied.

MOCKUPS

Apply mockups of each paint system indicated and each color and finish selected to verify selections made under Sample submittals, to demonstrate aesthetic effects, and to set quality standards for materials and execution.

Architect will select one surface to represent surfaces and conditions for application of each paint system.

Vertical and Horizontal Surfaces: Provide samples of at least 100 sq. ft. (9 sq. m).

Other Items: Architect will designate items or areas required.

Final approval of color selections will be based on mockups.

If preliminary color selections are not approved, apply additional mockups of additional colors selected by Architect at no added cost to Owner.

Approval of mockups does not constitute approval of deviations from the Contract Documents contained in mockups unless Owner specifically approves such deviations by Change Order.

Retain subparagraph below if the intention is to make an exception to the default requirement in Section 014000 "Quality Requirements" for demolishing and removing mockups.

Subject to compliance with requirements, approved mockups may become part of the completed Work if undisturbed at time of Substantial Completion.

DELIVERY, STORAGE, AND HANDLING

If necessary, insert special requirements for fire protection, heating, ventilation, and other conditions for storage areas on-site in paragraph below.

Store materials not in use in tightly covered containers in well-ventilated areas with ambient temperatures continuously maintained at not less than 45 deg F (7 deg C).

Maintain containers in clean condition, free of foreign materials and residue.

Remove rags and waste from storage areas daily.

FIELD CONDITIONS

Apply paints only when temperature of surfaces to be painted and ambient air temperatures are between 50 and 95 deg F (10 and 35 deg C).

Do not apply paints in snow, rain, fog, or mist; when relative humidity exceeds 85 percent; at temperatures less than 5 deg F (3 deg C) above the dew point; or to damp or wet surfaces.

PRODUCTS

Retain "Source Limitations" Article below to limit sources for the entire Section. Source limitations may also be specified in individual articles if desired.

SOURCE LIMITATIONS

Obtain each paint product from single source from single manufacturer.

EXTERIOR PAINTS, GENERAL

Retain "Exterior Paint Products" Paragraph below and include list of manufacturers if desired, in addition to MPI standards indicated and listed below.

See lists of products currently approved by MPI in its "MPI Approved Products List". See the "Writing Guide" Article in the Evaluations for further discussion.

Exterior Paint Systems: Subject to compliance with requirements, provide product listed in applicable exterior painting schedule articles for the paint category indicated.

Retain "Basis-of-Design Product" Paragraph and list of manufacturers below to identify a specific product or a comparable product from manufacturers listed.

Basis-of-Design Product: Subject to compliance with requirements, provide Pittsburgh Paints (formerly PPG Paints); products as designated in the Exterior Painting Schedule or comparable product by one of the following:

Behr Paint Company (Behr Process LLC).

Benjamin Moore & Co.

Sherwin-Williams Company (The).

<Insert manufacturer's name>.

MPI Standards: Provide products complying with MPI standards indicated in applicable exterior painting schedule articles and listed in the "MPI Approved Products List."

Generally, retain "Material Compatibility" Paragraph below. Systems could fail if paints used for separate coats are incompatible. MPI's paint systems match primers and topcoats and take compatibility into consideration.

Material Compatibility:

Provide materials for use within each paint system that are compatible with one another and substrates indicated, under conditions of service and application as demonstrated by manufacturer, based on testing and field experience.

For each coat in a paint system, provide products recommended in writing by topcoat manufacturers for use in paint system and on substrate indicated.

"VOC Content" Paragraph below applies to LEED v4 or LEED v4.1 for Schools and LEED v4 or LEED v4.1 for Healthcare credit for exterior-applied products.

VOC Content: For field applications, verify paints and coatings comply with VOC content limits of authorities having jurisdiction at Project location.

Colors: [As selected by Architect from manufacturer's full range] [Match Architect's samples] [As indicated in a color schedule on Drawings] <Insert requirements>.

[10] [20] [30] <Insert number> percent of surface area will be painted with deep tones.

EXECUTION

EXAMINATION

Examine substrates and conditions, with Applicator present, for compliance with requirements for maximum moisture content and other conditions affecting performance of the Work.

Maximum Moisture Content of Substrates: When measured with an electronic moisture meter as follows:

Percentages in subparagraphs below are based on MPI recommendations.

Concrete: 12 percent.

Cementitious Composition Board: 12 percent.

Masonry (Clay and CMU): 12 percent.

Wood: 15 percent.

Portland Cement Plaster (Stucco): 12 percent. Verify that plaster is fully cured.

Verify suitability of substrates, including surface conditions and compatibility, with existing finishes and primers. Proceed with coating application only after unsatisfactory conditions have been corrected.

Application of coating indicates acceptance of surfaces and conditions.

PREPARATION

For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise first paragraph below and paint systems specified in applicable exterior painting schedule articles.

Comply with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual" applicable to substrates and paint systems indicated.

Remove hardware, covers, plates, and similar items already in place that are removable and are not to be painted. If removal is impractical or impossible because of size or weight of item, provide surface-applied protection before surface preparation and painting.

After completing painting operations, use workers skilled in the trades involved to reinstall items that were removed. Remove surface-applied protection.

Clean substrates of substances that could impair bond of paints, including dust, dirt, oil, grease, and incompatible paints and encapsulants.

Coordination of shop-applied prime coats with topcoats is critical.

Remove incompatible primers and reprime substrate with compatible primers or apply tie coat as required to produce paint systems indicated.

Concrete Substrates: Remove release agents, curing compounds, efflorescence, and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces to be painted exceeds that permitted in manufacturer's written instructions.

Masonry Substrates: Remove efflorescence and chalk. Do not paint surfaces if moisture content or alkalinity of surfaces or mortar joints exceeds that permitted in manufacturer's written instructions.

Retain "Steel Substrates" Paragraph below if steel is not shop primed or if shop primer is removed in the field.

Steel Substrates: Remove loose rust, loose mill scale, loose shop primer, and other loose foreign matter. Clean using methods recommended in writing by paint manufacturer[.][ but not less than the following:]

Usually, retain one of first two subparagraphs below. SSPC-SP 2 and SSPC-SP 3 remove loose rust, mill scale, and paint. SSPC-SP 2 is minimum surface preparation accepted by AISC for painted steel.

SSPC-SP 2.

SSPC-SP 3.

SSPC-SP 7/NACE No. 4 "Brush-Off Blast Cleaning" permits tight residues of rust, mill scale, and coatings to remain. "Commercial Blast Cleaning" methods specified in SSPC-SP 6/NACE No. 3 may be impractical for use at Project site or allowed by authorities having jurisdiction.

SSPC-SP 7/NACE No. 4.

SSPC-SP 11 requires complete removal of rust, mill scale, and paint by power tools. SSPC-SP 11 uses nonabrasive methods and is more thorough than SSPC-SP 2, SSPC-SP 3, and SSPC-SP 7/NACE No. 4.

SSPC-SP 11.

Retain "Shop-Primed Steel Substrates" Paragraph below if primers are shop applied and are not removed in the field.

Shop-Primed Steel Substrates: Clean field welds, bolted connections, and areas where shop paint is abraded. Paint exposed areas with the same material as used for shop priming to comply with SSPC-PA 1 for touching up shop-primed surfaces.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized-Metal Substrates: Remove grease and oil residue from galvanized metal by mechanical methods to produce clean, lightly etched surfaces that promote adhesion of subsequently applied paints.

Aluminum Substrates: Remove loose surface oxidation.

Wood Substrates:

Scrape and clean knots. Before applying primer, apply coat of knot sealer recommended in writing by topcoat manufacturer for exterior use in paint system indicated.

Sand surfaces that will be exposed to view and remove sanding dust.

Prime edges, ends, faces, undersides, and backsides of wood.

After priming, fill holes and imperfections in the finish surfaces with putty or plastic wood filler. Sand smooth when dried.

Canvas and Cotton Insulation Covering Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

Plastic Trim Fabrication Substrates: Remove dust, dirt, and other foreign material that might impair bond of paints to substrates.

APPLICATION OF EXTERIOR PAINT PRODUCTS

Apply paints in accordance with manufacturer's written instructions and recommendations in "MPI Architectural Painting Specification Manual."

If Project requires restricted application method (e.g., using only spray or rollers), revise first subparagraph below accordingly.

Use applicators and techniques suited for paint and substrate indicated.

Paint surfaces behind movable items same as similar exposed surfaces. Before final installation, paint surfaces behind permanently fixed items with prime coat only.

Paint [both sides] [exterior side] and edges of exterior doors and entire exposed surface of exterior door frames.

Retain first subparagraph below if required for steel windows.

Paint entire exposed surface of window frames and sashes.

Do not paint over labels of independent testing agencies or equipment name, identification, performance rating, or nomenclature plates.

Primers specified in applicable exterior painting schedule articles may be omitted on items that are factory primed or factory finished if compatible with intermediate and topcoat coatings and acceptable to intermediate and topcoat paint manufacturers.

If tinting is not required, delete first paragraph below. Different tints show through as topcoat erodes.

Tint each undercoat a lighter shade to facilitate identification of each coat if multiple coats of same material are to be applied. Tint undercoats to match color of topcoat but provide sufficient difference in shade of undercoats to distinguish each separate coat.

If undercoats or other conditions show through topcoat, apply additional coats until cured film has a uniform paint finish, color, and appearance.

Apply paints to produce surface films without cloudiness, spotting, holidays, laps, brush marks, roller tracking, runs, sags, ropiness, or other surface imperfections. Cut in sharp lines and color breaks.

Painting Fire-Suppression, Plumbing, HVAC, Electrical, Communication, and Electronic Safety and Security Work:

Subparagraph below is for use where items are to be painted to blend in with surroundings; revise if painting is required to protect items from corrosion. Consider indicating painted items on Drawings or delineating extent of "exposed to view" for complex situations.

Paint the following work where exposed to view:

Subparagraphs below contain items that are often field painted, plus others that are often not. Revise list to suit Project.

Equipment, including panelboards[ and switch gear].

Uninsulated metal piping.

Uninsulated plastic piping.

Pipe hangers and supports.

Metal conduit.

Plastic conduit.

Tanks that do not have factory-applied final finishes.

<Insert requirements>.

FIELD QUALITY CONTROL

Dry Film Thickness (DFT) Testing: Owner may engage the services of a qualified testing and inspecting agency to inspect and test paint for DFT.

Touch up and restore painted surfaces damaged by testing.

If test results show that DFT of applied paint does not comply with paint manufacturer's written instructions, apply additional coats as needed to provide DFT that complies with paint manufacturer's written instructions.

Cost of retesting is Contractor's responsibility.

CLEANING AND PROTECTION

At end of each workday, remove rubbish, empty cans, rags, and other discarded materials from Project site.

Do not clean equipment with free-draining water and prevent solvents, thinners, cleaners, and other contaminants from entering into waterways, sanitary and storm drain systems, and ground.

Dispose of contaminants in accordance with requirements of authorities having jurisdiction.

Allow empty paint cans to dry before disposal.

Retain subparagraph below if paint recycling or collection facilities are available in vicinity of Project.

Collect waste paint by type and deliver to recycling or collection facility.

After completing paint application, clean spattered surfaces. Remove spattered paints by washing, scraping, or other methods. Do not scratch or damage adjacent finished surfaces.

Protect work of other trades against damage from paint application. Correct damage to work of other trades by cleaning, repairing, replacing, and refinishing, as approved by Architect, and leave in an undamaged condition.

At completion of construction activities of other trades, touch up and restore damaged or defaced painted surfaces.

EXTERIOR PAINTING SCHEDULE, CONCRETE SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Retain "Intermediate Coat" subparagraphs for high-quality systems; delete if not required.

Vertical (Nontraffic) Surfaces:

Latex System: [MPI EXT 3.1A] [MPI EXT 3.1B] [MPI EXT 3.1K].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 3.1A; second corresponds to MPI EXT 3.1B; third corresponds to MPI EXT 3.1K.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

Prime Coat: Textured coating, latex, flat, MPI #42.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex Aggregate System: MPI EXT 3.1N.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, flat, MPI #42; [fine] [medium hard] [medium soft] [course] texture.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

High-Build Latex System: MPI EXT 3.1L, dry film thickness of not less than 10 mils.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex, exterior, high build, MPI #40.

Pittsburgh Paints; Perma-Crete 100% Acrylic High Build Interior/Exterior Flat, 4-22XI Series; applied at 3.2 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 3.1C.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 3.1P] [MPI EXT 3.1PP].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 3.1P; second corresponds to MPI EXT 3.1PP.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

Prime Coat: Latex, exterior, high performance architectural, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system. No budget grade system is available if using all matching coats.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

<Insert manufacturer's name; product name or designation>.

High-Performance Architectural Latex over Latex Aggregate System: MPI EXT 3.1Q.

Prime Coat: Textured latex coating, flat, MPI #42; [fine] [medium] [medium hard] [course soft] texture.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Horizontal (Traffic) Surfaces:

Latex Floor Enamel System: MPI EXT 3.2A.

Prime Coat: Latex floor paint, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex floor paint, matching topcoat.

Topcoat: Latex floor paint, low gloss, MPI #60.

Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510XI Series; applied at 1.0 mil minimum DFT.

Latex Deck Coating System: MPI EXT 3.2B.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex deck coating, MPI #127.

Pittsburgh Paints; Flood Pro Series Resurfacer 100% Acrylic Stain, FLD 922 Series; applied at 75 sq. ft./gal. (1.84 sq. m/L) minimum DFT.

Epoxy Deck Coating System (non-slip): MPI EXT 3.2C.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: Epoxy, gloss, matching topcoat.

Topcoat: Epoxy, gloss (MPI Gloss Level 6) + NSA.

Pittsburgh Paints; Amerlock 600 Series High Build Epoxy; applied at 5.0 to 10.0 mils DFT.

Alkyd Floor Enamel System: MPI EXT 3.2D.

Prime Coat: Alkyd floor enamel, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd floor enamel, matching topcoat.

Topcoat: Alkyd floor enamel, gloss, MPI #27.

Pittsburgh Paints; Floor & Porch Waterborne Alkyd Gloss, 3-610 Series; applied at 1.3 mils minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Solvent-Based Concrete Floor Sealer System: MPI EXT 3.2G.

Prime Coat: Sealer, solvent based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Sealer, solvent based, matching topcoat.

Topcoat: Sealer, solvent based, for concrete floors, MPI #104.

<Insert manufacturer's name; product name or designation>.

Water-Based Concrete Floor Sealer System: MPI EXT 3.2H.

Prime Coat: Sealer, water based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Sealer, water based, matching topcoat.

Topcoat: Sealer, water based, for concrete floors, MPI #99.

Pittsburgh Paints; Perma-Crete Plex-Seal WB Interior/Exterior 100% Acrylic Clear Sealer, 4-6200XI Series; applied at 0.8 mil minimum DFT.

Latex Zone/Traffic-Marking Paint System: MPI EXT 3.2E.

Traffic-marking paint, latex, MPI #97.

Alkyd Zone/Traffic-Marking Paint System: MPI EXT 3.2F.

Traffic-marking paint, solvent-based, MPI #32.

EXTERIOR PAINTING SCHEDULE, CEMENTITIOUS SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Cementitious Composition Board Substrates: [Siding] [Trim] [Panels] <Insert requirements>.

Latex System: [MPI EXT 3.3A] [MPI EXT 3.3J].

Retain one of two "Prime Coat" subparagraphs below. First subparagraph corresponds to MPI EXT 3.3A; second corresponds to MPI EXT 3.3J.

Prime Coat: Latex, exterior, matching topcoat.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

Retain subparagraph below only if retaining second option above.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

              - Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

              - Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

              - Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex Aggregate System: MPI EXT 3.3G.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, flat, MPI #42; [fine] [medium hard] [medium soft] [course] texture.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

High-Build Latex System: MPI EXT 3.3H, dry film thickness of not less than 10 mils.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex, exterior, high build, MPI #40.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, High Build Interior/Exterior Flat, 4-22XI Series; applied at 3.2 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 3.3C.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 3.3B.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Alkyd Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 3.3K] [MPI EXT 3.3KK].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 3.3K; second corresponds to MPI EXT 3.3KK.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

Prime Coat: Latex, exterior, high performance architectural, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Portland Cement Plaster (Stucco) Substrates:

Latex System: [MPI EXT 9.1A] [MPI EXT 9.1J].

Retain one of two "Prime Coat" subparagraphs below. First to MPI EXT 9.1A; second corresponds to MPI EXT 9.1J.

Prime Coat: Latex, exterior, matching topcoat.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

High-Build Latex System: MPI EXT 9.1H, dry film thickness of not less than 10 mils.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex, exterior, high build, MPI #40.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, High Build Interior/Exterior Flat, 4-22XI Series; applied at 3.2 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 9.1B.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level 5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level 6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 9.1K] [MPI EXT 9.1KK].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 9.1K; second corresponds to MPI EXT 9.1KK.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

Prime Coat: Latex, exterior, high performance architectural, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

EXTERIOR PAINTING SCHEDULE, MASONRY SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Clay Masonry Substrates:

Latex System: MPI EXT 4.1A.

Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex Aggregate System: MPI EXT 4.1B.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, flat, MPI #42; [fine] [medium hard] [medium soft] [course] texture.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

High-Build Latex System: MPI EXT 4.1H, dry film thickness of not less than 10 mils.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex, exterior, high build, MPI #40.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, High Build Interior/Exterior Flat, 4-22XI Series; applied at 3.2 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 4.1C.

Prime Coat: Light industrial coating, exterior, water based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: MPI EXT 4.1K.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

CMU Substrates:

Latex System: MPI EXT 4.2A.

Prime Coat, Block Filler: Latex, interior/exterior, MPI #4.

Pittsburgh Paints; Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex over Alkali-Resistant Primer System: MPI EXT 4.2L.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex Aggregate System: MPI EXT 4.2B.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, flat, MPI #42; [manufacturer's standard] [fine] [medium] [course] texture.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

High-Build Latex System: MPI EXT 4.2K, dry film thickness of not less than 10 mils.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions recommendations for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex, exterior, high build, MPI #40.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, High Build Interior/Exterior Flat, 4-22XI Series; applied at 3.2 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 4.2C.

Prime Coat, Block Filler: Latex, interior/exterior, MPI #4.

Pittsburgh Paints; Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5)[, MPI #163].

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6)[, MPI #164].

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 4.2M] [MPI EXT 4.2MM].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 4.2M; second corresponds to MPI EXT 4.2MM.

Prime Coat: Primer, alkali resistant, water based, MPI #3.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI; applied at 1.4 mils minimum DFT.

Prime Coat: Block filler, latex, interior/exterior, MPI #4.

Pittsburgh Paints; Speedhide Interior/Exterior Masonry Hi Fill Latex Block Filler, 6-15XI; applied at 8.0 mils minimum DFT.

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI; applied at 8.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

EXTERIOR PAINTING SCHEDULE, METAL SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Steel and Iron Substrates:

Water-Based Light Industrial Coating System: [MPI EXT 5.1B] [MPI EXT 5.1C] [MPI EXT 5.1M] [MPI EXT 5.1N].

Retain one of four "Prime Coat" subparagraphs below for field-applied primers. First corresponds to MPI EXT 5.1B; second corresponds to MPI EXT 5.1C; third corresponds to MPI EXT 5.1M; and fourth corresponds to MPI EXT 5.1N.

Prime Coat: Primer, zinc rich, inorganic, MPI #19.

PPG Protective and Marine Coatings; Dimetcote 9 H Inorganic Zinc Silicate Primer; applied at 2.0 mils minimum DFT.

PPG Protective and Marine Coatings; Dimetcote 9 two-component, moisture-curing zinc (ethyl) silicate, applied at 2.0 mils minimum DFT.

PPG Protective and Marine Coatings; Metalhide One Pac one-component, inorganic zinc silicate primer, 97-676, applied at 3.0 mils minimum DFT.

Prime Coat: Primer, alkyd, anti-corrosive for metal, MPI #79.

Pittsburgh Paints; Speedhide Rust Inhibitive Steel Primer, 6-208 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, epoxy, water based, anti-corrosive, for metal MPI #301.

Pittsburgh Paints; Aquapon WB EP, 98E-46/98E-99 Series, Two-Component Waterborne Epoxy Primer; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, epoxy, anti-corrosive, MPI #101.

PPG Protective and Marine Coatings; Amerlock 2 AL Aluminum Epoxy Mastic; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amercoat 235 Multi-Purpose Phenalkamine Epoxy; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amercoat 600 High-Build Epoxy; applied at 5.0 to 10.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph below only if applicable for MPI EXT 5.1C. If retaining, specify primer complying with MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three in "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Water-Based Light Industrial Coating over Epoxy System: MPI EXT 5.1R.

Prime Coat: Primer, epoxy, anticorrosive, MPI #101.

PPG Protective and Marine Coatings; Amerlock 2 AL Aluminum Epoxy Mastic; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amercoat 235 Multi-Purpose Phenalkamine Epoxy; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amercoat 600 PA High-Build, Multi-Purpose Polyamide Cured Epoxy; applied at 5.0 to 10.0 mils minimum DFT.

Intermediate Coat: Epoxy, high build, low gloss, MPI #108.

PPG Protective and Marine Coatings; Amerlock 600 Series High Build Epoxy; applied at 5.0 to 10.0 mils DFT.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: [MPI EXT 5.1D] [MPI EXT 5.1Q].

Retain one of three "Prime Coat" subparagraphs below. First corresponds to MPI EXT 5.1D; third corresponds to MPI EXT 5.1Q.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Speedhide Rust Inhibitive Steel Primer, 6-208 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Shop primer specified in Section where substrate is specified.

Prime Coat: Primer, metal, surface tolerant, MPI #23.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

Retain "Shop-Applied Prime Coat" Subparagraph below only if applicable for MPI EXT 5.1D. If retaining, specify primer complying with MPI #79 in Section where substrate is specified.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

Quick-Dry Enamel System: MPI EXT 5.1A.

Prime Coat: Primer, alkyd, quick dry, for metal, MPI #76.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd, quick dry, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, quick dry, semigloss (MPI Gloss Level G5), MPI #81.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Pittsburgh Paints; HPC Rust Inhibitive Interior/Exterior Alkyd Enamel Semi-Gloss, 4306 Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, quick dry, gloss (MPI Gloss Level 7), MPI #96.

Pittsburgh Paints; Fast Dry 35 Interior/Exterior Alkyd Gloss, 95-912 Series; applied at 1.0 mil minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI EXT 5.1K.

Retain "Prime Coat" or "Shop-Applied Prime Coat" Subparagraph below. If retaining second, specify primer complying with MPI #79 in Section where substrate is specified.

Prime Coat: Primer, alkyd, anticorrosive, for metal, MPI #79.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT.

Shop-Applied Prime Coat: Shop primer specified in Section where substrate is specified.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Galvanized-metal substrates should not be chromate passivated if primers are field applied. If galvanized metal is chromate passivated, consult manufacturers for appropriate surface preparation and primers.

Galvanized-Metal Substrates:

Latex System: MPI EXT 5.3H.

Water-Based Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10] [(MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 499-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: [MPI EXT 5.3J] [MPI EXT 5.3K].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 5.3J; second corresponds to MPI EXT 5.3K.

Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT.

Prime Coat: Primer, epoxy, anti-corrosive, MPI #101.

PPG Protective and Marine Coatings; Amerlock 2 AL Aluminum Epoxy Mastic; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amercoat 235 Multi-Purpose Phenalkamine Epoxy; applied at 4.0 mils minimum DFT.

PPG Protective and Marine Coatings; Amerlock 600 Series High Build Epoxy; applied at 5.0 to 10.0 mils DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 5.3N.

Water-Based Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT.

Retain "Intermediate Coat" Subparagraph below if required.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000N Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI EXT 5.3P.

Water-Based Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

High-Performance Architectural Latex System: MPI EXT 5.3M.

Water-Based Prime Coat: Primer, galvanized, water based, MPI #134.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer/Finish, 90-1912 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Bituminous Coating System: MPI EXT 5.3E.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Bituminous coating, matching topcoat.

Topcoat: Bituminous coating, MPI #35.

<Insert manufacturer's name; product name or designation>.

Aluminum (Not Anodized or Otherwise Coated) Substrates:

Latex System: MPI EXT 5.4H.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 499-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 5.4G.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 5.4F.

Note that vinyl wash primer has a high VOC content and may be unavailable in some localities.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: MPI EXT 5.4J.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level 5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Aluminum Paint System: MPI EXT 5.4C.

Retain one of two options in "Prime Coat" Subparagraph below for MPI EXT 5.4C. Note that vinyl wash primer has a high VOC content and may be unavailable in some localities.

Prime Coat: [Vinyl wash primer, MPI #80] [Primer, quick dry, for aluminum, MPI #95].

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Bituminous Coating System: MPI EXT 5.4D.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Bituminous coating, matching topcoat.

Topcoat: Bituminous coating, MPI #35.

<Insert manufacturer's name; product name or designation>.

Copper Substrates:

Latex System: MPI EXT 5.5H.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 5.5G.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 5.5F.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: MPI EXT 5.5J.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multiprime Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Aluminum Paint System: MPI EXT 5.5C.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

Bituminous Coating System: MPI EXT 5.5D.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Bituminous coating, MPI #35.

<Insert manufacturer's name; product name or designation>.

Stainless Steel Substrates:

Latex System: MPI EXT 5.6F.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level g2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 5.6G.

Prime Coat: Primer, quick dry, for aluminum, MPI #95.

Pittsburgh Paints; Multi-Purpose Primer 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 5.6A.

Note that vinyl wash primer has a high VOC content and may be unavailable in some localities.

Prime Coat: Primer, alkyd, anti-corrosive for metal, MPI #79.

Pittsburgh Paints; Speedhide Rust Inhibitive Steel Primer, 6-208 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Multiprime Multi-Purpose Primer, 4160 Series; applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: MPI EXT 5.6H.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Aluminum Paint System: MPI EXT 5.6C.

Note that vinyl wash primer has a high VOC content and may not be available in some localities.

Prime Coat: Primer, vinyl wash, MPI #80.

<Insert manufacturer's name; product name or designation>.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

EXTERIOR PAINTING SCHEDULE, WOOD SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Glue-Laminated Wood Substrates:

Latex over Latex Primer System: MPI EXT 6.1L.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex over Alkyd Primer System: MPI EXT 6.1A.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Alkyd System: MPI EXT 6.1B.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, flat (MPI Gloss Level G1), MPI #8.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 6.1N] [MPI EXT 6.1NN].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.1N; second corresponds to MPI EXT 6.1NN.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, alkyd for exterior wood[, MPI #5].

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315[.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Exposed Wood-Framed Substrates:

Latex over Latex Primer System: MPI EXT 6.2M.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex over Alkyd Primer System: MPI EXT 6.2A.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Alkyd System: MPI EXT 6.2C.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 6.2Q] [MPI EXT 6.2QQ].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.2Q; second corresponds to MPI EXT 6.2QQ.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Dressed-Wood Substrates: [Wood trim] [Architectural woodwork] [Doors] [Windows] [Wood board siding] [Railings] [and] [Fences] <Insert requirements>.

Latex over Latex Primer System: MPI EXT 6.3L.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex System: MPI EXT 6.3A.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 6.3J.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 6.3B.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, flat (MPI Gloss Level G1), MPI #8.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 6.3P] [MPI EXT 6.3PP].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.3P; second corresponds to MPI EXT 6.3PP.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Wood-Based Panel Substrates:

Latex over Latex Primer System: MPI EXT 6.4K.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex over Alkyd Primer System: MPI EXT 6.4G.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Alkyd System: MPI EXT 6.4B.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 6.4M] [MPI EXT 6.4MM].

Retain one of two "Prime Coat" subparagraph below. First corresponds to MPI EXT 6.4M; second corresponds to MPI EXT 6.4MM.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Wood-Board, Traffic-Surface Substrates: [Lumber decking] [and] [stairs].

Latex Porch and Floor Enamel over Latex Primer System: MPI EXT 6.5E.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex floor paint, matching topcoat.

Topcoat: Latex floor paint, low gloss, MPI #60.

Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510 Series; applied at 1.0 mil minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Latex Porch and Floor Enamel over Alkyd Primer System: MPI EXT 6.5A.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex floor paint, matching topcoat.

Topcoat: Latex floor paint, low gloss, MPI #60.

Pittsburgh Paints; Floor & Porch 100% Acrylic Latex Satin, 3-510 Series; applied at 1.0 mil minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Latex Deck Coating System (for Plywood Decks): MPI EXT 6.5G.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Latex deck coating, MPI #127.

Pittsburgh Paints; Flood Pro Series Resurfacer 100% Acrylic Stain, FLD 922 Series; applied at 75 sq. ft./gal. (1.84 sq. m/L) minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Alkyd Floor Enamel System: MPI EXT 6.5B.

Prime Coat: Alkyd floor enamel, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Alkyd floor enamel, matching topcoat.

Topcoat: Alkyd floor enamel, gloss, MPI #27.

Pittsburgh Paints; Floor & Porch Waterborne Alkyd Gloss, 3-610 Series; applied at 1.3 mils minimum DFT.

Additive: Manufacturer's standard additive to increase skid resistance of painted surface.

Wood Shingle and Shake Siding Substrates:

Latex over Latex Primer System: MPI EXT 6.6E.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Latex over Alkyd Primer System: MPI EXT 6.6A.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Alkyd System: MPI EXT 6.6B.

Prime Coat, Alkyd: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 6.6G] [MPI EXT 6.6GG].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.6G; second corresponds to MPI EXT 6.6GG.

Prime Coat: Primer, latex for exterior wood, MPI #6.

Pittsburgh Paints; Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, alkyd for exterior wood, MPI #5.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

EXTERIOR PAINTING SCHEDULE, MISCELLANEOUS SUBSTRATES

Paint systems in this article are based on "MPI Architectural Painting Specification Manual" for new construction. For renovation or maintenance projects where repainting is required, consult "MPI Maintenance Repainting Manual" and revise paint systems accordingly.

If necessary, insert drawing designations. Use these designations on Drawings to identify locations of each paint system.

Fiberglass Substrates:

Latex System: MPI EXT 6.7A.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 6.7C.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 6.7B.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: MPI EXT 6.7G.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Plastic Trim Fabrication Substrates:

Latex System: [MPI EXT 6.8A] [MPI EXT 6.8AA].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.8A; second corresponds to MPI EXT 6.8AA.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: [MPI EXT 6.8C] [MPI EXT 6.8CC].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.8C; second corresponds to MPI EXT 6.8CC.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 1610 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: [MPI EXT 6.8B] [MPI EXT 6.8BB].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.8B; second corresponds to MPI EXT 6.8BB.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

High-Performance Architectural Latex System: [MPI EXT 6.8D] [MPI EXT 6.8DD].

Retain one of two "Prime Coat" subparagraphs below. First corresponds to MPI EXT 6.8D; second corresponds to MPI EXT 6.8DD.

Prime Coat: Primer, bonding, water based, MPI #17.

Pittsburgh Paints; Seal Grip Interior/Exterior 100% Acrylic Universal Primer/Sealer, 17-921XI Series; applied at 1.6 mils minimum DFT.

Prime Coat: Primer, bonding, solvent based, MPI #69.

Pittsburgh Paints; Seal Grip Interior/Exterior Universal Alkyd Primer/Sealer, 17-941NF; applied at 2.2 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Exterior Canvas and Cotton Substrates:

Latex System: MPI EXT 10.1A.

Prime Coat: Latex, exterior, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of five "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Topcoat: Latex, exterior, gloss (MPI Gloss Level G6), MPI #119.

Pittsburgh Paints; Speedhide Interior/Exterior Latex Gloss, 6-8534 Series; applied at 1.2 mils minimum DFT.

Pittsburgh Paints; Advantage 900 Interior/Exterior Styrene Acrylic Gloss, 909-10 Series; applied at 1.5 mils minimum DFT.

Water-Based Light Industrial Coating System: MPI EXT 10.1B.

Prime Coat: Light industrial coating, exterior, water based, matching topcoat.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Light industrial coating, exterior, water based, matching topcoat.

Retain one of three "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Light industrial coating, exterior, water based, (MPI Gloss Level G3), MPI #161.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Satin DTM Industrial Enamel, 90-1710 Series; applied at 2.0 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, semi-gloss (MPI Gloss Level G5), MPI #163.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Semi-Gloss DTM Industrial Enamel, 90-1610 Series; applied at 1.5 mils minimum DFT.

Topcoat: Light industrial coating, exterior, water based, gloss (MPI Gloss Level G6), MPI #164.

Pittsburgh Paints; Pitt-Tech Plus EP, Interior/Exterior Gloss DTM Industrial Enamel, 90-1510 Series; applied at 2.0 mils minimum DFT.

Alkyd System: MPI EXT 10.1C.

Prime Coat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI EXT 10.1D.

Prime Coat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

High-Performance Architectural Latex System: MPI EXT 10.1E.

Prime Coat: As recommended in writing by topcoat manufacturer.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Exterior Bituminous-Coated Substrates:

Latex System: MPI EXT 10.2A.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Red Primer, 90-1908, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, matching topcoat.

Retain one of four "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, flat (MPI Gloss Level G1), MPI #10.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Flat, 6-610XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Flat, 72-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Flat, 519-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Flat, 759-10 Series; applied at 2.3 mils minimum DFT.

Topcoat: Latex, exterior, (MPI Gloss Level G2), MPI #214.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Eggshell, 589-10 Series; applied at 1.6 mils minimum DFT.

Topcoat: Latex, exterior, low sheen (MPI Gloss Levels G3 and G4), MPI #15.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Satin, 6-2045XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Satin, 76-110XI Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, semi-gloss (MPI Gloss Level G5), MPI #11.

Pittsburgh Paints; Speedhide Exterior 100% Acrylic Latex Semi-Gloss, 6-900XI Series; applied at 1.4 mils minimum DFT.

Pittsburgh Paints; Sun Proof Exterior 100% Acrylic Latex Semi-Gloss, 78-811XI Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

Latex Aggregate Coating System: MPI EXT 10.2B.

"MPI Manual" states that application procedures and products used in this system vary; therefore, it relies on manufacturer's written instructions for primers and number of coats for a Premium Grade system and does not include a Budget Grade system.

Prime Coat: As recommended in writing by topcoat manufacturer.

Intermediate Coat: As recommended in writing by topcoat manufacturer.

Topcoat: Textured latex coating, flat, MPI #42; [manufacturer's standard] [fine] [medium] [course] texture.

PPG's "Perma-Crete 100% Acrylic Texture Coatings" are specifically designed for interior and exterior, aboveground, masonry, concrete, wood, and metal surfaces requiring high-performance textured finishes. PPG's "Perma-Crete" textured coatings provide resistance against water, UV light, and staining; and are breathable. Its "Perma-Crete" textured coatings provide a stain-resistant texture finish that is excellent for high-traffic large wall areas. These finishes are a decorative textured coating ideal for high-rise apartments and condominiums, hospitals, schools, hotels, resorts, and residential homes. PPG's "Perma-Crete" is available in "4-50 - Fine Texture," "4-60 - Medium Hard Texture," "4-65 - Medium Soft Texture," and "4-70 - Coarse Texture." VOC content is 60 g/L.

Pittsburgh Paints; Perma-Crete 100% Acrylic Texture Coatings, 4-50 Series; applied at 6.8 mils minimum DFT.

Alkyd System: MPI EXT 10.2C.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Exterior, alkyd paint, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Alkyd, exterior, semigloss (MPI Gloss Level G5), MPI #94.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Semi-Gloss, 4336H Series; applied at 2.0 mils minimum DFT.

Topcoat: Alkyd, exterior, gloss (MPI Gloss Level G6), MPI #9.

Pittsburgh Paints; Sil-Shield High Gloss Silicone Alkyd Enamel 95-5000 Series; applied at 1.5 mils minimum DFT.

Pittsburgh Paints; HPC Interior/Exterior Alkyd Gloss, 4308H Series; applied at 2.0 mils minimum DFT.

Aluminum Paint System: MPI EXT 10.2D.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Interior/Exterior Industrial DTM Primer, 90-1908 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Aluminum paint, matching topcoat.

Topcoat: Aluminum paint, MPI #1.

<Insert manufacturer's name; product name or designation>.

High-Performance Architectural Latex System: MPI EXT 10.2E.

Prime Coat: Primer, rust inhibitive, water based, MPI #107.

Pittsburgh Paints; Pitt-Tech Plus EP Interior/Exterior Industrial DTM Primer, 90-1908 Series, applied at 2.0 mils minimum DFT.

For a Premium Grade system, "MPI Manual" requires intermediate coat; delete "Intermediate Coat" Subparagraph below for a Budget Grade system.

Intermediate Coat: Latex, exterior, high-performance architectural, matching topcoat.

Retain one of two "Topcoat" subparagraphs below for desired gloss level.

Topcoat: Latex, exterior, high-performance architectural, low sheen (MPI Gloss Levels G3 and G4), MPI #315.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Satin, 739-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Satin, 769-10 Series; applied at 2.2 mils minimum DFT.

Topcoat: Latex, exterior, high performance architectural, semi-gloss (MPI Gloss Level G5), MPI #311.

Pittsburgh Paints; Acri-Shield Max Exterior 100% Acrylic Latex Semi-Gloss, 649-10 Series; applied at 1.6 mils minimum DFT.

Pittsburgh Paints; Permanizer Exterior 100% Acrylic Latex Semi-Gloss, 749-10 Series; applied at 2.1 mils minimum DFT.

END OF SECTION 099114