- Section 099123 
Interior Painting

PART 1  GENERAL

SECTION INCLUDES

Surface preparation.

Field application of paints.

Materials for back priming woodwork.

Scope:  Finish interior surfaces exposed to view, unless fully factory-finished and unless otherwise indicated.

Both sides and edges of plywood backboards for electrical and telecom equipment before installing equipment.

Elevator pit ladders.

Surfaces inside cabinets.

Prime surfaces to receive wall coverings.

Exposed walls and bottom of swimming pools and fountains.

Mechanical and Electrical:

In finished areas, paint insulated and exposed pipes, conduit, boxes, insulated and exposed ducts, hangers, brackets, collars and supports, mechanical equipment, and electrical equipment, unless otherwise indicated.

In finished areas, paint shop-primed items.

Paint interior surfaces of air ducts and convector and baseboard heating cabinets that are visible through grilles and louvers with one coat of flat black paint to visible surfaces.

Paint dampers exposed behind louvers, grilles, and convector and baseboard cabinets to match face panels.

Do Not Paint or Finish the Following Items:

Items factory-finished unless otherwise indicated; materials and products having factory-applied primers are not considered factory finished.

Items indicated to receive other finishes.

Items indicated to remain unfinished.

Fire rating labels, equipment serial number and capacity labels, bar code labels, and operating parts of equipment.

Stainless steel, anodized aluminum, bronze, terne-coated stainless steel, and lead items.

Marble, granite, slate, and other natural stones.

Floors, unless specifically indicated.

Ceramic and other tiles.

Brick, architectural concrete, cast stone, integrally colored plaster, and stucco.

Glass.

Concrete masonry units in utility, mechanical, and electrical spaces.

Acoustical materials, unless specifically indicated.

Concealed pipes, ducts, and conduits.

RELATED REQUIREMENTS

Section 016116 - Volatile Organic Compound (VOC) Content Restrictions.

Section 055000 - Metal Fabrications:  Shop-primed items.

Section 055100 - Metal Stairs:  Shop-primed items.

Section 099113 - Exterior Painting.

Section 099600 - High-Performance Coatings.

Section 099725 - Mineral-Based Coatings.

Section 210553 - Identification for Fire Suppression Piping and Equipment:  Painted identification.

Section 210553 - Identification for Fire Suppression Piping and Equipment:  Color coding scheme for items to be painted under this section.

Section 220553 - Identification for Plumbing Piping and Equipment:  Painted identification.

Section 220553 - Identification for Plumbing Piping and Equipment:  Color coding scheme for items to be painted under this section.

Section 230553 - Identification for HVAC Piping and Equipment:  Painted identification.

Section 230553 - Identification for HVAC Piping and Equipment:  Color coding scheme for items to be painted under this section.

Section 260553 - Identification for Electrical Systems:  Painted identification.

Section 260553 - Identification for Electrical Systems:  Color coding scheme for items to be painted under this section.

Section 321723 - Pavement Markings:  Painted pavement markings.

Section 331600 - Water Utility Storage Tanks:  Painting inside and outside of tanks.

DEFINITIONS

Comply with ASTM D16 for interpretation of terms used in this section.

REFERENCE STANDARDS

40 CFR 59, Subpart D - National Volatile Organic Compound Emission Standards for Architectural Coatings; U.S. Environmental Protection Agency; Current Edition.

ASTM D16 - Standard Terminology for Paint, Related Coatings, Materials, and Applications; 2024.

ASTM D4258 - Standard Practice for Surface Cleaning Concrete for Coating; 2023.

ASTM D4259 - Standard Practice for Preparation of Concrete by Abrasion Prior to Coating Application; 2018.

ASTM D4260 - Standard Practice for Liquid and Gelled Acid Etching of Concrete; 2023.

ASTM D4442 - Standard Test Methods for Direct Moisture Content Measurement of Wood and Wood-Based Materials; 2020.

CARB (SCM) - Suggested Control Measure for Architectural Coatings; California Air Resources Board; 2020.

SCAQMD 1113 - Architectural Coatings; 1977, with Amendment (2016).

SSPC V1 (PM1) - Good Painting Practice:  Painting Manual Volume 1; 2016.

SSPC V2 (PM2) - Systems and Specifications:  Steel Structures Painting Manual Volume 2; 2021.

SSPC-SP 1 - Solvent Cleaning; 2015, with Editorial Revision (2016).

SSPC-SP 2 - Hand Tool Cleaning; 2018.

SSPC-SP 3 - Power Tool Cleaning; 2018.

SSPC-SP 6/NACE No.3 - Commercial Blast Cleaning; 2006.

SSPC-SP 13/NACE No.6 - Surface Preparation of Concrete; 2018.

SUBMITTALS

See Section 013000 - Administrative Requirements, for submittal procedures.

Product Data:  Provide complete list of products to be used, with the following information for each:

Manufacturer's name, product name and/or catalog number, and general product category (e.g., "alkyd enamel").

Cross-reference to specified paint system products to be used in project; include description of each system.

Manufacturer's installation instructions.

If proposal of substitutions is allowed under submittal procedures, explanation of substitutions proposed.

Samples:  Submit three paper "draw down" samples, 8-1/2 by 11 inches (216 by 279 mm) in size, illustrating range of colors available for each finishing product specified.

Where sheen is specified, submit samples in only that sheen.

Where sheen is not specified, discuss sheen options with Architect before preparing samples, to eliminate sheens not required.

Allow 30 days for approval process, after receipt of complete samples by Architect.

Paint color submittals will not be considered until color submittals for major materials not to be painted, such as masonry, have been approved.

Samples:  Submit two paper chip samples, ____x____ inch (____x____ mm) in size illustrating range of colors and textures available for each surface finishing product scheduled.

Samples:  Submit two painted samples, illustrating selected colors and textures for each color and system selected with specified coats cascaded. Submit on aluminum sheet, ____x____ inch (____x____ mm) in size.

Certification:  By manufacturer that paints and finishes comply with VOC limits specified.

Manufacturer's Instructions:  Indicate special surface preparation procedures.

Maintenance Data:  Submit data including finish schedule showing where each product/color/finish was used, product technical data sheets, material safety data sheets (MSDS), care and cleaning instructions, touch-up procedures, repair of painted and finished surfaces, and color samples of each color and finish used.

Maintenance Materials:  Furnish the following for Owner's use in maintenance of project.

See Section 016000 - Product Requirements, for additional provisions.

Extra Paint and Finish Materials:  1 gal (4 L) of each color; from the same product run, store where directed.

Label each container with color in addition to the manufacturer's label.

QUALITY ASSURANCE

Manufacturer Qualifications:  Company specializing in manufacturing the products specified, with minimum three years documented experience.

Applicator Qualifications:  Company specializing in performing the type of work specified with minimum __________ years’ experience and approved by manufacturer.

MOCK-UP

See Section 014000 - Quality Requirements, for general requirements for mock-up.

Provide panel, ____ feet (____ m) long by ____ feet (____ m) wide, illustrating paint color, texture, and finish.

Provide door and frame assembly illustrating paint color, texture, and finish.

Locate where directed by Architect.

Mock-up may remain as part of the work.

DELIVERY, STORAGE, AND HANDLING

Deliver products to site in sealed and labeled containers; inspect to verify acceptability.

Container Label:  Include manufacturer's name, type of paint, brand name, lot number, brand code, coverage, surface preparation, drying time, cleanup requirements, color designation, and instructions for mixing and reducing.

Paint Materials:  Store at minimum ambient temperature of 45 degrees F (7 degrees C) and a maximum of 90 degrees F (32 degrees C), in ventilated area, and as required by manufacturer's instructions.

FIELD CONDITIONS

Do not apply materials when surface and ambient temperatures are outside the temperature ranges required by the paint product manufacturer.

Follow manufacturer's recommended procedures for producing best results, including testing of substrates, moisture in substrates, and humidity and temperature limitations.

Do not apply materials when relative humidity exceeds 85 percent, at temperatures less than 5 degrees F (3 degrees C) above the dew point, or to damp or wet surfaces.

Minimum Application Temperatures for Paints:  50 degrees F (10 degrees C) for interiors unless required otherwise by manufacturer's instructions.

Provide lighting level of 80 fc (860 lux) measured mid-height at substrate surface.

PART 2  PRODUCTS

MANUFACTURERS

Provide paints and finishes from the same manufacturer to the greatest extent possible.

If a single manufacturer cannot provide specified products; minor exceptions will be permitted provided approval by Architect is obtained using the specified procedures for substitutions.

Substitution of other products by the same manufacturer is preferred over substitution of products by a different manufacturer.

Substitution of a different paint system by the same manufacturer will be considered.

Paints:

Pittsburgh Paints:  www.pittsburghpaintsco.com/#sle.

PAINTS AND FINISHES - GENERAL

Paints and Finishes:  Ready-mixed, unless intended to be a field-catalyzed paint.

Provide paints and finishes of a soft paste consistency, capable of being readily and uniformly dispersed to a homogeneous coating, with good flow and brushing properties, and capable of drying or curing free of streaks or sags.

Provide materials that are compatible with one another and the substrates indicated under conditions of service and application, as demonstrated by manufacturer based on testing and field experience.

For opaque finishes, tint each coat including primer coat and intermediate coats, one-half shade lighter than succeeding coat, with final finish coat as base color.

Supply each paint material in quantity required to complete entire project's work from a single production run.

Do not reduce, thin, or dilute paint or finishes or add materials unless such procedure is specifically described in manufacturer's product instructions.

Volatile Organic Compound (VOC) Content:

Provide paints and finishes that comply with the most stringent requirements specified in the following:

40 CFR 59, Subpart D--National Volatile Organic Compound Emission Standards for Architectural Coatings.

SCAQMD 1113 Rule.

CARB (SCM).

Ozone Transport Commission (OTC) Model Rule, Architectural, Industrial, and Maintenance Coatings; www.otcair.org; specifically:

Opaque, Flat:  50 g/L, maximum.

Opaque, Non-flat:  150 g/L, maximum.

Opaque, High Gloss:  250 g/L, maximum.

Architectural coatings VOC limits of the State in which the Project is located.

USGBC LEED Rating System for interior wall and ceiling finishes (all coats), anti-corrosive paints on interior ferrous metal, sanding sealers, other sealers, and floor coatings.

Determination of VOC Content:  Testing and calculation in accordance with 40 CFR 59, Subpart D (EPA Method 24), exclusive of colorants added to a tint base and water added at project site; or other method acceptable to authorities having jurisdiction.

Flammability:  Comply with applicable code for surface burning characteristics.

Sheens:  Provide the sheens specified; where sheen is not specified, sheen will be selected later by Architect from the manufacturer's full line.

Colors:  To be selected from manufacturer's full range of available colors.

Selection to be made by Architect after award of contract.

Allow for minimum of three colors for each system, unless otherwise indicated, without additional cost to Owner.

Extend colors to surface edges; colors may change at any edge as directed by Architect.

In finished areas, finish pipes, ducts, conduit, and equipment the same color as the wall/ceiling under which they are mounted.

In utility areas, finish equipment, piping, conduit, and exposed duct work in colors according to the color-coding scheme indicated.

PAINT SYSTEMS - INTERIOR

Paint I-OP - Interior Surfaces to be Painted, Unless Otherwise Indicated:  Including gypsum board, concrete, concrete masonry units, brick, wood, plaster, uncoated steel, shop primed steel, galvanized steel, aluminum, and acoustical ceilings.

Two topcoats and one coat primer.

Topcoat(s):  High Performance Architectural Interior Latex.

Products:

Pittsburgh Paints Pure Performance Interior Latex, 9-110XI Series, Flat.

Pittsburgh Paints Pure Performance Interior Latex, 9-310XI Series, Eggshell.

Pittsburgh Paints Pure Performance Interior Latex, 9-510XI Series, Semi-Gloss.

Pittsburgh Paints Prominence Interior Latex, 84-3110 Series, Flat.

Pittsburgh Paints Prominence Interior Latex, 84-3310 Series, Eggshell.

Pittsburgh Paints Prominence Interior Latex, 84-3410 Series, Satin.

Pittsburgh Paints Prominence Interior Latex, 84-3510 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1310 Series, Eggshell.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1510 Series, Semi-Gloss.

Pittsburgh Paints Advantage 900 Styrene Acrylic, 919-10 Series, Semi-Gloss.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9310 Series, Eggshell.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9410 Series, Satin.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9610 Series, Lo-Lustre.

Topcoat(s):  Institutional Low Odor/VOC Interior Latex.

Products:

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-70ZV Series, Flat.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9310 Series, Eggshell.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9410 Series, Satin.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9610 Series, Lo Lustre.

Pittsburgh Paints Speedhide zero Interior Latex, 6-500ZV Series, Semi-Gloss.

Pittsburgh Paints Pure Performance Interior Latex, 9-110XI Series, Flat.

Pittsburgh Paints Pure Performance Interior Latex, 9-310XI Series, Eggshell.

Pittsburgh Paints Pure Performance Interior Latex, 9-510XI Series, Semi-Gloss.

Pittsburgh Paints Prominence Interior Latex, 84-3110 Series, Flat.

Pittsburgh Paints Prominence Interior Latex, 84-3310 Series, Eggshell.

Pittsburgh Paints Prominence Interior Latex, 84-3410 Series, Satin.

Pittsburgh Paints Prominence Interior Latex, 84-3510 Series, Semi-Gloss.

Topcoat(s):  Interior Latex.

Products:

Pittsburgh Paints Speedhide Pro-EV Zero Interior Wall and Ceiling Latex, 12-110XI Series, Flat.

Pittsburgh Paints Speedhide Pro-EV Zero Interior Latex Enamel, 12-310XI Series, Eggshell.

Pittsburgh Paints Speedhide Pro-EV Zero Interior Latex Enamel, 12-510XI Series, Semi-Gloss.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-0011ZV Series, Ultra-Flat.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-70ZV Series, Flat.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-4101 Series, Low Sheen Eggshell.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-411ZV Series, Eggshell.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-3511ZV Series, Satin.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-3011ZV Series, Lo Lustre.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-500ZV Series, Semi-Gloss.

Pittsburgh Paints Speedhide Interior Latex, 6-0011 Series, Ultra-Flat.

Pittsburgh Paints Speedhide Interior Latex, 6-70 Series, Flat.

Pittsburgh Paints Speedhide Interior Latex, 6-4101 Series, Low-Sheen Eggshell.

Pittsburgh Paints Speedhide Interior Latex, 6-411 Series, Eggshell.

Pittsburgh Paints Speedhide Interior Latex, 6-3511 Series, Satin.

Pittsburgh Paints Speedhide Interior Latex, 6-3011 Series, Low-Lustre.

Pittsburgh Paints Speedhide Interior Latex, 6-500 Series, Semi-Gloss.

Pittsburgh Paints Speedhide Interior/Exterior Latex, 6-8534 Series, Gloss.

Pittsburgh Paints Advantage 900 Interior/Exterior Styrene Acrylic, 919-10 Series, Semi-Gloss.

Pittsburgh Paints Advantage 900 Interior/Exterior Styrene Acrylic, 909-10 Series, Gloss.

Paint I-OP-MD-DT - Medium Duty Door/Trim:  For surfaces subject to frequent contact by occupants, including metals and wood:

Medium duty applications include doors, door frames, railings, handrails, guardrails, and balustrades.

Two topcoats and one coat primer.

Topcoat(s):  Interior Epoxy-Modified Latex.

Products:

Pittsburgh Paints Aquapon WB EP Two-Component Waterborne Epoxy Coating, 98E-1/98E-100 Series, Semi-Gloss.

Pittsburgh Paints Aquapon WB EP Two-Component Waterborne Epoxy Coating, 98E-1/98E-98 Series, Gloss.

Topcoat(s):  High Performance Architectural Interior Latex.

Products:

Pittsburgh Paints Pure Performance Interior Latex, 9-110XI Series, Flat.

Pittsburgh Paints Pure Performance Interior Latex, 9-310XI Series, Eggshell.

Pittsburgh Paints Pure Performance Interior Latex, 9-510XI Series, Semi-Gloss.

Pittsburgh Paints Prominence Interior Latex, 84-3110 Series, Eggshell.

Pittsburgh Paints Prominence Interior Latex, 84-3310 Series, Eggshell.

Pittsburgh Paints Prominence Interior Latex, 84-3410 Series, Satin.

Pittsburgh Paints Prominence Interior Latex, 84-3510 Series, Semi-Gloss.

Pittsburgh Paints Advantage 900 Styrene Acrylic, 919-10 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1310 Series, Eggshell.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1510 Series, Semi-Gloss.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9310 Series, Eggshell.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9410 Series, Satin.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9610 Series, Lo Lustre.

Topcoat(s):  Interior Light Industrial Coating, Water Based.

Products:

Pittsburgh Paints Advantage 900 Interior/Exterior Styrene Acrylic, 919-10 Series, Semi-Gloss.

Pittsburgh Paints Advantage 900 Interior/Exterior Styrene Acrylic, 909-10 Series, Gloss.

Pittsburgh Paints Pitt-Glaze WB1 Pre-Catalyzed Water-Borne Acrylic Epoxy, 16-1310 Series, Eggshell.

Pittsburgh Paints Pitt-Glaze WB1 Pre-Catalyzed Water-Borne Acrylic Epoxy, 16-1510 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Tech Plus EP WB DTM Industrial Enamel, 90-1710 Series, Satin.

Pittsburgh Paints Pitt-Tech Plus EP WB DTM Industrial Enamel. 90-1610 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Tech Plus EP WB DTM Industrial Enamel, 90-1510 Series, Gloss.

Topcoat(s):  Interior Alkyd.

Products:

Pittsburgh Paints Glyptex Interior Alkyd Enamel 39-10 Series, Satin.

Pittsburgh Paints Glyptex Interior Alkyd Enamel, 439-10 Series, Semi-Gloss.

Pittsburgh Paints Glyptex Interior/Exterior Alkyd Enamel, 4139-10 Series, Gloss.

Pittsburgh Paints Interior/Exterior Industrial Enamel, 7-282 Series, Gloss.

Pittsburgh Paints HPC Rust Preventative Alkyd, 4306, Semi-Gloss.

Pittsburgh Paints HPC Industrial Alkyd, 4308H Series, Gloss.

Pittsburgh Paints Fast Dry 35 Quick Drying Enamel, 95-912 Series, Gloss.

Topcoat(s):  Interior Alkyd, Water Based.

Products:

Pittsburgh Paints Speedhide Interior/Exterior WB Alkyd, 6-1410XI Series, Satin.

Pittsburgh Paints Speedhide Interior/Exterior WB Alkyd, 6-1510XI Series, Semi-Gloss.

Pittsburgh Paints Speedhide Interior/Exterior WB Alkyd, 6-1610XI Series, Gloss.

Paint I-OP-MD-WC - Medium Duty Vertical and Overhead:  Including gypsum board, plaster, concrete, concrete masonry units, uncoated steel, shop primed steel, galvanized steel, and aluminum.

Two topcoats and one coat primer.

Topcoat(s):  Interior Epoxy-Modified Latex.

Products:

Pittsburgh Paints Aquapon WB EP Two-Component Waterborne Epoxy Coating, 98E-1/98E-100 Series, Semi-Gloss.

Pittsburgh Paints Aquapon WB EP Two-Component Waterborne Epoxy Coating, 98E-1/98E-98 Series, Gloss.

Topcoat(s):  High Performance Architectural Interior Latex.

Products:

Pittsburgh Paints Pure Performance Interior Latex, 9-110XI Series, Flat.

Pittsburgh Paints Pure Performance Interior Latex, 9-310XI Series, Eggshell.

Pittsburgh Paints Pure Performance Interior Latex, 9-510XI Series, Semi-Gloss.

Pittsburgh Paints Prominence Interior Latex, 84-3110 Series, Flat.

Pittsburgh Paints Prominence Interior Latex, 84-3310 Series, Eggshell.

Pittsburgh Paints Prominence Interior Latex, 84-3410 Series, Satin.

Pittsburgh Paints Prominence Interior Latex, 84-3510 Series, Semi-Gloss.

Pittsburgh Paints Advantage 900 Styrene Acrylic, 919-10 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1310 Series, Eggshell.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1510 Series, Semi-Gloss.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9310 Series, Eggshell.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9410 Series, Satin.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9610 Series, Lo Lustre.

Topcoat(s):  Institutional Low Odor/VOC Interior Latex.

Products:

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-70ZV Series, Flat.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9310 Series, Eggshell.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9410 Series, Satin.

Pittsburgh Paints Speedhide Max Interior Latex, 6-9610 Series, Lo Lustre.

Pittsburgh Paints Speedhide Interior Zero VOC Latex, 6-70ZV Series, Semi-Gloss.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1310 Series, Eggshell.

Pittsburgh Paints Pitt-Glaze WB1 Epoxy, 16-1510 Series, Semi-Gloss.

Pittsburgh Paints Prominence Interior Latex, 84-3110 Series, Flat.

Pittsburgh Paints Prominence Interior Latex, 84-3310 Series, Eggshell.

Pittsburgh Paints Prominence Interior Latex, 84-3410 Series, Satin.

Pittsburgh Paints Prominence Interior Latex, 84-3510 Series, Semi-Gloss.

Pittsburgh Paints Pure Performance Interior Latex, 9-110XI Series, Flat.

Pittsburgh Paints Pure Performance Interior Latex, 9-310XI Series, Eggshell.

Pittsburgh Paints Pure Performance Interior Latex, 9-510XI Series, Semi-Gloss.

Topcoat(s):  Interior Light Industrial Coating, Water Based.

Products:

Pittsburgh Paints Advantage 900 Interior/Exterior Styrene Acrylic, 919-10 Series, Semi-Gloss.

Pittsburgh Paints Advantage 900 Interior/Exterior Styrene Acrylic, 909-10 Series, Gloss.

Pittsburgh Paints Pitt-Glaze WB1 Pre-Catalyzed Water-Borne Acrylic Epoxy, 16-1310 Series, Eggshell.

Pittsburgh Paints Pitt-Glaze WB1 Water-Borne Acrylic Epoxy, 16-1510 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Tech Plus EP WB DTM Industrial Enamel, 90-1710 Series, Satin.

Pittsburgh Paints Pitt-Tech Plus EP WB DTM Industrial Enamel, 90-1610 Series, Semi-Gloss.

Pittsburgh Paints Pitt-Tech Plus EP WB DTM Industrial Enamel, 90-1510 Series, Gloss.

Topcoat(s):  Interior Alkyd.

Products:

Pittsburgh Paints Glyptex Interior Alkyd Enamel, 39-10 Series, Satin.

Pittsburgh Paints Glyptex Interior Alkyd Enamel, 439-10 Series, Semi-Gloss.

Pittsburgh Paints Glyptex Interior/Exterior Alkyd Enamel, 4139-10 Series, Gloss.

Pittsburgh Paints 7-Line LV Alkyd Interior/Exterior Industrial Enamel, 7-282N Series, Gloss.

Pittsburgh Paints HPC Rust Preventative Alkyd, 4306, Semi-Gloss.

Pittsburgh Paints Fast Dry 35 Quick Drying Enamel, 95-912 Series, Gloss.

Topcoat(s):  Interior Alkyd, Water Based.

Products:

Pittsburgh Paints Speedhide Interior/Exterior WB Alkyd, 6-1410XI Series, Satin.

Pittsburgh Paints Speedhide Interior/Exterior WB Alkyd, 6-1510XI Series, Semi-Gloss.

Pittsburgh Paints Speedhide Interior/Exterior WB Alkyd, 6-1610XI Series, Gloss.

Topcoat(s):  Topcoat for Multicolored Coating, Clear.

Products:

Pittsburgh Paints ProLuxe Interior/Exterior Polyurethane Water Based Acrylic, PLX257, Gloss.

Topcoat(s):  Vinyl Acrylic Ceiling Paint; _____.

Products:

Pittsburgh Paints Speedhide Pro-EV Zero Interior Wall and Ceiling Latex, 12-110XI Series, Flat.

Pittsburgh Paints Interior Ceiling Paint, 9585 Series, Flat.

Paint I-OP-DF - Dry Fall:  Metals; exposed structure and overhead-mounted services in utilitarian spaces, including shop primed steel deck, structural steel, metal fabrications, galvanized ducts, galvanized conduit, galvanized piping, and _______.

Shop primer by others.

One topcoat ______.

Topcoat:  Alkyd Dry Fall.

Products:

Pittsburgh Paints Speedhide Interior Alkyd Dry Fog, 6-160XI, Flat.

Pittsburgh Paints Speedhide Super Tech Interior Alkyd Dry Fog, 6-151XI, Eggshell.

Pittsburgh Paints Speedhide Interior Alkyd Dry Fog, 6-161XI, Lo Lustre Semi-Gloss.

Topcoat:  Latex Dry Fall.

Products:

Pittsburgh Paints Speedhide Super Tech Water Based Interior Dry-Fog Latex, 6-725XI Series, Flat.

Pittsburgh Paints Speedhide Super Tech Water Based Interior Dry-Fog Latex, 6-724XI, Eggshell.

Pittsburgh Paints Speedhide Super Tech Water Based Interior Dry-Fog Latex, 6-727XI, Semi-Gloss.

Topcoat:  Water Based Dry Fall for Galvanized Steel.

Products:

Pittsburgh Paints Speedhide Super Tech Water Based Interior Dry-Fog Latex, 6-725XI Series, Flat.

Pittsburgh Paints Speedhide Super Tech Water Based Interior Dry-Fog Latex, 6-724XI, Eggshell.

Pittsburgh Paints Speedhide Super Tech Water Based Interior Dry-Fog, 6-727XI, Semi-Gloss.

Paint I-OP-FL - Concrete and Wood Floors to be Painted.

​Two topcoats without primer​.

Topcoat(s):  Alkyd Floor Enamel, Gloss.

Products:

Pittsburgh Paints Floor and Porch Enamel WB Alkyd, 3-610 Series, Gloss.

Topcoat(s):  Latex Floor Paint, Low Gloss.

Products:

Pittsburgh Paints Floor and Porch Enamel 100% Acrylic Latex, 3-510XI Series, Satin.

Pittsburgh Paints Break-Through Interior/Exterior Water-Borne Acrylic, V52-410 Series, Satin.

Topcoat(s):  Latex Floor Paint, Semi-Gloss.

Products:

Pittsburgh Paints Break-Through Interior/Exterior Water-Borne Acrylic, V62-510 Series, Semi-Gloss.

Topcoat(s):  Latex Floor Paint, Gloss.

Products:

Pittsburgh Paints Break-Through Interior/Exterior Water-Borne Acrylic, V72-610 Series, Gloss.

Paint I-TR-C - Transparent Finish on Concrete Floors.

​_______​.

Stain:  Solid Color Stain for Concrete.

Products:

Pittsburgh Paints Perma-Crete Color Seal WB Interior/Exterior Acrylic Concrete Stain, 4-4210XI Series, Satin.

Sealer:  Water Based Sealer for Concrete Floors.

Products:

Pittsburgh Paints Perma-Crete Plex-Seal WB Interior/Exterior Clear Sealer, 4-6200XI, Satin.

PRIMERS

Primers:  Provide the following unless other primer is required or recommended by manufacturer of topcoats.

Alkali Resistant Water Based Primer.

Products:

Pittsburgh Paints Perma-Crete Interior/Exterior Alkali Resistant Primer, 4-603XI.

Pittsburgh Paints Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series.

Interior Institutional Low Odor/VOC Primer Sealer.

Products:

Pittsburgh Paints Speedhide Interior Zero VOC Latex Sealer, 6-4900XI.

Pittsburgh Paints Pure Performance Interior Latex Primer, 9-900.

Interior/Exterior Latex Block Filler.

Products:

Pittsburgh Paints; Perma-Crete Concrete Block & Masonry Surfacer/Filler, 4-100XI.

Pittsburgh Paints Speedhide Masonry Hi Fill Latex Block Filler, 6-15XI.

Interior Latex Primer Sealer.

Products:

Pittsburgh Paints Speedhide Interior Latex Sealer, 6-2.

Pittsburgh Paints Speedhide Interior Zero VOC Latex Sealer, 6-4900XI.

Pittsburgh Paints Pure Performance Interior Latex Sealer, 9-900.

Interior Drywall Primer Sealer.

Products:

Pittsburgh Paints Speedhide Pro-EV Zero Latex Sealer, 12-900XI.

Pittsburgh Paints Speedhide Interior Latex Sealer, 6-2.

Pittsburgh Paints Speedhide Zero Interior Latex Sealer, 6-4900XI.

Anti-Corrosive Alkyd Primer for Metal.

Products:

Pittsburgh Paints Speedhide LV Rust-Inhibitive Alkyd Metal Primer, 6-208N Series.

Pittsburgh Paints Multiprime Multi-Purpose Primer, 4160 Series.

Interior Rust-Inhibitive Water Based Primer.

Products:

Pittsburgh Paints Pitt-Tech Plus Interior/Exterior EP DTM Waterborne Acrylic Primer/Finish, 90-1908.

Interior/Exterior Quick Dry Alkyd Primer for Metal.

Products:

Pittsburgh Paints Multiprime Multi-Purpose Primer, 4160 Series.

Interior Water Based Primer for Galvanized Metal.

Products:

Pittsburgh Paints Pitt-Tech Plus EP DTM Industrial Primer, 90-1912 Series.

Interior/Exterior Quick Dry Primer for Aluminum.

Products:

Pittsburgh Paints Multiprime Multi-Purpose Primer, 4160 Series.

Interior Alkyd Enamel Undercoat.

Products:

Pittsburgh Paints Seal Grip Interior/Exterior Alkyd Universal Primer/Sealer, 17-941NF.

Stain Blocking Primer.

Products:

Pittsburgh Paints Seal Grip Interior/Exterior Alkyd Universal Primer/Sealer, 17-941NF.

Stain Blocking Primer, Water Based.

Products:

Pittsburgh Paints Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series.

Latex Primer for Interior Wood.

Products:

Pittsburgh Paints Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series.

Bonding Primer, Water Based.

Products:

Pittsburgh Paints Seal Grip Interior/Exterior Acrylic Universal Primer/Sealer, 17-921XI Series.

ACCESSORY MATERIALS

Accessory Materials:  Provide primers, sealers, cleaning agents, cleaning cloths, sanding materials, and clean-up materials as required for final completion of painted surfaces.

Patching Material:  Latex filler.

Fastener Head Cover Material:  Latex filler.

PART 3  EXECUTION

INSTALLERS

Acceptable Applicators:

____________________________________.

EXAMINATION

Do not begin application of paints and finishes until substrates have been adequately prepared.

Verify that surfaces are ready to receive work as instructed by the product manufacturer.

Examine surfaces scheduled to be finished prior to commencement of work.  Report any condition that may potentially affect proper application.

If substrate preparation is the responsibility of another installer, notify Architect of unsatisfactory preparation before proceeding.

Test shop-applied primer for compatibility with subsequent cover materials.

Measure moisture content of surfaces using an electronic moisture meter. Do not apply finishes unless moisture content of surfaces is below the following maximums:

Gypsum Wallboard:  12 percent.

Plaster and Stucco:  12 percent.

Masonry, Concrete, and Concrete Masonry Units:  12 percent.

Interior Wood:  15 percent, measured in accordance with ASTM D4442.

Concrete Floors and Traffic Surfaces:  8 percent.

PREPARATION

Clean surfaces thoroughly and correct defects prior to application.

Prepare surfaces using the methods recommended by the manufacturer for achieving the best result for the substrate under the project conditions.

Remove or repair existing paints or finishes that exhibit surface defects.

Remove or mask surface appurtenances, including electrical plates, hardware, light fixture trim, escutcheons, and fittings, prior to preparing surfaces or finishing.

Seal surfaces that might cause bleed through or staining of topcoat.

Remove mildew from impervious surfaces by scrubbing with solution of tetra-sodium phosphate and bleach. Rinse with clean water and allow surface to dry.

Acoustical Panel Ceilings:

Pretreat ceiling water stains according to manufacturer's written instructions.

Pretreat tiles saturated with grease or nicotine according to manufacturer's written instructions.

Concrete:

Remove release agents, curing compounds, efflorescence, and chalk.  Do not coat surfaces if moisture content or alkalinity of surfaces to be coated exceeds that permitted in manufacturer's written instructions.

Clean surfaces with pressurized water. Use pressure range of 1,500 to 4,000 psi (10,350 to 27,580 kPa) at 6 to 12 inches (150 to 300 mm). Allow to dry.

Clean concrete according to ASTM D4258. Allow to dry.

Prepare surface as recommended by topcoat manufacturer and in accordance with SSPC-SP 13/NACE No.6.

Masonry:

Remove efflorescence and chalk. Do not coat surfaces if moisture content, alkalinity of surfaces, or if alkalinity of mortar joints exceed that permitted in manufacturer's written instructions. Allow to dry.

Prepare surface as recommended by topcoat manufacturer.

Clean surfaces with pressurized water. Use pressure range of 600 to 1,500 psi (4,140 to 10,350 kPa) at 6 to 12 inches (150 to 300 mm). Allow to dry.

Concrete Floors and Traffic Surfaces:  Remove contamination, acid etch and rinse floors with clear water. Verify required acid-alkali balance is achieved. Allow to dry.

Gypsum Board:  Fill minor defects with filler compound. Spot prime defects after repair.

Plaster:  Fill hairline cracks, small holes, and imperfections with latex patching plaster. Make smooth and flush with adjacent surfaces. Wash and neutralize high-alkali surfaces.

Insulated Coverings:  Remove dirt, grease, and oil from canvas and cotton.

Aluminum:  Remove surface contamination and oils and wash with solvent according to SSPC-SP 1.

Copper:  Remove contamination by steam, high-pressure water, or solvent washing.

Galvanized Surfaces:

Remove surface contamination and oils and wash with solvent according to SSPC-SP 1.

Prepare surface according to SSPC-SP 2.

Ferrous Metal:

Solvent clean according to SSPC-SP 1.

Shop-Primed Surfaces:  Sand and scrape to remove loose primer and rust. Feather edges to make touch-up patches inconspicuous. Clean surfaces with solvent. Prime bare steel surfaces. Re-prime entire shop-primed item.

Remove rust, loose mill scale, and other foreign substances using methods recommended in writing by paint manufacturer and blast cleaning in accordance with SSPC-SP 6/NACE No.3. Protect from corrosion until coated.

Wood Surfaces to Receive Opaque Finish:  Wipe off dust and grit prior to priming. Seal knots, pitch streaks, and sappy sections with sealer. Fill nail holes and cracks after primer has dried; sand between coats. Back prime concealed surfaces before installation.

Glue-Laminated Beams:  Prior to finishing, wash surfaces with solvent, remove grease and dirt.

Wood Doors to be Field Finished:  Seal wood door top and bottom edge surfaces with clear sealer.

Metal Doors to be Painted:  Prime metal door top and bottom edge surfaces.

APPLICATION

Remove unfinished louvers, grilles, covers, and access panels on mechanical and electrical components and paint separately.

Apply products in accordance with manufacturer's written instructions.

Where adjacent sealant is to be painted, do not apply finish coats until sealant is applied.

Do not apply finishes to surfaces that are not dry. Allow applied coats to dry before next coat is applied.

Apply each coat to uniform appearance in thicknesses specified by manufacturer.

Dark Colors and Deep Clear Colors:  Regardless of number of coats specified, apply as many coats as necessary for complete hide.

Sand wood and metal surfaces lightly between coats to achieve required finish.

Vacuum clean surfaces of loose particles. Use tack cloth to remove dust and particles just prior to applying next coat.

Wood to Receive Transparent Finishes:  See Section 099300.

Reinstall electrical cover plates, hardware, light fixture trim, escutcheons, and fittings removed prior to finishing.

FIELD QUALITY CONTROL

See Section 014000 - Quality Requirements, for general requirements for field inspection.

Owner will provide field inspection.

Inspect and test questionable coated areas in accordance with ________.

CLEANING

Collect waste material that could constitute a fire hazard, place in closed metal containers, and remove daily from site.

PROTECTION

Protect finishes until completion of project.

Touch-up damaged finishes after Substantial Completion.

Schedule - Paint Systems

Concrete, Concrete Masonry Units (CMU), Concrete Block, Brick Masonry:  Finish surfaces exposed to view, except _____.

Gypsum Board:  Finish surfaces exposed to view, except _____.

Plaster:  Finish surfaces exposed to view, except _____.

Wood:  Finish surfaces exposed to view, except _____.

Wood Cabinets:  Finish exposed and semi-exposed surfaces.

Steel Doors and Frames:  Finish surfaces exposed to view; MI-OP-3A, gloss.

Steel Fabrications:  Finish surfaces exposed to view and to concealed surfaces where required to conform to performance requirements and resist corrosion.

Galvanized Steel:  Finish surfaces exposed to view, except _____.

Shop-Primed Metal Items:  Finish surfaces exposed to view, except _____.

Finish the following items:

Elevator pit ladders.

Exposed surfaces of steel stairs and railings.

Mechanical equipment.

Electrical equipment.

[_____] equipment.

Wall Surfaces Under Vinyl Wall Covering:

Pipe and Duct Insulation Jackets:  Finish surfaces exposed to view.

- END OF SECTION