PROTOTYPING CHECKLIST

A Technical White Paper for Rapid Prototyping Professionals

Complete Fabrication Model Makers

2025 Edition

This checklist contains a large amount of information. The best way to get the highest quality prototypes in the fastest time is to call us and we can give advice based on 40 years of experience in the industry.

# Executive Summary

This white paper is a technical reference for the key decision points that come up during a rapid prototyping job, from getting the CAD file ready through to final surface finishing. Each checklist item is backed up with industry data, tolerance benchmarks, material specifications, and best-practice guidance based on real-world fabrication work.

Rapid prototyping covers a wide range of additive and subtractive manufacturing technologies (FDM, SLA, SLS, PolyJet, MJF, Carbon DLS, and CNC), and each one has its own constraints around geometry, resolution, material, and finish. Errors at any stage of preparation can lead to build failures, dimensional inaccuracy, excessive post-processing cost, or a complete rework.

Research by Wohlers Associates suggests that up to 37% of prototype failures come down to pre-processing errors, most of which are preventable through systematic file validation and parameter selection. A well-run prototyping checklist cuts rework rates by an estimated 25–40% and shaves 1–3 days off average lead time on typical production volumes.

# 1. CAD File Preparation

## 1.1 CAD Resolution and Triangle Count

All major prototyping processes use tessellated mesh formats (most commonly STL or OBJ) in which curved surfaces are approximated by triangular facets. The quality of that approximation is governed by two output parameters: chord height (sometimes called sag or deviation tolerance) and angular deviation.

A chord height of 0.01 mm to 0.05 mm is appropriate for most industrial prototypes. Tighter values produce smoother curved surfaces but generate exponentially larger file sizes and slower slice times. Angular deviation should typically be set between 0.5° and 1.0°.

| Application | Recommended Chord Height | Typical Triangle Count | Approx. File Size |
| --- | --- | --- | --- |
| Consumer product (visual) | 0.02 mm | 200k – 800k triangles | 10 – 40 MB |
| Mechanical fit part | 0.05 mm | 50k – 200k triangles | 3 – 10 MB |
| Jewellery / fine detail | 0.005 mm | 1M – 5M triangles | 50 – 250 MB |
| Large structural component | 0.1 mm | 20k – 100k triangles | 1 – 5 MB |

Overly high triangle counts slow slicing without improving print quality. The 'diminishing returns' threshold is generally reached below 0.02 mm chord height for any FDM or SLA system with a layer height above 0.05 mm.

## 1.2 Closed Surfaces (Watertight Geometry)

A valid printable mesh has to be topologically closed: every edge has to be shared by exactly two faces, and the mesh has to enclose a definable interior volume. Open shells, non-manifold edges, reversed normals, and intersecting bodies are the four most common geometry faults picked up during pre-processing.

Industry data from Materialise and Netfabb indicates that approximately 62% of raw CAD exports contain at least one mesh error. Auto-repair tools (Magics, Netfabb, Meshmixer) resolve the majority, but complex errors such as overlapping shells or inverted volumes require manual intervention.

- Reversed normals cause the slicer to misidentify inside and outside surfaces, leading to hollow walls or inverted features.

- Non-manifold edges (three or more faces meeting at one edge) create ambiguous geometry that most slicers cannot resolve.

- Internal voids left from boolean operations can trap uncured resin (SLA/DLS) or unsintered powder (SLS), requiring drainage holes.

## 1.3 Fit Tolerance

Fit tolerance defines the clearance between mating parts. Prototyping processes shrink, expand, or warp at characteristic rates that must be accounted for in the original design. Failure to apply process-specific fit allowances is one of the leading causes of assembly failure on first-article prototypes.

| Process | Typical Dimensional Accuracy | Recommended Clearance (slip fit) | Recommended Clearance (press fit) |  |
| --- | --- | --- | --- | --- |
| FDM (PLA/ABS) | ±0.2 – 0.5 mm | 0.3 – 0.5 mm per side | 0.0 – 0.1 mm per side |  |
| SLA / DLP | ±0.05 – 0.1 mm | 0.1 – 0.2 mm per side | −0.05 – 0.0 mm per side |  |
| SLS (Nylon PA12) | ±0.1 – 0.3 mm | 0.2 – 0.4 mm per side | 0.0 – 0.1 mm per side |  |
| PolyJet | ±0.025 – 0.05 mm | 0.05 – 0.15 mm per side | −0.025 – 0.0 mm per side |  |
| CNC Machined | ±0.01 – 0.05 mm | 0.02 – 0.05 mm per side | −0.01 – 0.02 mm per side |  |
| Carbon DLS | ±0.025 – 0.075 mm | 0.05 – 0.15 mm per side | −0.025 – 0.0 mm per side |  |

## 1.4 Boss Sizes

Bosses (cylindrical protrusions used to take screws, heat-set inserts, or snap-fit features) need process-specific sizing. Printed bosses behave differently from injection-moulded equivalents because of anisotropic strength and layer adhesion mechanics.

General design rules for printed bosses:

- Minimum boss outer diameter: 2.0× the fastener nominal diameter (e.g., M3 screw = 6 mm OD minimum).

- Wall thickness of boss: 0.8× the inner diameter minimum to prevent splitting under torque.

- Boss height: no more than 3× its outer diameter without gusset reinforcement.

- Heat-set insert bosses: bore diameter should match insert OD −0.2 mm for FDM, −0.1 mm for SLS.

- Carbon DLS bosses: bore tolerance is tighter than FDM. Apply −0.1 mm interference for press-fit inserts; isotropic parts give uniform pull-out strength in all orientations.

For M3 threaded inserts in FDM parts, a bore of 4.0 – 4.2 mm provides reliable pull-out strength above 250 N when installed with a controlled-temperature press or soldering iron at 200–220°C.

## 1.5 Paint Tolerance

Any surface that will receive a painted finish must incorporate dimensional compensation for coating thickness. Ignoring paint build-up is particularly consequential on mating faces, snap fits, and boss bores.

| Coating Type | Typical Thickness per Coat | Typical Total Build (2–3 coats) | Recommended Design Compensation |
| --- | --- | --- | --- |
| Aerosol primer | 0.03 – 0.06 mm | 0.06 – 0.18 mm | +0.1 mm on mating faces |
| Brush-applied enamel | 0.05 – 0.12 mm | 0.10 – 0.36 mm | +0.2 mm on mating faces |
| 2K polyurethane (sprayed) | 0.06 – 0.10 mm | 0.12 – 0.30 mm | +0.15 mm on mating faces |
| Powder coat | 0.06 – 0.20 mm | 0.06 – 0.20 mm (single pass) | +0.2 – 0.4 mm on threads/bores |
| Automotive lacquer | 0.04 – 0.08 mm | 0.08 – 0.24 mm | +0.1 mm on mating faces |

# 2. Build Parameters

## 2.1 Build Envelope Size and Part Positioning

The build envelope defines the maximum printable volume for a given machine. Parts have to fit within this volume, and where they sit inside it affects support structures, surface quality, and thermal distribution. A lot of machines also have accuracy gradients: parts at the centre of the bed are usually more accurate than those at the periphery.

| Technology | Representative Build Volume (XYZ mm) | Accuracy Gradient (centre vs. edge) |  |
| --- | --- | --- | --- |
| FDM (desktop) | 250 × 210 × 210 | ±0.1 mm vs. ±0.3 mm |  |
| FDM (industrial) | 900 × 600 × 900 | ±0.2 mm vs. ±0.5 mm |  |
| SLA (benchtop) | 290 × 160 × 400 | ±0.03 mm vs. ±0.1 mm |  |
| SLS industrial | 340 × 340 × 600 | ±0.1 mm vs. ±0.25 mm |  |
| PolyJet (J750) | 490 × 390 × 200 | ±0.025 mm vs. ±0.05 mm |  |
| MJF (HP 5200) | 380 × 284 × 380 | ±0.1 mm vs. ±0.2 mm |  |
| Carbon M2 (DLS) | 189 × 118 × 326 | ±0.025 mm vs. ±0.075 mm |  |
| Carbon M3 Max (DLS) | 310 × 196 × 372 | ±0.025 mm vs. ±0.075 mm |  |
| Carbon L1 (DLS) | 400 × 250 × 458 | ±0.025 mm vs. ±0.1 mm |  |

Nesting multiple parts in a single build is common in SLS and MJF because the powder bed supports all the geometry. In FDM and SLA, every additional part adds to total support volume and the risk of print failure. Carbon DLS handles nested builds well thanks to the continuous liquid-interface process: parts hang from the build platform with no powder bed to manage.

## 2.2 Build Orientation (Horizontal vs. Vertical)

Part orientation during the build is one of the highest-impact decisions in rapid prototyping. It directly affects mechanical strength, surface quality on critical faces, support volume, build time, and the risk of delamination or warping.

- Vertical build (Z-axis tall): makes the most of print area and reduces footprint, but increases anisotropy. Z-direction tensile strength in FDM can be 40–60% lower than XY-plane strength.

- Horizontal build (part laid flat): usually gives stronger parts and a better surface finish on top and bottom faces, but takes up more build plate area and often needs more supports for overhangs.

- 45° orientation: a common compromise that keeps support volume down and runs layer lines away from critical stress directions.

- Carbon DLS: because DLS produces isotropic parts via the continuous liquid-interface process, orientation is driven by support volume and A-face surface quality rather than by mechanical anisotropy. This is a real workflow advantage for structural parts.

For functional structural parts, orient so that the primary load path is parallel to the XY plane. A vertical (Z-axis aligned) FDM beam may fail at 40% of the load of the same geometry printed horizontally. This constraint does not apply to Carbon DLS parts.

| Orientation | Surface Quality (A-face) | Strength (Z-axis load) | Support Volume | Typical Use Case |
| --- | --- | --- | --- | --- |
| Flat / Horizontal | Excellent | High (XY plane load) | High | Visual show models, flat panels |
| Vertical / Upright | Good (sides), Poor (top) | Low | Low | Tall thin features, cylinders |
| 45° diagonal | Good | Medium | Medium | Functional brackets, clips |
| Custom (per feature) | Excellent on target face | Variable | Variable | Precision mating surfaces |

## 2.3 Material Choice

Material choice affects every downstream decision. It determines post-processing options, surface finish, mechanical properties, chemical resistance, and regulatory compliance. The main things to weigh up are: mechanical requirements, thermal environment, aesthetic requirements, and any end-use testing requirements.

| Material | Process | Tensile Strength | Heat Deflection Temp. | Best Use Case |
| --- | --- | --- | --- | --- |
| PLA | FDM | 37 – 60 MPa | 52 – 65°C | Visual models, low-stress parts |
| ABS | FDM | 30 – 45 MPa | 80 – 100°C | Functional housings, snap fits |
| ASA | FDM | 33 – 48 MPa | 95 – 108°C | Outdoor / UV-resistant models |
| PA12 (Nylon) | SLS / FDM | 45 – 55 MPa | 150 – 175°C | Functional mechanical parts |
| Standard Resin | SLA/DLP | 50 – 65 MPa | 46 – 58°C | High detail visual prototypes |
| Tough Resin (ABS-like) | SLA | 38 – 55 MPa | 45 – 60°C | Snap fits, living hinges |
| PETG | FDM | 48 – 53 MPa | 70 – 80°C | Transparent parts, food-contact |
| TPU / TPE | FDM / SLS | 25 – 50 MPa | 60 – 90°C | Gaskets, grips, flexible parts |
| PC (Polycarbonate) | FDM | 55 – 72 MPa | 110 – 130°C | High-temp enclosures, optics |
| Glass-filled PA12 | SLS | 70 – 85 MPa | 180 – 200°C | Structural, under-bonnet parts |
| RPU 70 / CE 221 | Carbon DLS | 40 – 50 MPa | 70 – 100°C | Functional prototypes, end-use parts, rigid housings |
| EPU 45 / EPU 44 | Carbon DLS | 4 – 8 MPa | - | Energy-return lattices, flexible/elastomeric functional parts |
| UMA 90 | Carbon DLS | 50 – 65 MPa | 55 – 65°C | High-detail rigid visual prototypes; comparable to SLA quality |

Carbon DLS materials are photopolymer resins run through Carbon's proprietary Digital Light Synthesis technology. The main production materials are RPU 70 (rigid polyurethane, high elongation-at-break, impact resistant), CE 221 (cyanate ester, high-temp up to 219°C HDT, used for under-bonnet and sterilisable housings), EPU 44/45 (elastomeric PU, very good energy return for lattice structures), UMA 90 (urethane methacrylate, fine detail with surface quality on a par with SLA), and MPU 100 (medical-grade white PU with USP Class VI and ISO 10993 certification, covered in Section 4.2).

## 2.4 Surface Finish

Surface finish is specified using Ra (arithmetic mean roughness) in micrometres (µm). Different prototyping processes and orientations produce characteristic Ra values, and post-processing steps can reduce these significantly.

| Process / Condition | As-printed Ra (µm) | After sanding (320 grit) | After vapour smoothing / priming |
| --- | --- | --- | --- |
| FDM – 0.2 mm layers | 12 – 30 | 3 – 8 | 1 – 4 |
| FDM – 0.1 mm layers | 6 – 15 | 2 – 5 | 0.8 – 2 |
| SLA – standard resin | 1 – 4 | 0.5 – 2 | 0.2 – 0.8 |
| SLS – PA12 | 8 – 20 | 2 – 6 | 1 – 3 |
| PolyJet – glossy mode | 0.5 – 1.5 | Not typically required | 0.1 – 0.5 |
| MJF – PA12 | 8 – 14 | 2 – 5 | 1 – 3 |
| Carbon DLS (RPU/UMA) | 1 – 3 | 0.5 – 1.5 | 0.2 – 0.6 |
| CNC machined (aluminium) | 0.4 – 3.2 | 0.1 – 0.8 | Not applicable |

Class-A automotive surfaces typically need Ra < 0.4 µm. Achieving this from FDM means at least 400-grit sanding, primer surfacer, wet flatting to 1200 grit, and polishing compound (around 4–8 hours of hand finishing on a typical panel). Carbon DLS parts come off the build at a much lower as-printed Ra than FDM, which cuts finishing labour significantly for visual-grade work.

## 2.5 Support Positions

Support structures are necessary for any overhanging geometry below the self-supporting angle of the process (typically 45° for FDM, 25–30° for SLA and Carbon DLS). Poorly planned supports cause surface damage on contact faces, increase post-processing time, and can introduce distortion when removed.

- Tree supports (FDM/SLA/DLS): touch the model at minimal points, which cuts witness marks and removal time.

- Block/lattice supports (FDM): stronger but leave larger contact scars; suitable for non-visible faces.

- Soluble supports (PVA/HIPS in FDM, wax-jet in PolyJet): allow complex internal channels and eliminate removal damage.

- SLS/MJF: powder acts as self-support; no dedicated support structures required for most geometries.

- Carbon DLS: supports are generated automatically by Carbon's print preparation software (Carbon Design Engine). Tips are fine, leaving minimal witness marks; supports come off by hand after washing. Flag critical A-surfaces in the job brief so the software can avoid them.

When specifying support positions, always identify A-surfaces (see Section 2.6) and configure supports to avoid contact with those faces. A minimum contact tip diameter of 0.6 mm and breakaway gap of 0.2 mm is recommended for SLA tree supports on visual surfaces.

## 2.6 A-Surface Identification

A-surfaces are the primary visible or functional surfaces of a prototype: the faces that will be seen, touched, or measured by the end client. Identifying A-surfaces at the CAD stage lets the print team optimise orientation (placing A-surfaces on the underside or towards the best-resolution axis), keep supports off those faces, and concentrate post-processing effort where it counts.

- Mark A-surfaces in the CAD model using a distinct colour, material designation, or annotation layer before exporting.

- Communicate A-surfaces explicitly in the job brief, with photographs or annotated renders if possible.

- For multi-part assemblies, identify primary, secondary and tertiary A-surfaces. Primary: seen in normal use. Secondary: visible on close inspection. Tertiary: internal or structural.

Studies by the Rapid Prototyping Journal show that projects with explicit A-surface designation reduce post-processing time by an average of 28%, as finishing effort is concentrated correctly rather than applied uniformly across all faces.

## 2.7 Build Layer Thickness / Resolution

Layer thickness directly controls vertical resolution, as-printed surface roughness on angled faces, and build speed. Thinner layers produce smoother results but increase build time and can reduce mechanical stability of very tall features.

| Process | Minimum Layer Thickness | Standard Layer Thickness | Maximum Layer Thickness | Time Impact (0.1→0.2 mm) |  |
| --- | --- | --- | --- | --- | --- |
| FDM | 0.05 mm | 0.1 – 0.2 mm | 0.4 mm | ~50% faster |  |
| SLA | 0.025 mm | 0.05 – 0.1 mm | 0.2 mm | ~50% faster |  |
| DLP | 0.025 mm | 0.05 – 0.1 mm | 0.15 mm | ~40% faster |  |
| SLS | 0.08 mm (fixed) | 0.1 mm (fixed) | 0.12 mm | Fixed, not adjustable |  |
| PolyJet | 0.014 mm (16 µm) | 0.027 – 0.032 mm | 0.032 mm | Minimal variation |  |
| MJF | 0.08 mm (fixed) | 0.08 mm | 0.08 mm | Fixed |  |
| Carbon DLS | 0.025 mm | 0.05 – 0.1 mm | 0.15 mm | ~40% faster |  |

## 2.8 File Type

File format affects geometry fidelity, colour/material information, and interoperability with slicing and post-processing software. Carbon DLS uses Carbon's proprietary .cbm slice format generated from STL or STEP inputs via the Carbon Design Engine. Customers can submit standard STL or STEP files; no special export format is needed.

| File Format | Primary Use | Supports Colour | Supports Multi-material | Max Recommended File Size |  |
| --- | --- | --- | --- | --- | --- |
| STL (Binary) | Universal prototyping | No | No | 200 MB |  |
| STL (ASCII) | Debugging only | No | No | 50 MB |  |
| OBJ + MTL | Colour models, visual review | Yes (texture map) | Partial | 500 MB |  |
| 3MF | FDM (Bambu, Prusa, MakerBot) | Yes | Yes | 200 MB |  |
| AMF | Multi-material, colour | Yes | Yes | 200 MB |  |
| STEP / STP | CNC machining, hybrid workflows | No | No | N/A (native CAD) |  |
| VRML / WRL | Full-colour PolyJet | Yes | Yes | 1 GB |  |

STL binary format remains the most universally supported export. 3MF is rapidly becoming the preferred standard for FDM workflows due to its compact size and ability to carry print settings alongside geometry.

## 2.9 Build Speed

Build speed is a composite variable affected by layer count, layer area, material deposition rate, and any post-exposure or curing steps. Carbon DLS is unusual in that it uses a continuous photopolymerisation process rather than discrete layer-by-layer exposure: the build platform pulls continuously upward from the resin pool, eliminating the inter-layer separation steps that limit conventional DLP and SLA speeds. That makes Carbon DLS the fastest single-part option for complex photopolymer geometries.

| Process | Typical Build Speed (vertical Z) | Notes |
| --- | --- | --- |
| FDM (0.2 mm layer, 60 mm/s) | 20 – 60 mm/hour | Varies greatly with infill and perimeter count |
| FDM (0.2 mm layer, 200 mm/s) | 50 – 150 mm/hour | High-speed machines (Bambu X1, Voron) |
| SLA (standard) | 15 – 30 mm/hour | Exposure time per layer is limiting factor |
| MSLA/DLP | 30 – 100 mm/hour | Full-layer flash exposure; faster than SLA |
| SLS | 10 – 20 mm/hour | Includes powder deposition and sintering |
| PolyJet | 25 – 55 mm/hour | Slows significantly with support volume |
| MJF | 3,500 cm³/hour (volumetric) | Near-constant regardless of geometry complexity |
| Carbon DLS (M2) | 50 – 150 mm/hour | Continuous liquid-interface process; no discrete layer pauses, fastest photopolymer throughput per part |
| Carbon DLS (L1) | 40 – 100 mm/hour | Large-format production; optimal for mid-volume end-use runs |

For time-critical projects, MJF and Carbon DLS give the fastest throughput per unit volume. FDM speed scales poorly with complexity: a part that needs dense supports may take 3× longer than an equivalent open geometry at the same layer height. Carbon DLS throughput is largely geometry-independent, which makes it efficient for highly complex or organic forms.

# 3. Painting and Surface Finishing

## 3.1 Paint-on-Paint Finish

Achieving a high-quality painted finish on rapid prototypes requires systematic layering: substrate preparation, primer, colour coats, and clear lacquer. Each stage must be allowed to cure fully before the next is applied, as premature recoating causes solvent trapping, blistering, and adhesion failure.

Recommended paint system for prototype models:

- Step 1 - Substrate preparation: sand printed surface to 240–400 grit, then degrease with isopropanol or acetone (use IPA only on SLA, resin, and DLS parts).

- Step 2 - Adhesion promoter (optional but recommended for PP-like or waxy surfaces): apply 1 thin coat, allow 10 minutes flash-off.

- Step 3 - Primer surfacer (2K or high-build aerosol): apply 1–2 medium coats at 20–25 cm. Flash-off 30 minutes between coats. Full cure: 60 minutes at 20°C or 30 minutes at 60°C.

- Step 4 - Wet flat primer with 800 grit. Re-prime any sanded-through areas.

- Step 5 - Colour coat (2K polyurethane or automotive base coat): 2–3 medium coats, 10–15 minutes flash between coats.

- Step 6 - Clear lacquer / top coat: 2 coats. Full cure 16–24 hours before handling.

2K (two-component) polyurethane systems provide superior hardness (typically 2H pencil hardness) and chemical resistance compared to single-pack systems. They are strongly recommended for any prototype that will undergo functional testing or client handling.

Carbon DLS parts have a smooth, slightly waxy surface from the process oxygen-inhibition zone. A light scuff with 400-grit before primer is enough; the as-printed Ra of 1–3 µm means DLS parts usually need one fewer sanding stage than FDM equivalents.

## 3.2 Paint Thickness and Its Dimensional Implications

Built-up paint has to be treated as a structural addition to the model surface. For display models that's rarely a problem, but for any part that has to assemble with another component, even a sub-0.1 mm film can cause interference.

| Paint System | Film Thickness per Coat (µm) | Full System Thickness (µm) | Dimensional Impact (per mating surface) |
| --- | --- | --- | --- |
| Aerosol primer only | 30 – 60 µm | 60 – 120 µm | 0.06 – 0.12 mm |
| Primer + 1K colour | 80 – 130 µm | 80 – 130 µm | 0.08 – 0.13 mm |
| Primer + 2K colour + lacquer | 120 – 250 µm | 120 – 250 µm | 0.12 – 0.25 mm |
| High-build primer + full 2K system | 200 – 400 µm | 200 – 400 µm | 0.20 – 0.40 mm |
| Powder coat (single pass) | 60 – 200 µm | 60 – 200 µm | 0.06 – 0.20 mm |

For all assemblies receiving paint, design nominal clearances should be increased by the full system thickness on each painted mating surface. Threads, bores, and snap-fit features on painted prototypes should be masked before painting or re-drilled/tapped post-cure.

# 4. Medical Grade Requirements

## 4.1 Regulatory Framework

Prototypes intended for use in medical contexts (handled by clinical staff, in contact with patients, used in surgical simulation, or submitted as part of a regulatory filing) have to meet a more demanding set of material and process requirements than general-purpose prototypes.

The principal regulatory frameworks governing medical device prototypes are:

- ISO 10993 (Biocompatibility): defines a series of tests for cytotoxicity, sensitisation, irritation, and systemic toxicity for materials intended for patient contact.

- ISO 13485: the quality management system standard for medical device manufacturing. Prototyping facilities supplying to regulated customers may need certification.

- FDA 21 CFR Part 820 (US): Quality System Regulation for medical devices including prototypes used in pre-submission testing.

- EU MDR 2017/745: the Medical Device Regulation governing devices placed on the European market, including rules on materials and testing evidence for regulatory submissions.

Not all rapid prototyping materials are biocompatible. Verification of ISO 10993 compliance has to come from the material manufacturer; it can't be assumed based on material type alone.

## 4.2 Biocompatible Materials for Prototyping

Only a small subset of prototyping materials carry validated biocompatibility testing. The choice should be made together with the client's regulatory team, as the right testing tier depends on the type and duration of patient contact.

| Material | Process | ISO 10993 Status | Contact Type Supported | Notes |
| --- | --- | --- | --- | --- |
| MED610 (PolyJet) | PolyJet | ISO 10993-5/10 certified | Short-term skin & mucosal | Stratasys validated; clean separately |
| MED625FLX (PolyJet) | PolyJet | ISO 10993-5/10 certified | Flexible implant simulation | Not for implantation |
| BioMed Clear (SLA) | SLA/DLP | ISO 10993-5 (cytotoxicity) | Short-term contact | Formlabs validated |
| BioMed Durable (SLA) | SLA/DLP | ISO 10993-5/10 certified | Prolonged skin contact | Formlabs medical range |
| MPU 100 (Carbon DLS) | Carbon DLS | USP Class VI; ISO 10993-5,-10,-23 | Skin-contact, single-use instruments, drug-contact | FDA Master File available; white, rigid; EtO/e-beam/gamma sterilisable; comparable to medical ABS |
| PA 2200 (EOS SLS) | SLS | Biocompatible (class I) | Non-contact / enclosures | Check current EOS data sheet |
| PEEK (FDM/CNC) | FDM (Apium) / CNC | Long-term implant data | Implant-grade applications | Requires validated machine |
| 316L Stainless (SLM) | Metal SLM | ISO 10993 tested | Surgical instruments | Post-process and passivate |

Carbon's MPU 100 is currently the only DLS material with full medical-grade certification. It runs on Carbon M2, M3 Max, or L1 machines via Carbon's Digital Light Synthesis process, producing isotropic, fully dense white parts at a feature resolution suited to single-use instruments, diagnostic equipment components, and skin-contact devices. The FDA Master File cuts the documentation burden for customers going through 510(k) or PMA submissions.

## 4.3 Post-Processing and Sterilisation

Medical prototype post-processing must consider sterilisation compatibility. Not all materials survive common sterilisation methods, and sterilisation can alter dimensional accuracy and mechanical properties.

| Sterilisation Method | Max Temperature | Compatible Materials | Effect on Printed Parts |
| --- | --- | --- | --- |
| Autoclave (steam, 134°C) | 134°C | PEEK, metal SLM, glass-filled PA | Most polymers warp or degrade, NOT suitable for FDM/SLA |
| EtO (ethylene oxide gas) | < 60°C | Most polymers, Carbon MPU 100 | Residual EtO must outgas; cycle adds 24–48 hrs |
| Gamma radiation | Ambient | PA12, PEEK, PC, metals, Carbon MPU 100 | Can cause yellowing or embrittlement in some resins; MPU 100 compatible |
| VHP (vaporised H₂O₂) | < 40°C | Most polymers | Minimal dimensional impact; preferred for SLA/PolyJet |
| UV / plasma | Ambient (surface only) | All | Surface decontamination only, not terminal sterilisation |

## 4.4 Traceability and Documentation Requirements

Medical projects typically require a higher level of build traceability than standard prototyping. The following documentation should be generated and retained for all medical-grade builds:

- Material batch/lot number and supplier certificate of conformity.

- Machine calibration records at time of build.

- Build log (start/end time, layer count, ambient conditions).

- Post-processing log (cleaning agent, duration, operator, date).

- Dimensional inspection report (CMM or calliper with measurement positions defined).

- Biocompatibility data sheets from material supplier.

If the prototype will be submitted as supporting evidence in a regulatory filing (e.g., FDA 510(k) or EU MDR Technical File), the fabrication record must be maintained for a minimum of 5 years and must include a clear description of any deviations from the approved process.

# 5. Rapid Reference Checklist Summary

Use this consolidated checklist at each project stage to confirm all critical parameters have been reviewed before submitting a build job.

| # | Checklist Item | Key Action | Status |  |
| --- | --- | --- | --- | --- |
| 1 | CAD resolution & triangle count | Set chord height 0.01–0.05 mm; verify file size is manageable | ☐ |  |
| 2 | Closed / watertight surfaces | Run mesh repair; zero open edges, no non-manifold geometry | ☐ |  |
| 3 | Fit tolerance | Apply process-specific clearance per fit type (see table) | ☐ |  |
| 4 | Boss sizes | OD ≥ 2× fastener dia.; wall ≥ 0.8× bore; height ≤ 3× OD | ☐ |  |
| 5 | Paint tolerance | Add 0.1–0.4 mm to mating faces per paint system chosen | ☐ |  |
| 6 | Build envelope & position | Part fits with 5 mm clearance to envelope boundaries | ☐ |  |
| 7 | Build orientation | A-surface faces down or towards highest resolution axis | ☐ |  |
| 8 | Material choice | Verified against mechanical, thermal & regulatory needs | ☐ |  |
| 9 | Surface finish spec | Ra target defined; post-processing steps agreed | ☐ |  |
| 10 | Support positions | Supports excluded from A-surfaces; soluble supports if required | ☐ |  |
| 11 | A-surface identification | Annotated in CAD and communicated to build team | ☐ |  |
| 12 | Layer thickness / resolution | Selected to balance quality and build time for application | ☐ |  |
| 13 | File type | Binary STL or 3MF confirmed; file validated pre-submission | ☐ |  |
| 14 | Build speed / schedule | Estimated build time reviewed against project deadline | ☐ |  |
| 15 | Paint-on-paint system | Process and product system agreed; mating faces masked | ☐ |  |
| 16 | Paint thickness | Dimensional compensation applied to relevant features | ☐ |  |
| 17 | Medical grade requirements | ISO 10993 materials confirmed; sterilisation method compatible; Carbon DLS MPU 100 for single-use | ☐ |  |
| 18 | Carbon DLS process check | Confirm part compatible with DLS continuous print process; no trapped volumes; drain holes for hollow sections | ☐ |  |

# References and Further Reading

- Wohlers Associates, Wohlers Report 2024: Additive Manufacturing and 3D Printing State of the Industry.

- ISO 10993 Series, Biological evaluation of medical devices (ISO, Geneva).

- ISO 13485:2016, Medical devices: Quality management systems.

- Materialise, Magics User Guide and STL Repair Reference.

- Stratasys, PolyJet Technology Overview and MED610 Material Data Sheet.

- Formlabs, BioMed Resin Technical Documentation and ISO 10993 Reports.

- Carbon, Inc., MPU 100 Technical Data Sheet, Biocompatibility Test Summary, and FDA Master File documentation.

- Carbon, Inc., DLS Technology Overview; M2, M3 Max, and L1 Machine Specifications (current edition).

- Rapid Prototyping Journal, Thompson et al., 'Effect of A-surface designation on post-processing efficiency', Vol. 29 No. 4, 2023.

- EOS GmbH, PA 2200 Material Data Sheet and Processing Guidelines.

© 2025 Complete Fabrication Model Makers. All rights reserved.